## Slide 1: 20 T – Cos(𝛳) Designs
G. Vallone1, P. Ferracin1, V. Marinozzi2, Y. Pansari1
03-August-2022
1LBNL, 2FNAL
General MDP Meeting

## Slide 2: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 3: Introduction
We want to compute the mechanical stresses for 20T cos(ϑ) design
  CT I: 4 Bi2212 layers
  CT II: 2 Bi2212 layers
We select CT II as best ($) design
CT I
CT II

## Slide 4: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 5: Magnetic Field
ANSYS magnetic model
  20 T central field at I = 13 kA, with the iron yoke
  Results consistent with the Roxie model
  Used to extract e.m. forces for mechanical study
B, T
No Iron
B, T
With Iron

## Slide 6: Magnetic Model Results
Reasonable Lorentz stress in all layers
Assumed mechanical limits:
  Bi2212 (layer 1, 2): 125 MPa
  Nb3Sn (layer 3 to 6): 175 MPa
Layer | Bpeak | jo | Lorentz Stress
/ | T | A/mm2 | MPa
1 | 20.2 | 305 | -81
2 | 18.1 | 305 | -119
3 | 16.0 | 215 | -137
4 | 13.0 | 215 | -133
5 | 11.7 | 398 | -144
6 | 11.0 | 398 | -128

## Slide 7: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 8: Modeling assumptions
Coil modelled as linear elastic
Rigid structure around the outer coil
Rigid winding poles, no prestress
Frictionless contact on the intercoil insulation
Glued contact on the interlayers
Rigid
Structure
Separation
Allowed
Intercoil
Frictionless
Contact
Interlayer
Bonded Contact

## Slide 9: Rigid Structure
Max stress, mid plane:
  Radial: 183 MPa, Azimuthal: 353 MPa
  Inner radius stress due to coil deformability
Lorentz stress on layer 1 was only 80 MPa, but bending…
Radial
Stress
Azimuthal
Stress

## Slide 10: Rigid Structure, Intercepting (Fixed intercoil)
Intercepting structure - intercoil fixed (u=0)
  Removes bending and accumulation of radial forces
140 MPa radial, 155 MPa azimuthal
With perfect interception between coils, layer 2 has to be stress managed
  Radial+azimuthal stresses exceed limits
Radial
Stress
Azimuthal
Stress

## Slide 11: Rigid Structure, Intercepting (Fixed intercoil+interlayer)
Intercepting structure – intercoil and interlayers fixed (u=0)
Even with perfect interception between layers, layer 2 has to be stress managed
101 MPa radial, 147 MPa azimuthal
Radial
Stress
Azimuthal
Stress

## Slide 12: Result Summary - Intercepting
In red stresses that are over conductor limits
Rigid intercoil + interlayer close to Lorentz stress

## Slide 13: Rigid Structure, Layer 2 Stress Managed
If we stress manage L2, do we need to do the same on L1?
  Is the additional stiffness from stress management enough to remove the stress peaks in L1?
  Model with L2 in stainless steel (coil and spacers)
179 MPa radial, 302 MPa azimuthal
Layer 1 has to be stress managed
  Azimuthal stresses exceed limits
Radial
Stress
Azimuthal
Stress

## Slide 14: Result Summary – Stress Management
We can repeat the exercise ‘stress-managing’ only some layers (x means stress managed)
Stress managed solutions show that in reality we might be able to stress manage only layer 1, 2, but layer 3 is very close to the limit
  Field is low, but stress might become higher when outer structure and stress management are not ‘ideal’
  On the other hand, coil 3 can work with no stress management

## Slide 15: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 16: Steel Intercoil – Magnetic Field
5 mm thick stainless steel intercoil shim/structure
Current ramped up to get back to 20 T
  From 13 kA to 13.45 kA
  Lower margin but this is a ‘mechanical’ test
Old
New
Design 2, I = 13.5 kA, B = 20 T |  |  | 
Layer | Bpeak | jo | Lorentz Stress
/ | T | A/mm2 | MPa
1 | 20.3 | 317 | -84
2 | 18.1 | 317 | -123
3 | 15.5 | 223 | -139
4 | 12.8 | 223 | -136
5 | 11.5 | 413 | -148
6 | 10.8 | 413 | -134
Design 1, I = 13.0 kA, B = 20 T |  |  | 
Layer | Bpeak | jo | Lorentz Stress
/ | T | A/mm2 | MPa
1 | 20.2 | 305 | -81
2 | 18.1 | 305 | -119
3 | 16.0 | 215 | -137
4 | 13.0 | 215 | -133
5 | 11.7 | 398 | -144
6 | 11.0 | 398 | -128

## Slide 17: Case A – Steel ‘Open Rings’
Intercoil shims open at 90°
Azimuthal: 331 MPa, Radial: 173 MPa
  Does not solve the bending problem on the first layer
  Similar results with closed rings (shells)
Radial
Stress
Azimuthal
Stress

## Slide 18: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 19: A test with an SMCT ‘Design’ - Assumptions
A ‘test’ design obtained adding 5 mm thick stainless steel spars to the CT design
  Mandrel = spar + wedges (ribs)
  Frictionless contacts between coil and mandrels
  Frictionless contact between mandrels
  Layer 5 and 6 impregnated, with no stress management
Rigid
Structure
Interlayer
Bonded Contact
Frictionless
Contact

## Slide 20: A test with an SMCT ‘Design’ - Results
Limit stresses exceeded on the inner coil upper right edges
Coil 2 and 3 are ok
Eqv.
Stress
Eqv.
Stress

## Slide 21: A test with an SMCT ‘Design’
The high stresses are due to radial forces and contact with the second layer spar
This result suggests that we need more radial support
Eqv.
Stress

## Slide 22: SMCT Designs – Mid-plane rib
Adding a mid-plane ‘shim/rib’
High stresses in layer 1 and 2
  The rib does not solve the issue
Layer 3 to 6 are fine
Eqv.
Stress
Eqv.
Stress

## Slide 23: SMCT Designs – Aligned Wedges
Aligned wedges near the mid-plane
Inner coil still not working
Eqv.
Stress
Eqv.
Stress

## Slide 24: SMCT Designs – Shared Mandrel
New design with a shared mandrel for layer 1 and 2 (an idea by Sasha)
Stresses are worse in this configuration, but probably this is due to this particular coil design
Eqv.
Stress
Eqv.
Stress

## Slide 25: Design Comparison
None of the proposed designs solves the stress issues in the inner coil
  Probably we need more ribs in the first 2 layers
  A magneto/mechanical optimization might help
Test
Mid Plane Rib
Aligned Ribs
Shared Mandrel
seqv.,Pa

## Slide 26: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 27: Conclusion
Solution with rigid intercoil shims shows that layer 2 requires stress management (both radial and azimuthal)
Solution with ‘stress-managed’ layer 2 shows that also layer 1 needs stress management
  Layer 1 sees high azimuthal stresses even when introducing thick intercoil shims
  Layer 3 is very close to the stress limits, might also need stress management
  Layers 4, 5 and 6 seem feasible also with no stress management (with a rigid structure around)
Thick steel intercoils do not provide enough stiffness to reduce the stresses in a CT design
Mixed SMCT and CT designs are being considered
  No viable solution for the moment, optimization in progress

## Slide 28: Extra

## Slide 29: Rigid Structure and Coil
Coil modelled as linear elastic, E = 1e4 GPa
  ~226 MPa radial, 195 MPa azimuthal
  REMOVE
Radial
Stress
Azimuthal
Stress

## Slide 30: Rigid Structure, Intercepting (Rigid intercoil)
Coil modelled as linear elastic, E = 20 GPa
Intercepting structure, rigid intercoil (E=1e7 GPa)
~127 MPa radial, 248 MPa azimuthal
Should try with thicker intercoil
IN EXTRA / Non funziona il modello (contatti?)

## Slide 31: Case 0 – Rigid Intercoil
Rigid 5 mm thick intercoil shells (locked on x=0)
Azimuthal: 163 MPa, Radial: 154 MPa
Not super promising – reality will be worse

## Slide 32: Case B – Steel Shells
Intercoil shims closed at 90° (shell design)
Azimuthal: 325 MPa, Radial: 167 MPa
  Similar to open rings and more complicated to assembly / not worth considering

## Slide 33: Case C – Steel Collars – Coil Impregnated
Intercoil shims closed at 90° (shell design)
Coils impregnated together
Still does not work

## Slide 34: SMCT-CT hybrid: v17
2 layer HTS, 4 layer LTS
Strands: 0.9 – 1.1 – 0.8 mm, 40 – 44 – 35
Cable width: 20.65 – 26.82– 15.51 mm
Stabilizer/Superconductor: 3 – 1 – 1.2
Coil width: 158 mm
Current: 14200 A
Peak field: 20.8 – 16.26 – 13.36 T
Margin: 84.4 – 85.3 – 85.6 %
Jcu on LTS: 1479 A/mm2

## Slide 35: SMCT-CT hybrid: v18
2 layer HTS, 4 layer LTS
Strands: 0.9 – 1.1 – 0.8 mm, 40 – 44 – 35
Cable width: 20.65 – 26.82– 15.51 mm
Stabilizer/Superconductor: 3 – 1 – 1.2
Coil width: 158 mm
Current: 14200 A
Peak field: 21.2 – 16.23 – 13.09 T
Margin: 84.9 – 85.2 – 84.3 %
Jcu on LTS: 1479 A/mm2