## Slide 1
Overview of LWR and Advanced Reactor Fuel Forms
02/28/2022
Sebastian Schunert
Idaho National Laboratory – Reactor Physics Methods and Analysis

## Slide 2: Requirements for Nuclear Fuel for Power Production
Neutronics: Critical under operating conditions with margin for burnup & power level changes
(excess reactivity * for PWRs 0.3 dk/k, 30,000 pcm)
Thermal-hydraulics: fuel must be coolable
Fuel performance: withstand harsh reactor conditions for reasonable duration & retain fission products
Chemistry: Chemical compatibility with moderator, coolant, structural materials
Chicago pile 10th layer [1]
Does CP1 make the cut?
*

## Slide 3: Fuel – Moderator – Coolant: Mix & Match
Thermal reactors
Fast reactors
Fuels
U, Pu, Th
Enrichment
Metal, Ceramic, Dissolved, TRISO
Moderator
Graphite, Beryllium,
H20, D20, Hydrites (ZrH), Flibe
Coolant
Liquid metals, Molten salts, Water, Gas, Heat pipes
Light water reactor
5% enriched UO2 rods
H20 coolant & Moderator
Fast Molten Salt Reactor (MSFR)
U-Pu-Th dissolved in molten LiF:
LiF-(U,Pu)F3-ThF4
Fluoride salt-cooled high-temperature reactor (FHR)
TRISO fuel in pebbles HALEU (<20% enriched)
Molten salt coolant (Flibe)
Graphite moderator [some moderation from Flibe]
Geometry: homogeneous, dissolved, dispersed, plate, rods, pebbles

## Slide 4: Mix & Match
RBMK (graphite moderated BWRs)
1.8% enriched UO2
Graphite moderated
H20 cooled
Positive power coefficients of reactivity
Metal fuel in Light water reactor
Metallic U
H20 cooled & moderated
Water oxidizes metallic fuel
Cladding failure is severe!
Power reactor without coolant?
Ultrasmall high-temperature
UC or UN CERMET fuel
Graphite moderated
Conduction + radiation + PV
Ref [2]

## Slide 5: Genealogy of Nuclear Reactors
Thermal
Fast
H20
D20
Graphite
Spectrum
Moderator
Coolant
Fuel
form
PWR
BWR
VVER
*Advanced Test Reactor
**UN [Westinghouse design], MOX or metallic fuels possible
CANDU
PHWR
Molten salt
Gas
He, H2
UO2 5%
pins
UO2 0.7%
pins
U3O8 94% in Al plates
ATR*
Not an exhaustive list!
HALEU TRISO in pebbles
HALEU TRISO in cylinders
Pebble Bed Reactors
Prismatic
Gas-cooled
Reactors
HALEU TRISO in pebbles
Dissolved
FHR
MSRE
Sodium
Lead
Salt
U Metal
UO2**
Sodium fast reactor
(EBR-II)
Lead cooled fast reactor
Dissolved
Fast pool-type MSRs

## Slide 6: Why so many reactor concepts?
Reactor types have advantages and disadvantages and no one reactor is perfect for every need!
PWR
  High power density, relatively low fuel enrichment, economy of scale, water is not toxic, transparent, liquid at room temperature & pressure
  Require active safety systems, pressurized, low outlet temperatures (330ºC), difficult fuel reprocessing, relatively small discharge burnup, small margin to boiling, generates H2 from cladding
Gas cooled pebble bed reactors
  Passively safe, deployable at moderate powers (100 MW), high outlet temperatures (750ºC), high discharge burnup, continuous refueling and low excess reactivity
  HALEU is required, Low power density, pressurized, no fuel reprocessing, create dust during operation
Sodium fast reactors
  Passively safe, supports fuel reprocessing, decent outlet temperature (550ºC), atmospheric or near atmospheric pressure, high discharge burnup, high power density
  HALEU is required, sodium reacts with air & water, metal fuel poses fuel performance issues

## Slide 7: Example 1: Pressurized water reactor (Gen II)
Ceramic UO2 fueled, light water moderated
Square assemblies (20 cm across), 17x17 pins (D = 0.94 cm)
High pressure (15.5 MPa) keeps most water from boiling (yet some channels boil!)
LWRs are mostly used for grid scale electricity production with once-through fuel cycles
Quantity | Value
Spectrum | Thermal
Power | ~3,000 MWth
Average core power density | ~100 MW/m3
Maximum burnup | 62.5 MWd/kg
Fuel | 5% enriched UO2
4 m
Ref [3]
Ref [5]
20 cm
x-y view of the core
Ref [4]

## Slide 8: Example 2: Sodium Cooled Fast Reactor – EBR-II
Ref [6]
3m
Metal fuel – sodium cooled breeder reactor
Integral (no direct pipes out of vessel) pool type concept
Hexagonal assemblies (6 cm across), fuel pins (D = 0.37 cm)
Phase 1: technological demonstration of complete breeder power plant + reprocessing of metallic fuel
Phase 2: demonstrate the integral fast reactor with a focus on material’s testing & safety transients
Quantity | Value
Spectrum | Fast
Power | ~60 MWth
Driver fuel power density | ~400 MW/m3
Typical burnup | 100 MWd/kg
Driver fuel | 95 wt% U (62.5% enriched) + 5% Fissium*
Ref [7]
x-y view of the core + blanket
x-y view of driver
assembly
axial view of driver
assembly
Core, ~ 1ft
6 cm
30 cm
Ref [7]
Ref [7]
* Fissium: metal fuel + small amount of fission products

## Slide 9: Example 3: Pebble Bed Reactor – XE-100
4m
~0.8 mm
XE-100 is X-energies ARDP design
200 MWth Helium cooled pebble bed reactor
Special feature of PBRs is online refueling, pebbles move through the core while being irradiated
Fuel:
  Several 100,000 pebbles in the core
  Pebble contains thousands of tristructural
  isotropic particles (TRISO)
  TRISOs are extremely robust:
  retain fission products for longer than
  300 h at 1800C
Quantity | Value
Spectrum | Thermal
Power | ~200 MWth
Average core power density | ~4 MW/m3
Typical burnup | 160 MWd/kg
Fuel | 15.5% enriched UCO TRISO in graphite pebbles
*Note: fuel enrichment and fuel type (UO2 vs. UCO) varies between designs and operational phase
Ref [8]
Ref [9]
Fuel
Buffer
IPyC
SiC
OPyC

## Slide 10: Example 4: Pool-type Fast Molten Salt Reactor
Pictures are all from Ref [13]
Design based on the molten salt fast reactor (MSFR) concept initially developed at CNRS (European conceptual design)
MSFR is a very big machine compared to other MSRs
Very simple design:
  Pool of molten salt with dissolved fuel
  Molten salt flows into reactor cavity most of the power is created
  16 pump & heat exchanger legs around the core
  Online reprocessing of fission products
Fast pool-type MSRs can be designed as breeders (Th and U) or for burning transuranics
Salt can be fluoride or chloride based
  LiF: fluoride is chemically reactive, Li creates Tritium
  UCl3 – NaCl, Cl is a neutron absorber
Big R&D need: Corrosion & material compatibility!
Quantity | Value
Spectrum | Fast
Power | ~3,000 MWth
Average core power density (per salt volume) | ~350 MW/m3 (167 MW/m3)
Typical burnup | Very high
Fuel | LiF-ThF4-(233U or enrU)F4 or LiF-ThF4-(Pu-MA)F3 with 77.5 mol% LiF
2.5m

## Slide 11: Where do fission products matter for reactor engineering?
Example 1: Reactivity effects when reactor power changes - Xenon pit
Example 2: Fission products’ chemical interaction with the clad after going into contact (fuel-cladding-chemical-interaction, FCCI)
Example 3: Source term in TRISO fuel – diffusion of fission products through TRISO layers
Honorable mention: Decay heat (important but unfortunately not enough time)

## Slide 12: Fission Product Impact 1: Xenon pit
Xenon-135 is a strong neutron absorber
It is created by fission & decay from I-135
During reactor steady-state its level remains constant
What happens when power/flux levels change (say drop)?
  If power drops, both direct creation and destruction reduce, but indirect reduction reduces slower
  Initial buildup and then slump of Xe-135
  This has significant reactivity consequences
Xe pit occurred before Chernobyl accident and led the operator to remove all control rods
Relevant during power changes in reactors – not important for base load but very important for load following
Issue for all thermal reactors
Fission
135I
135Xe
135Cs
Simplified Xe decay scheme
Ref [14]

## Slide 13: Fission Product Impact 2: Fuel-Cladding-Chemical-Interaction
SFR fuel: Metallic U-Fis with stainless-steel cladding & sodium bond
Metallic fuel swells significantly under irradiation => cladding failure if fuel contacts clad before fission gas release (FCMI)
Reduce smear density to release fission gases before cladding contact
This creates Lanthanide fission product pathways
Lanthanides form low melting eutectics at the pellet cladding interface => cladding failure
Ref [10]
Fuel
Sodium
Cladding
Gas bubbles
Cracks
Cladding
Smear density =
Contact + Stress
FCMI
FCCI
Fission gas release
Lanthanide migration paths

## Slide 14: Fission Product Impact 3: TRISO Fission Product Retention
Nuclear fuel should retain fission products from entering the coolant as much as possible
Traditionally, fuel matrix + cladding serve that purpose
For TRISO fuel, the TRISO layers provide that function
Fission products: Sr-90, Ag-110, Cs-137 & 134
How well do TRISOs retain fission products?
AGR-1 reported 0 TRISO failures out of 300,000 TRISOs
Ref [12]
Sr is retained by SiC & Kernel but Ag is only retained by the SiC => need to avoid SiC failure!
Fuel
Buf
PyC
PyC
SiC
FP
Ref [11]
T>1600C!!
Large Ag release
Everything else is retained

## Slide 15: Summary and Conclusion
Power reactors come in a variety of shapes and sizes because no single concept fits all needs
A variety of fuel forms is used: ceramic, metallic, TRISO, dissolved in molten salts
With different fuel forms come different challenges to handle fission products – think FCCI in metallic fuel & retention in TRISOs
Some challenges stemming from fission products are common to many reactors: Xenon pit is an example for all thermal reactors
Data needs in the future will not just require fission product yields but also uncertainties as we include uncertainties in our designs

## Slide 17: References
[1] https://en.wikipedia.org/wiki/Chicago_Pile-1, ENERGY.GOV, Public domain, via Wikimedia Commons
[2] Naiki Kaffezakis et al., High temperature ultra-small modular reactor: Pre-conceptual design, Annals of Nuclear Energy 141, https://doi.org/10.1016/j.anucene.2020.107311
[3] Public Domain, https://commons.wikimedia.org/w/index.php?curid=475349
[4] Forget, Benoit, Smith, Kord, Kumar, Shikhar, Rathbun, Miriam, and Liang, Jingang. Integral Full Core Multi-Physics PWR Benchmark with Measured Data. United States: N. p., 2018. Web. doi:10.2172/1432668, https://www.osti.gov/servlets/purl/1432668
[5] https://commons.wikimedia.org/wiki/File:Nuclear_fuel_element.jpg#/media/File:Nuclear_fuel_element.jpg
[6] By Federal Government of the United States - Shutdown and closure of the experimental breeder reactor - II, Argonne National Laboratory, ANL/ENT/CP-106386, Public Domain, https://commons.wikimedia.org/w/index.php?curid=16917477
[7] T. Fei at al.. “Neutronics Benchmark Specifications for EBR-II Shutdown Heat Removal Test SHRT-45R – Revision 1”, https://publications.anl.gov/anlpubs/2018/05/143362.pdf
[8] Hans Gougar, “High Temperature Gascooled Reactor - History, Physics, Design Features”, INL/MIS-19-52882-Revision-0 https://inldigitallibrary.inl.gov/sites/sti/sti/Sort_24839.pdf
[9] https://www.energy.gov/ne/articles/triso-particles-most-robust-nuclear-fuel-earth
[10] Yi Xie, “Lanthanide Migration and Immobilization in Metallic Fuel ”, INL/JOU-18-51305-Revision-0, https://inldigitallibrary.inl.gov/sites/sti/sti/Sort_7248.pdf
[11] Dave Petti, “A Summary of the Results from the DOE Advanced Gas Reactor (AGR) Fuel Development and Qualification Program”, INL/EXT-16-40784 https://inldigitallibrary.inl.gov/sites/sti/sti/7323666.pdf
[12] J. Hales, “Modeling fission product diffusion in TRISO fuel particles with BISON”, https://www.osti.gov/biblio/1829987, https://www.osti.gov/servlets/purl/1829987
[13] M. Allibert et al., “Molten salt fast reactors”, Handbook of Generation IV Nuclear Reactors, https://doi.org/10.1016/B978-0-08-100149-3.00007-0
[14] DOE-HDBK-1019/2-93, DOE Fundamentals Handbook, Nuclear Physics and Reactor Theory, Volume 2 of 2, https://www.standards.doe.gov/standards-documents/1000/1019-bhdbk-1993-v2