## Slide 1: Progress on Nb3Sn APC Wires
JF. Croteau1, A. Baskys1, I. Pong1, F. Wan2, X. Xu2
1LBNL and 2FNAL (jcroteau@lbl.gov)

## Slide 2: Outline
Nanoprecipitate dimensions: APS feasibility study
Investigation of Hf-rich phase
Oxygen content and distribution

## Slide 3: Main Objectives
The main (or practical) objective of the ongoing research is to better understand the heat treatment of Nb3Sn superconducting wires with artificial pinning centers (ZrO2 and HfO2) to optimize the heat treatments and produce wires with higher superconducting properties (Jc and Hc2) for particle accelerator magnets.
This will be accomplished by:
Studying the size and density evolution of nanoprecipitates at different stages and dwell times of a heat treatment
Studying the formation of intermediate phases in the sub-elements at different stages and dwell times of a heat treatment
Modelling the growth of the nanoprecipitates for different heat treatment conditions
1. APS study
2. Hf-rich phase
3. Oxygen content

## Slide 4: Nanoprecipitate Dimensions: APS Feasibility Study

## Slide 5: Current State of the Research
Nanoprecipitates were characterized using TEM for different temperatures and dwell time at TU Vienna by Alice Moros (previously at LBNL) and colleagues
TEM is limited in the volume of material analyzed
Only few regions in a sub-element were analyzed for each HT condition
We need more data to have a better understanding of nanoprecipitate size from different heat treatments
We want a model to predict/estimate their size for given conditions

## Slide 6: Limited Volume and Statistics from TEM Studies
Current approach with TEM
48 sub-elements/wire → analyzing ~ 700 x 700 x 100 nm3 per lamella
TEM region
Pt
Sub-element
SEM and TEM images from A. Moros’s PhD
Cross-section of a 40-strand Rutherford cable
18.15 mm
Lamella extracted with a FIB
Pt

## Slide 7: Nanoprecipitate Characterization
Largest precipitates appear to be for samples heat treated at the highest temperature (700–720°C) for a short dwell time (45–69 h)
Large variation between samples heat treated in the same conditions
Large standard deviation in precipitate size for the same sample
Need (1) more data and (2) a more systematic approach to understand growth and coarsening of the nanoprecipitates
…
…
720 °C
700 °C
685 °C
675 °C
T (°C)
t (h)
0
100
200
300
400
Hf
Zr
ø 5 nm 10 nm
Approx. precipitate diameter
stdv
Heat treatment conditions previously studied
Precipitate size data from A. Moros (CERN, previously at LBNL)

## Slide 8: 1. Machine Learning to Analyze TEM Images
Machine learning for image analysis of superconducting materials
  More data and systematic study: Nanoprecipitate identification from all available TEM images
Nanoprecipitate identification
Labeling
HfO2 precipitates*
*Z-contrast is similar for HfO2 and Nb3Sn matrix Zeff: Nb3Sn = 43.25, HfO2 = 29.33, ZrO2 = 18.67
TEM image and labelled data from A. Moros (CERN, previously at LBNL)
See A. Baskys’s talk

## Slide 9: 2. Synchrotron High Energy X-Rays
x-ray
SAXS detector
WAXS detector
*if the wires are twisted, the extracted sub-elements will be spirals
Cu
Nb3Sn, ZrO2 or HfO2, Kirkdendall voids, Nb
Top view/cross-section
Cu
Cu
Nb
Nb3Sn
Cu + Voids
Precipitate size
Precipitate density
Phase identification (“similar” to XRD)

## Slide 10: Sample Preparation: Masking and Etching
Masking with Teflon tape works well (enough) for our purpose
  Paraffin wax and beeswax were also tried. They are better at masking, but more complicated to completely remove after etching (essential for the heat treatment)
Masked AUP Wires
Masked wires after etching and after removing the masks

## Slide 11: Masking and Etching
Trials with RRP (AUP) wires showed that 20 min etches the Cu around the 1st layer of sub-elements and 5 h leaves only the core Cu. The Nb barriers are not reacting with HNO3
Cross-section of etched wires
20min etch
5h etch
Unreacted
Reacted
Edge of the masked region

## Slide 12: Heat Treatment of Etched Wires
Heat treatment of AUP wire etched for 5h: no apparent Sn leak or other issues
(a) Reference wire for comparison
(b) Partially etched (5h) AUP wire
(a)
(b)
Promising for in-situ study

## Slide 13: Feasibility Study Wires
Heat treatment conditions
Wires with ZrO2 at 700°C for 0h, 2h, 9.7h, and 30h
Wires with HfO2 at 700°C for 9.7h
Wires with Hf, but no internal oxidation at 700°C for 2h
Sample preparation conditions
With copper matrix (not etched)
Without copper matrix (etched for 0.5h and 5.5h)
Extracted sub-elements (1 sub-element and a bunch of 3 sub-elements)
Wire and sub-elements in quartz tubes (for future in-situ study)

## Slide 14: Feasibility Study: Sample Preparation
Masking with Teflon tape worked
Samples etched in nitric acid
Wire cutting and masking
Nitric acid etching and unmasking
Not masked
1 end masked
2 ends masked

## Slide 15: Feasibility Study: Sample Preparation
Analysis of the same wire at different stages of a heat treatment for different sample preparation conditions (total of 22 samples)
1 and 3 sub-elements
Exposed sub-elements
Quartz tubes

## Slide 16: Project Timeline
Rapid access proposal was approved for a feasibility study on October 14 and 15
Aiming to conduct an in-situ study during cycle run 2023-1
*https://www.aps.anl.gov/APS-Upgrade
June
August
September
October
November
December
January
February
April
May
2022
2023
July
shutdown APS-U*
March
Feasibility study (10/14 – 10/15)
Cycle run 2023-1
Oct 28
Rapid access proposal
First calls with beamline scientists
https://www.aps.anl.gov/Users-Information/About-Proposals/Proposal-Deadlines-and-Meetings

## Slide 17: Conclusions and Next Steps
Conclusions
We need more data on nanoprecipitate size and density to have a better understanding of their formation and growth during heat treatment
Next Steps
Feasibility study will take place at the APS in 2 weeks
New proposal for an in-situ study in 2023

## Slide 18: Investigation of Hf-Rich Phase

## Slide 19: Scios 2 DualBeam SEM from ThermoFischer
We have access to a state-of-the-art dual beam SEM at UC Berkeley’s Nuclear Engineering department
SEM and FIB (Ga+ ions)
Detectors
  SE
  BSE
  Combined in-column SE+BSE
  EDS
  EBSD
  STEM (BF, DF, HAADF)
https://www.iitk.ac.in/meesa/SEM/tutorial/SEM_TGP.pdf

## Slide 20: SEM Capabilities
In-column combined SE and BSE detectors
BSE

## Slide 21: SE Detector: High Resolution at High Magnification
Grain and twin boundaries in copper (“hexagons cut by parallel lines”)
Crack/line between cladded and stacked sub-elements visible
Image enhanced to show features
Crack/line
GB
Twin
Nb/Nb3Sn boundary

## Slide 22: EBSD – Phases and Grain Orientations
Not indexing the Nb3Sn phase and the NbSn2 and/or Nausite
Nb has a 110 fiber texture (expected for BCC metal deformed in tension)

## Slide 23: BSE and SE Images – Hf- and/or Ta-Rich Phase
2.5 µm
Hf-/Ta-rich
Cu-rich
NbSn2 and/or Nausite
Nb3Sn
C-contamination
Nb barrier
Cu

## Slide 24: Conclusions and Next Steps
Conclusions
Access to well equipped and relatively new SEM at UC Berkeley
We’ve observed an intermediate phase that was not previously known to form in Nb3Sn wires with Hf (might have been observed in casted Cu-Hf alloys)
Next Steps
Analysis of reacted wires with internal oxidation to see if the phase is also present
Analysis of WAXS data to see if we can detect it

## Slide 25: Oxygen content and distribution

## Slide 26: Summary of Ongoing Research
The expulsion of O from the core (SnO2 powder) and the formation of the oxide nanoprecipitates is not well understood
Oxygen content between different HT conditions was not accurately measured using EDX
  Tried using EDX with image analysis methods for radial distribution in unreacted Nb and in entire sub-elements
Unpublished results – Please do not use
Nb3Sn
Backscattered electron images from LBNL, wires from FNAL and Hyper Tech Research Inc.
Upon reaching 700°C
700°C–2 h
700°C–8 h
700°C–60 h
Sn-leak (over reacted)
Cu
Nb

## Slide 27: Method – Image Analysis and Radial O Content
Cu
Nb
Sn
O
Zr
Ta
SE
BSE
EDX composition maps

## Slide 28: Method – Image Analysis and Radial O Content
Nb
Sn
O
Unreacted Nb
O in unreacted Nb
–
*atomic % maps were used, this illustration is an example of the method used
Python library used for image analysis: https://scikit-image.org/

## Slide 29: Method – Image Analysis and Radial O Content
1-Nb3Sn/Nb
O in unreacted Nb
Analysis for different radii
2
3
4
5
6
7
8
9-Nb/Cu
mean O at% avg. radius
r = 0
r = 1

## Slide 30: Nanoindentation
Objective: indent unreacted Nb barrier
Number of specimens (wires): 4
  Heat treatment temperature: 700°C
  Dwell times: 0, 2, 8, 60h
Samples were vibratory polished
Samples are hot mounted in a “puck”
50 µm
Nb3Sn
Nb
Cu
Cu
Cu
~6.7 µm
~4 µm
~13 µm
4. 700°C–0 h
5. 700°C–2 h
6. 700°C–8 h
7. 700°C–60 h

## Slide 31: Conclusions and Next Steps
Conclusions
Oxygen was not accurately measured using EDX
Next Steps
Nanoindentation of Nb-barrier of wires heat treated at different dwell times planned
  Attempt to indirectly measure different oxygen content by measuring changes in mechanical properties (expecting higher hardness for higher O-content)

## Slide 32: Conclusions
Nanoprecipitate Dimensions
APS feasibility study mid-October
Proposal for in-situ study in 2023
Hf-rich Phase
Investigation of non-reference wires
Oxygen Content
Nanoindentation measurements planned at UC Berkeley

## Slide 33: Thank you!
JF. Croteau1, A. Baskys1, I. Pong1, F. Wan2, X. Xu2
1LBNL and 2FNAL (jcroteau@lbl.gov)

## Slide 34: Backup Slides

## Slide 35: Ostwald Ripening – Lifshitz-Slyozov-Wagner Theory
S.K. Bhattacharyya and K.C. Russell, 1976, Coarsening Kinetics of Silica in Copper, Metallurgical Transactions A, V7A, pp. 453-462 ..\..\..\..\..\My Drive\References\Papers\bhattacharyya1976.pdf
simplification to a linear equation:
slope could be experimentally determined for different temperatures
Compound
the metal. We will assume that the matrix is pure niobium (Nb) for the purpose of finding parameters in the literature, but it should be Nb3Sn
is the rate controlling species
Plots of r3 vs time for SiO2 in Cu for different temperatures (Bhattacharyya and Russell 1976)
coarsening rate
Hafnium

## Slide 36: Ostwald Ripening – Lifshitz-Slyozov-Wagner Theory
slope could be experimentally determined for different temperatures
This should be linear for “diffusion-controlled coarsening”
A dependence with (or something else) would indicate different governing processes, such as “interface kinetics”
Chart: r (nm)
| 317 | 380
T = 675 C | 2.6187 | 3.1101
T = 685 C | 2.2909 | 2.8607
T = 700 C | 6.974 | 2.3137 | 2.508
T = 720 C | 4.3457 | 4.308 | 5.9878
Chart: r2 (nm2)
| 317 | 380
T = 675 C | 6.8574 | 9.6729
T = 685 C | 5.2481 | 8.1837
T = 700 C | 48.6364 | 5.3533 | 6.29
T = 720 C | 18.8851 | 18.5587 | 35.8535
Chart: t (h)
| 317 | 380
T = 675 C | 17.9573 | 30.0841
T = 685 C | 12.0228 | 23.4113
T = 700 C | 339.1896 | 12.386 | 15.7752
T = 720 C | 82.0687 | 79.9508 | 214.6826
675 °C
685 °C
700 °C
720 °C
Hafnium
Are we still in the formation phase and not the coarsening (growth) phase?