## Slide 1: Machine Learning for Nb3Sn wire image analysis
Algirdas Baskys, Kevin Gillespie, Jean-Francois Croteau, Ian Pong
(abaskys@lbl.gov)
Lawrence Berkeley National Laboratory

## Slide 2: Problems to tackle using ML
Image analysis (IA) in a commonly used tool in many sciences (software tools available)
Some problems are not easily tractable using conventional IA techniques:
  Where color/brightness/edges do not encode all necessary information
  Where morphology of the region plays a large role in pixel classification
Nanoprecipitates
in Nb3Sn
Grain size from fracture surfaces
Fractured subelements

## Slide 3: Outline
01
Nanoprecipitate characterization in Nb3Sn
02
Fractography for grain size determination
03
Crack counting in coil sections for destructive testing

## Slide 4: Nb3Sn with artificial pinning centers (APC)
Sample preparation and workflow for nanoprecipitate analysis in APC Nb3Sn wires. A thin lamella is extracted from a polished wire cross-section (circled in red) a), the thinned lamellas are images using a transmission electron microscope. The nanoprecipitates are identified and manually masked c), the masked image can be used to obtain nanoprecipitate statistics. Sample preparation and imaging by A. Moros, CERN.
The sample preparation and analysis workflow is typically:
Polishing the sample
Extracting a thin lamella using FIB
Imaging using TEM/STEM
Manual precipitate labeling
Analysis of the B/W image for determining the size/density distribution
Both sample preparation and analysis is time-consuming.
Analysis can potentially be sped up using ML
Notes: Methods for getting relevant data:
Atom probe tomography
TEM
Small angle X-Ray Scattering

## Slide 5: Nb3Sn with artificial pinning centers (APC)
Grain boundary
ZrO2 precipitates
Images courtesy of A. Moros, CERN
HfO2 precipitates
ZrO2 precipitates
HfO2 precipitates
Notes: Methods for getting relevant data:
Atom probe tomography
TEM
Small angle X-Ray Scattering

## Slide 6: Machine learning approach
The National Energy Research Scientific Computing Center (NERSC) is the primary scientific computing facility for the Office of Science in the U.S. Department of Energy and it is located at LBNL.
We were awarded an exploratory grant to use Perlmutter supercomputer for analysis of Nb3Sn wires using machine learning.
Other computing facilities available at LBNL:
Lawrencium cluster
Einsteinium cluster (with GPU nodes)
Access to AWS and GCP
CPU Node Hours Award: 500 h
GPU Node Hours Award: 100 h
Archive Storage Award (TB): 1 TB
Project CFS Award (TB): 20 TB
Having the software stack in a container (Docker) can help with portability and encapsulation of development environments.

## Slide 7: Nb3Sn with artificial pinning centers (APC)
U-NET
Convolutional neural network used U-Net. Figure from https://pytorch.org/hub/mateuszbuda_brain-segmentation-pytorch_unet/
We are developing NN based on U-NET [1] architecture:
Often used for bio-medical image segmentation
PyTorch (python) implementations widely available as starting point
Once the datasets are no longer the limiting aspect, other neural network architectures such as fully convolutional networks [1] and deepLabv3 [2] will be evaluated.
[1] http://arxiv.org/abs/1505.04597
[2] doi: 10.1109/TPAMI.2016.2572683
[3] http://arxiv.org/abs/1706.05587
Notes: U-Net good starting point for semantic segmentation problems

## Slide 8: Nb3Sn with artificial pinning centers (APC)
With ~75 images labeled, we can start with training… however:
Need a training set (for model training)
Need a validation set (for tweaking hyperparameters)
Need a test set (for evaluating the model)
This considerably shrinks our training dataset, to at least alleviate the problem, we can consider:
Image augmentation (image rotation, flipping, distortion, ...)
Synthetic data
Before evaluation, need to decide on the metrics. Sørensen–Dice coefficient (DSC) is commonly used for semantic segmentation problems, but others may be used as well.
Training using training dataset
Evaluation of the model using validation dataset
Tune model according to results on validation dataset
Model performing best on validation data
Confirm performance on test dataset
Notes: Methods for getting relevant data:
Atom probe tomography
TEM
Small angle X-Ray Scattering

## Slide 9: Nb3Sn with artificial pinning centers (APC)
Initial results with no model “tuning”
Model seems to capture most features of interest
DSC in the range of 0.37-0.72
There is some ambiguity in the data labels with makes the evaluation difficult.
Other parameters to check:
Identification of PPTs regardless of their size
Size comparison of correctly identified PPTs
Samples

## Slide 10: Nb3Sn with artificial pinning centers (APC)
Hyperparameter sweeps can be useful to determine optimal parameters
Grid search of Bayesian methods are often used
Directs to what parameters are most important
Increased the mean DSC from 0.58 to 0.76 using same dataset
Lack of data is the primary difficulty
Notes: Check DSC in the test dataset

## Slide 11: Outline
01
Nanoprecipitate characterization in Nb3Sn
02
Fractography for grain size determination
03
Crack counting in coil sections for destructive testing

## Slide 12: Fractography
Grain size is one of the more important characteristics of Nb3Sn as grain boundaries act as magnetic flux pinning centers inhibiting energy dissipation as current flows though the superconductor.
Typical grain sizes range from ~20 to 200 nm depending on the heat-treatment schedule and wire architecture.
Given their small size, determination of grain size is not trivial.
Although not the only available method, analysis of wire fracture surfaces is by far the most common method for determining Nb3Sn grain size
  Nb3Sn exhibits intergranular fracture
  Easy sample preparation
  Imaging requires an SEM
  Analysis is labor intensive
Maximum pinning force as a function of grain size at 4.2 K in Nb3Sn wires with no artificial pinning centers [1]
Workflow for manually grain size analysis. Individual grains in an Nb3Sn fractograph a) as imaged, b) after manual contour tracing; c) with an overlay of the image analysis results.
Analysis would benefit from automation using ML
[1] A. Godeke, “Performance Boundaries in Nb3Sn”, PhD thesis, June. 2005

## Slide 13: Fractography
A rule of thumb for training ML models, 103 of labeled images are required.
  Prohibitively extensive endeavor for this problem
Pursuing to augment hand-labeled data with synthetic data
A 3D grain structure in generated using Voronoi construction from randomly distributed points (equiaxed grains)
A section of grains is removed to show a “fracture” surface
The grains are textured and lit as to resemble an SEM SE image
Workflow developed for generating synthetic fractography images and associated labels. Grain structure analog is created using a 3D Voronoi construction. Portion of the grains removed to reveal "an intergranular fracture surface". The grains are then textured and lit to imitate a secondary electron contrast image taken using an SEM. Visible grain interfaces are rendered as well to create the label image.
A true ground truth!

## Slide 14: Fractography
  We are just about done with generating the synthetic data
  Initial results of labeling synthetic data very promising with accuracy of > 90%
  Next steps include integration with hand labeled data, image augmentation and model/hyperparameter tuning

## Slide 15: Fractography
Offshoot of the synthetic data generation work:
Kevin Gillespie was investigating how the grain sizes determined by different methods relate to the true – volume based – value and to each other.
  Fractography (area)
  “Flat polish” (area)
  “Flat polish” (line intercept) [1]
Information on the topic is somewhat limited as although standards exist (ASTM E112) [1], they are based on analytical formulae with many assumptions
Full control on the grain structure:
  Various size distributions
  Columnar grains
[1] “Standard Test Methods for Determining Average Grain Size“, ASTM E112-13(2021), DOI: 10.1520/E0112-13R21
a)
b)
Grain diameter based on volume vs. grain size based on a) 2D projection are of a fractography; b) 2D projection of a polished specimen. Figures based on a grain structure generated using Voronoi construction. (Kevin Gillespie).
Flat polish
Fractography
Flat polish observation
Hidden grain shape
Notes: Put labels on

## Slide 16: Outline
01
Nanoprecipitate characterization in Nb3Sn
02
Fractography for grain size determination
03
Crack counting in coil sections for destructive testing

## Slide 17: Cracked Nb3Sn Subelement Identification
Nb3Sn dipole magnets present a challenge in their mechanical design as the brittle Nb3Sn subelements are susceptible to damage by cracking if stresses are not managed carefully. Even a small number of cracks can significantly reduce strand performance.
A single coil cross-section may have on the order of ~500,000 individual subelements that need to be investigated for potential cracks – an effort that would require one month at a rate of one second per subelement!
A cross-section of a Nb3Sn cosine theta dipole accelerator magnet. An enlarged image of a Rutherford cable from the coil cross-section is shown in green, image of a wire from the cable cross-section is shown in blue box. An individual subelement from a wire is shown in a red box.

## Slide 18: Cracked Nb3Sn Subelement Identification
Unsupervised learning – feature clustering
Image to be segmented
Histogram of 2 properties of pixels in the image
K-Means decision boundary
Gaussian Mixtures decision boundary
Segmented image
Segmented image

## Slide 19: Cracked Nb3Sn Subelement Identification
Similar approach can be used for segmentation of cracked subelements:
Isolate subelements and darker features within subelement via clustering based on color
Isolate cracks from porosity/voids using morphological features (size, aspect ratio, etc)
Once the cracks are segmented, parameters of interest can be calculated trivially (density of cracks and their orientation) that can be used to determine their origin.
Size of the dataset is the largest challenge:
High magnification required
Large area
Automated stage and autofocusing required
Stitching of images on-demand
Keyence confocal microscope

## Slide 20: Conclusions and next steps
Some problems necessitate ML approaches
  Non-supervised ML is now commonplace in IA
  Use of supervised machine learning (CNNs) in literature is increasing
Initial results promising but dataset size requirements are an issue
Synthetic data and data augmentation can help
Ground truth in some cases in not easily attainable making model evaluation difficult
Next steps include obtaining more labeled data
Synthetic data generation and evaluation of its effectiveness
Model architecture/training parameter refinement

## Slide 21: Thank you! Questions?
Machine Learning for Nb3Sn wire image analysis
Algirdas Baskys, Kevin Gillespie, Jean-Francois Croteau, Ian Pong
(abaskys@lbl.gov)
Lawrence Berkeley National Laboratory

## Slide 22: Synthetic data
To minimize the need for real data, we create our own:
“Data” and label created together
Straight forward to automate to create large dataset for training
The pre-trained model is likely to need less real data to achieve good performance
Only read data would be used for validation
Notes: The 3D models will also help to investigate how the grain size determined by fractography relates to actual grain size/diameter

## Slide 23: Nb3Sn with artificial pinning centers (APC)
APCs contribute to:
  Additional point pinning
  Reduction in grain coarsening during HT
To optimize heat-treatment of APC wires it is of interest to determine:
  Precipitates size,
  Density
  Growth rate
Multiple samples need to be analyzed, but both sample preparation and analysis are very time consuming
The images are not suitable for analysis via conventional IA techniques
[1] X. Xu et. al., doi: 10.1016/j.scriptamat.2020.05.043
[2] J. Rochester et. al., doi: 10.1109/TASC.2021.3057560
a) Internally oxidized wire performances compared with state-of-the-art PIT and RRP wires, and CERN’s FCC’s specifications [1]; b) Grain boundary (APC GB) and point pinning due to nanoprecipitates (APC PP) contributions to the pining force in APC wires as well as data from powder in tube (PIT) Nb3Sn wires for reference [2].
a)
b)
APC wires developed at Fermilab (X. Xu) and Hypertech Inc. The first Nb3Sn wire measured in transport to meet the FCC specification in terms of critical current.
TEM images by Alice Moros, CERN
Notes: Potentially remove as JF will be covering the material