## Slide 1: Key parameters for strong a-axis grain growth in narrow filament cavities of Bi-2212 round wires
F. Kametani, J. Jiang, M. Matras*, Y. Oz, A. Oloye, D. Abraimov, A. Francis, U. P. Trociewitz, E. E. Hellstrom, D. C. Larbalestier
Applied Superconductivity Center, National High Magnetic Field Laboratory, Florida State University
* Now at CERN, Switzerland

## Slide 2: Superconducting magnets over 16 T need HTS
Plots by P. J. Lee
FCC performance target for Nb3Sn
(A. Ballarino, FCC Workshop April 2016)
Je(4.2K, 16T) = 600 A/mm2
Bi-2212 is the only HTS cuprate with which high Jc round wires can be made.
Recently Jc increased 70% with the new US-made powder (4MO1-03 J. Jiang)
Why is high Jc possible in Bi-2212 round wires?

## Slide 3: Bi-2212 grain alignment along the wire direction is the key for high Jc/Je
Inverse pole figure color coding and crystallographic direction in Bi-2212
SEM
EBSD IPF
EBSD GB
GB misorientation angle fraction
0.3-1.0 µm thin, 50-300 µm long grains
Majority of GB misorientation are <20° by quasi-biaxial grain alignment

## Slide 4: Same scale comparison of grain structure in different transverse cross-sections of filaments
Wire direction
[100]
Single filament
Two filament bonded
6-7 filament bonded

## Slide 5: Comparison of inverse pole figures along the wire direction - The more filament bonding, the more degradation of a-axis texture
IPF along the wire direction of the IPF grain maps in the previous slide.
FWHM of a-axis texture in a single filament is <10°. When the two filaments merge in one, it allows more distribution of in-plane grain misorientation. The 6-7 filaments bonded into the large one, the grain misorientations distribute >25° in both in-plane and out-of-plane, presumably degrading Jc most significantly.
Single filament
Two filament bonded
6-7 filament bonded

## Slide 6: Cooling rate changes the grain size
Cooling rate RF controls:
  Amount of second phases
  Amount of 2212
  Filament coupling
  Grain size
  Grain alignment
  2212 connectivity along the length
RF = 1.3°C/h
Design of Experiments (DoE) Conclusions (37x18 and 27x7):
  Cooling rate RF and Time in melt tmelt affect IC the most
RF = 9.7°C/h
M. Matras, PhD thesis at FSU (2016)
Slow cooling
Fast cooling
Ic(4.2K, 5T) = 380 A
Ic(4.2K, 5T) = 110 A

## Slide 7: Cooling rate appears not to affect a-axis grain nucleation
asdf
5 µm
5 µm
Large Bi-2212 grains doesn’t form by fast cooling, perhaps spoiling the grain connectivity along the filament length
Fast cooling
Slow cooling
EBSD by A. Oloye

## Slide 8: The long and thin Bi-2212 grains can plastically twist during growth
One long grain can twist and compensate the c-axis misorientation up to ~30°
Larger grains allow more twisting to decrease GB misorientation along the filament direction

## Slide 9: Why don’t the15° GBs in Bi-2212 show weak connectivity?
The bicrystal experiments of HTS cuprates indicates that 15° GBs are still high angle, and would be weakly coupled
But high Jc Bi-2212 RWs don’t show a signature of weakly coupled GBs
Is Bi-2212 special among the HTS cuprates?
Does oxygen overdoping strengthen the connectivity of grain boundaries?

## Slide 10: Post annealing in low oxygen atmosphere underdopes Bi-2212
Y. Oz
Standard HT
1 bar pO2
Post annealing
0.01 bar pO2
Can we make the GB coupling weaker by underdoping?

## Slide 11: Underdoping affects Tc, Hirr, Jc
But no Jc hysteresis was observed in significantly underdoped samples
Was the GB connectivity not affected by underdoping?
Y. Oz
PO2 = 0.01 bar
PO2 = 0.01 bar
Post-annealing pO2 = 0.01 bar

## Slide 12: Conclusion
Bi-2212 has the unique quasi-biaxial grain structure
  Strong a-axis (NOT c-axis) texture, although prior deformation (wire drawing) can play no role in the grain growth
  Surprisingly in-plane misorientation is ~15° too
Bi-2212 quasi-biaxial texture development is dependent on filament cavities
Cooling rate affects the grain size, but doesn’t affect very much on the a-axis texture development
  The larger grain size, the more plastic twisting to decrease GB misorientation along the wire direction?
Bi-2212 under oxygen-overdoped, possibly enhancing the carrier density at the GBs, but the underdoping experiments could not alter the GB connectivity

## Slide 13: Acknowledgements
Supported by the US DOE Office of High Energy Physics under grant number DE-SC0010421, and by the NHMFL, which is supported by NSF under NSF/DMR-1157490 and by the State of Florida.
All Bi-2212 round wires were fabricated by Bruker-OST