## Slide 1: From Nb3Sn USL* to ESE** Relation and Spreadsheet
Ian Pong (ipong@lbl.gov)
Jack Ekin (jackekin1@gmail.com)
*USL: Unified Scaling Law (Ekin 1980 Cryogenics)
**ESE: Extrapolative Scaling Expression (Ekin 2016 SuST)

## Slide 2: Outline
Introduction: superconducting surface (a.k.a. critical surface)
Scaling parameterization
  A graphical presentation
  A mathematical presentation
  From USL to ESE
Addressing Temperature and Strain Dependence Issues
Addressing Transport vs. Magnetization Issues
ESE Spreadsheet usage – Live Demo (dedicated group)

## Slide 3: Introduction
The customary plot of J-H-T surface:
For practical purposes Nb-Ti is considered insensitive to strain
Nb3Sn, by contrast, is highly strain sensitive:
  IC (B, T, ε) = B-1 C g(ε) h(t) f(b)
Requires 4D plot
    Or multiple 2D and 3D plots
Figure by courtesy of Lyn Evans
Figure from SMH ed. 1

## Slide 4: Pinning force curve and its scalability
Supercond. Sci. Technol. 29 (2016) 123002
The pinning curves at different temperatures and strains coalesce into one master scaling curve, and this is what gives the extrapolation capability
Global fitting is more expedient than fundamental scaling, but it greatly diminishes extrapolation capability.
Red: 4.2 K
Green: 8.0 K
Blue: 12.0 K
Key thing about scaling laws
is scalability
When something scales
it can be extrapolated
Thousands of IC can be predicted from just a few IC(B) measurements!

## Slide 5: Determining BC2* and K from IC(B) Data
Chart: B [T]
Chart: b
Chart: 
| 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16
 | 67.2785 | 63.8198 | 60.3611 | 56.9025 | 53.4438 | 49.9852 | 46.5265 | 43.0678
[A0.5 T0.25]
f (b) = bp (1-b)q
p = 0.5
q = 2
BC2* -- effective upper critical field (determined from IC using trimmed data)
Note: Trimming required due to natural measurement limits and flux creep effects at high T and B.
Formally:
For Nb3Sn

## Slide 6: Temperature Dependence of the FP Curve
T [K]
Chart: B [T]
Chart: b
Chart: B
Chart: B
Chart: B
BC2 [T]
T = 0 K
T = 4.2 K
T = 10 K
T = 16 K
4.2
10
16
Nb3Sn FP curve is temperature and strain dependent
If we plot the pinning force F against the actual field B instead, the curves at increasing temperatures will have a decreasing BC2, but the shape of the curve remains the same.
Now, if we plot the temperature on the third axis, we can see the BC2 dependence on T more clearly.

## Slide 7: BC2* (T)
T [K]
BC2 [T]
Chart: T [K]
Chart: T [K]
bC2
t
bC2 (t) = 1 – t v
If we plot reduced field against reduced temperature, we can see a power law relationship.
This is one of two ways to determine TC* -- the “effective flux-pinning critical temperature”

## Slide 8: BC2* (ε)
Chart: Strain component, ε0 [%]
| -1.9 | -1.8 | -1.7 | -1.6 | -1.5 | -1.4 | -1.3 | -1.2 | -1.1000000000000001 | -1 | -0.89999999999999991 | -0.8 | -0.7 | -0.60000000000000009 | -0.5 | -0.39999999999999991 | -0.30000000000000004 | -0.19999999999999996 | -0.10000000000000009 | 0 | 0.10000000000000009 | 0.20000000000000018 | 0.29999999999999982 | 0.39999999999999991 | 0.5 | 0.60000000000000009 | 0.70000000000000018 | 0.79999999999999982 | 0.89999999999999991 | 1 | 1.1000000000000001 | 1.2000000000000002 | 1.2999999999999998 | 1.4 | 1.5 | 1.6 | 1.7000000000000002 | 1.7999999999999998 | 1.9 | 2 | 2.0999999999999996 | 2.2000000000000002 | 2.2999999999999998 | 2.4000000000000004 | 2.5 | 2.5999999999999996 | 2.7
Total strain | 0.42298 | 0.44398 | 0.46575 | 0.48835 | 0.51184 | 0.53634 | 0.56199 | 0.58896 | 0.61747 | 0.64775 | 0.68001 | 0.71437 | 0.75077 | 0.78882 | 0.82761 | 0.86555 | 0.90026 | 0.9287 | 0.94751 | 0.95371 | 0.94536 | 0.9222 | 0.88574 | 0.83886 | 0.78512 | 0.72804 | 0.67056 | 0.61482 | 0.56218 | 0.51336 | 0.4686 | 0.42787 | 0.39098 | 0.35762 | 0.3275 | 0.30031 | 0.27575 | 0.25354 | 0.23346 | 0.21528 | 0.19879 | 0.18382 | 0.1702 | 0.15779 | 0.14646 | 0.13609 | 0.12657
Hydrostatic | 0.39541 | 0.40985 | 0.42374 | 0.43694 | 0.44928 | 0.46061 | 0.47076 | 0.4796 | 0.48698 | 0.49279 | 0.49693 | 0.49934 | 0.49998 | 0.49883 | 0.49592 | 0.49129 | 0.48502 | 0.47722 | 0.46799 | 0.45749 | 0.44585 | 0.43325 | 0.41984 | 0.40577 | 0.39121 | 0.3763 | 0.36118 | 0.34597 | 0.33079 | 0.31573 | 0.30087 | 0.2863 | 0.27206 | 0.25822 | 0.24479 | 0.23182 | 0.21933 | 0.20732 | 0.1958 | 0.18477 | 0.17424 | 0.16419 | 0.15461 | 0.1455 | 0.13684 | 0.12861 | 0.12081
Deviatoric | 0.027564 | 0.034134 | 0.04201 | 0.051405 | 0.062556 | 0.075729 | 0.091223 | 0.10936 | 0.1305 | 0.15497 | 0.18308 | 0.21503 | 0.25079 | 0.28999 | 0.33169 | 0.37425 | 0.41523 | 0.45148 | 0.47952 | 0.49622 | 0.49951 | 0.48896 | 0.46591 | 0.43309 | 0.39391 | 0.35174 | 0.30938 | 0.26885 | 0.2314 | 0.19763 | 0.16773 | 0.14158 | 0.11891 | 0.099409 | 0.082712 | 0.068485 | 0.056418 | 0.046229 | 0.037665 | 0.030505 | 0.024552 | 0.019631 | 0.015589 | 0.012293 | 0.0096225 | 0.0074761 | 0.005764
Chart: Strain component, ε0 [%]
| -1.9 | -1.8 | -1.7 | -1.6 | -1.5 | -1.4 | -1.3 | -1.2 | -1.1000000000000001 | -1 | -0.89999999999999991 | -0.8 | -0.7 | -0.60000000000000009 | -0.5 | -0.39999999999999991 | -0.30000000000000004 | -0.19999999999999996 | -0.10000000000000009 | 0 | 0.10000000000000009 | 0.20000000000000018 | 0.29999999999999982 | 0.39999999999999991 | 0.5 | 0.60000000000000009 | 0.70000000000000018 | 0.79999999999999982 | 0.89999999999999991
Total strain | 0.42298 | 0.44398 | 0.46575 | 0.48835 | 0.51184 | 0.53634 | 0.56199 | 0.58896 | 0.61747 | 0.64775 | 0.68001 | 0.71437 | 0.75077 | 0.78882 | 0.82761 | 0.86555 | 0.90026 | 0.9287 | 0.94751 | 0.95371 | 0.94536 | 0.9222 | 0.88574 | 0.83886 | 0.78512 | 0.72804 | 0.67056 | 0.61482 | 0.56218
Hydrostatic | 0.39541 | 0.40985 | 0.42374 | 0.43694 | 0.44928 | 0.46061 | 0.47076 | 0.4796 | 0.48698 | 0.49279 | 0.49693 | 0.49934 | 0.49998 | 0.49883 | 0.49592 | 0.49129 | 0.48502 | 0.47722 | 0.46799 | 0.45749 | 0.44585 | 0.43325 | 0.41984 | 0.40577 | 0.39121 | 0.3763 | 0.36118 | 0.34597 | 0.33079
Deviatoric | 0.027564 | 0.034134 | 0.04201 | 0.051405 | 0.062556 | 0.075729 | 0.091223 | 0.10936 | 0.1305 | 0.15497 | 0.18308 | 0.21503 | 0.25079 | 0.28999 | 0.33169 | 0.37425 | 0.41523 | 0.45148 | 0.47952 | 0.49622 | 0.49951 | 0.48896 | 0.46591 | 0.43309 | 0.39391 | 0.35174 | 0.30938 | 0.26885 | 0.2314
Chart: 
BC2* (ε) [T]
  The strain function
  bC2 (ε) =
Note: in reality there is irreversibility

## Slide 9: BC2* (ε)
Chart: 
BC2* (ε, 0) [T]
  The strain function
  bC2 (ε) =
BC2* (ε, T)

## Slide 11
BC2* (ε, T) [T]
TC (ε) [K]
ε0 [%]

## Slide 12: Temperature dependence of K
T [K]
Chart: B [T]
Chart: B
Chart: B
Chart: B
BC2 [T]
T = 0 K
T = 4.2 K
T = 10 K
T = 16 K
4.2
10
16
This is the other way to determine TC*

## Slide 13: K (t)

## Slide 14: K (ε)

## Slide 15: K (t)

## Slide 16: Mathematically…
  where

## Slide 17: Mathematically…
Scaling parameters:
  TC*(0), s, η, and the various strain parameters modeling bC2(ε);
  C, BC2*(0, 0);
  w, v, u;
  p, q
“Core Scaling Parameters”
“Individual Wire Scaling Parameters”
USL
ESE
“Scaling Constants” – have a consistent value within a family of Nb3Sn conductors
“p = 0.5, q = 2 for strong (g.b.) pinning Nb3Sn. Fitting accurately over technological B-T range

## Slide 18: USL to ESE
USL:
  FP measured at different T and ε are shape invariant
  All data coalesce into a single master unified-scaling curve
  Significance: extrapolation capability from this master curve
ESE:
  Derivation of ESE is an extensive but single study of many Nb3Sn conductors
  Application of ESE is just a fit, even allowing combined data from different measurement apparatuses

## Slide 19: Outline – to be continued…
Introduction: superconducting surface (a.k.a. critical surface)
Scaling parameterization
  A graphical presentation
  A mathematical presentation
  From USL to ESE
Addressing Temperature and Strain Dependence Issues
Addressing Transport vs. Magnetization Issues
ESE Spreadsheet usage – Live Demo