## Slide 1
D. Arbelaez, L. Brouwer, S. Caspi, D. Dietderich, S. Gourlay, R. Hafalia, T. Lipton, M. Martchevskii, S. Myers, J. Swanson, S. Prestemon
US Magnet Development Program
Lawrence Berkeley National Laboratory
Subscale CCT Plans

## Slide 2: Motivation
CCT4 exhibited a large number of training quenches
Subscale models can lead to faster turnaround for dedicated training experiments
  Epoxy (or other matrix) influence on training
  Structural influences
  Interface conditions
Allows for testing of novel instrumentation
Subscale models are complementary to overall CCT program
  CCT subscale – provides feedback for large bore magnets
  CCT5 – Drawings are currently being finalized for mandrels and interface technology is being developed
  CCT6 – Conceptual design phase

## Slide 3: Design Goals
Similar Lorentz force density as CCT4
Similar stress as CCT4
Small and easy to test for quick turn around (epoxy etc.)
Test in small cryostat with 10 kA power supply
Plan to use existing conductor (RRP 132/169) that has been characterized for critical current and stability (previously used for undulator project)

## Slide 4: RRP 132/169 Conductor
  RRP Nb3Sn
  0.6 mm diameter strand
  50% ncf
  2880 A/mm^2 at 10 T
Lorentz force density peaks at 4.5 T

## Slide 5: Choice of a 11 strand cable
  A two layer 11 strand design
  matches the Lorentz force density of CCT4
  keeps the power supply current under 10 kA
  keeps the current per wire < 1000 A for stability
  4.9 x 1.7 mm channel (4.0 x 1.1 mm cable)
Short-sample bore field of 5.37 T, and conductor field of 6.30 T @ 857 A / wire (9.4 kA)

## Slide 6: Fields along the length
  85 mm straight-section

## Slide 7: Lorentz Force Density Compared to CCT4
Comparison of the Lorentz force vs angle (from tosca)

## Slide 8: Normal Stress Distribution Compared to CCT4
-3 MPa
-87 MPa
21 MPa
-35 MPa
Normal stress is close when compared to CCT4 (strongly dependent on choice of spar thickness)
* Comparison at short sample (CCT4 started training slightly above 50% of short sample)
Normal Stress transverse to cable
Normal Stress along cable
CCT4
CCT Subscale (2mm spar)
33 MPa
-54 MPa
-62 MPa
-6 MPa

## Slide 9: Normal Stress Distribution Compared to CCT4
Shear stress is approximately one-half when compared to CCT4 (not strongly dependent on overall deformation)
tangent-binormal shear stress
radial-binormal
tangent-radial
CCT4
CCT Subscale (2mm spar)
20 MPa
-20 MPa
38 MPa
-8 MPa
49 MPa
-49 MPa
21 MPa
-21 MPa
23 MPa
-9 MPa
11 MPa
-11 MPa

## Slide 10: Current Status
Mandrel drawings are ready
Cable parameters have been defined
Minimal tooling is needed
  End plugs for potting tooling
  Splice tooling

## Slide 11: Possible Training Studies
Baseline Test
  Same as CCT4
  layer 1 and layer 2 impregnated together inside of Al shell
  CTD101K epoxy
Wax Impregnation Test
  Layer 1 and layer 2 impregnated together inside of Al shell
  Wax impregnation
Individual Layer impregnation
  Impregnate inner layer with CTD 101K
  Impregnate inner layer with FSU mix 61
Test effect of surface roughness and/or surface preparation in grooves
Multiple subscale magnets (2 to 3) can be wound can be fabricated and tested together in order to carry out the testing more efficiently