## Slide 1
Emerging Combustion Synthesis Methods to Prepare Thin Targets for Nuclear Science Research
Khachatur Manukyan
Nuclear Science Laboratory
Department of Physics and Astrophysics
Workshop on Applied Nuclear Data Activities (WANDA)
Feb. 26 – Mar. 1, 2024, Hilton Arlington National Landing, Crystal City, VA

## Slide 2
Outline
Solution Combustion Synthesis (SCS): SCS of Actinides
Thin-film target by SCS methods
Irradiation studies of targets
Conclusions
Acknowledgments

## Slide 3
Solution combustion synthesis (SCS)
SCS is a rapid chemical reaction between metal nitrates (oxidizer) and solvent-soluble organic compounds (fuel) that produce nanoscale materials.

## Slide 4
Ni(NO3)2
NiO
TiO2
(Anatase)
Oxides
CeO2
Fe2O3
(Hematite)
NiS
Perovskites
(SrTiO3)
Garnets
( Y3Al5O12)
Phosphates
(Ca₃(PO₄)₂)
Silicates
(CaSiO3)
Metals & Alloys
Metal-oxide Composites
Pt/CeO2
NiCu
Ni
Nitrides
Fe3N
Carbides
Mo2C
Sulfides
Materials prepared by SCS

## Slide 5
SCS in preparing nanoscale materials

## Slide 6
6
SCS OF ACTINIDES
UO2(NO3)2 + Glycine + H2O

## Slide 7
Kinetics of ThO2 combustion synthesis reaction
Th(NO3)4 +

## Slide 8
Complexation in the UO2(NO3)2 + (φ)Glycine + H2O solutions

## Slide 9
UO2(NO3)2 + Acetylacetone + 2-methoxyethanol
Mechanistic investigations of SCS

## Slide 10
ThO2 nanoscale materials prepared by combustion of the Th(NO3)4 + solutions.
=1.5
Characteristics of “bulk” combustion products
TEM image (A), selected area diffraction pattern (B), and high-resolution TEM images (C,D) for UO2+x.

## Slide 11
Outline
Solution Combustion Synthesis (SCS): SCS of Actinides
Thin-film target by SCS methods
Irradiation studies of targets
Conclusions
Acknowledgments
Outline

## Slide 12
Target preparation methods: Spin-coating-assisted-SCS

## Slide 13
Thin-film uniformity
U Mα
Al Kα

## Slide 14
Target preparation methods: Spraying-assisted-SCS

## Slide 15
Tuning the target thickness
Representative a particle spectrum (A) and U amount vs. the solution flow rate (B) and the spraying time (C).
B
C
A

## Slide 16
Deposition setup (A) and photos of the pure 243Am (B) and the 243Am/235U targets (C).
243Am, and 243Am/235U Targets
Analogue material preparation

## Slide 17
Target preparation methods: Printing-assisted-SCS

## Slide 18
Eu2O3 target preparation with the inkjet method
0.0125 M Eu
0.125 M Eu

## Slide 19
Solution Combustion Synthesis (SCS)
SCS of Actinides: Fundamentals
Preparation of thin-film target by SCS methods
Irradiation studies of targets
Conclusions
Acknowledgments
Outline

## Slide 20
Over 500 UO2, ThO2, and Th1-xUxO2 targets on Al, C, and Si backings were prepared.
One 243Am and one 243Am/235U targets sandwiched between Al foils were prepared.
UO2 targets on Al backings were irradiated at Notre Dame Nuclear Science Laboratory.
UO2 targets on Al or C backings were tested in neutron measurements at LANL.
Detector for Advanced Neutron Capture
Experiments (DANCE) array at LANSCE
5U Sta. Ana accelerator at
Notre Dame Nuclear Science Laboratory
Target preparation and testing

## Slide 21
Images: Dede S, Manukyan K V, Roach JM, Robertson D, Burns PC, Aprahamian A. Irradiation-induced Interactions at UO2/Al2O3/Al Interfaces. J. Phys. Chem. C 2023, 127, 20, 9850–9857
TEM images of targets (spraying)

## Slide 22
Irradiation: Ar2+ (1.7 MeV energy) 1.3×1017 ions/cm2
Annealed at 550oC
Annealed at 350oC
Al Kα1
U Mα1
O Kα1
Mg Kα1_2
Al Kα1
U Mα1
O Kα1
Mg Kα1_2
Major structural changes
Notes: We see the UO2 layer before and after irradiation -> for the 550 it is definitely robust, 350 has
Further analysis of the layers
Diffusion of mg/al from the backing

## Slide 23
Neutron-irradiated target
Pristine target
Neutron capture measurements at LANSCE

## Slide 24
Student taring

## Slide 25
Current & Former Students
Noah Cabanas
PhD student
Konstantin Bauer
undergraduate student
Victor Williams
undergraduate student
Stefania Dede
LANL
Jordan Roach
ORNL
Bryce Frentz
Humana
Ashabari Majumdar
ND Physics
Sabrina Strauss, CGG
Nathaniel Hiott
Northwestern
Michael Mlodzik
ND
Jacob Galden
Myriad Neuroscience
Peter Guerra
Epic
Raj Chilukuri
undergraduate student
Tomas Romero
undergraduate student

## Slide 26
17 Published articles and 3 articles are in preparation
I.P. Borovinskaya, K.V. Manukyan, A.S. Mukasyan, SHS Ceramics: History and Recent Advances, Ceramics in Modern Technologies, 1, 3-19 (2019).
A.S. Mukasyan, S. Roslyakov, J.M. Pauls, L.C. Gallington, T. Orlova, X. Liu, M. Dobrowolska, J.K. Furdyna, K.V. Manukyan, Nanoscale Metastable ε Fe3N Ferromagnetic Materials by Self- Sustained Reactions, Inorganic Chemistry, 58, 5583−5592 (2019).
S.L. Kharatyan, H.A. Chatilyan, K.V. Manukyan, Kinetics and Mechanism of Nickel Oxide Reduction by Methane, J. Phys. Chem. C, 123, 21513-21521 (2019)
V.V. Baghramyan, A.A. Sargsyan, N.B. Knyzyan, V.V. Harutyunyan, A.H. Badalyan, N.E. Grigoryan, A. Aprahamian, K.V. Manukyan, Pure and cerium-doped zinc orthosilicate as a pigment for thermoregulating coatings, Ceramics International, 46, 4992-4997 (2020).
P. Sapkota, A. Aprahamian, K.Y. Chan, B. Frentz, K.T. Macon, S. Ptasinska, D. Robertson, K.V. Manukyan, Irradiation-induced reactions at the CeO2/SiO2/Si interface, J. Chem. Phys. 152, 104704 (2020).
N. Amirkhanyan, S.L. Kharatyan, K.V. Manukyan, A. Aprahamian, Thermodynamics and Kinetics of Solution Combustion Synthesis: Ni(NO3)2 + Fuels Systems, under review at Combustion and Flame, 221, 110-119 (2020).
M.K. Zakaryan, S.L. Kharatyan, A. Aprahamian, K.V. Manukyan, Combustion in the ZrF4-Mg-Si and ZrF4-Al-Si Systems for Preparation of Zirconium Silicides, Combust. Flame 232, 111514 (1-9), (2021).
B. Frentz*, A. Aprahamian, A.M. Clark, C. Dulal, J.D. Enright, R.J. deBoer, J. Goerres, S. L. Henderson, K.B. Howard, R. Kelmar, K. Lee, L. Morales, S. Moylan, Z. Raman, W. Tan, L. E. Weghorn, and M. Wiescher "Lifetime measurements of excited states in 15O". Phys. Rev. C 103, 045802 (2021).
A. Majumdar*, K.V. Manukyan, J.M. Roach*, S. Dede*, D. Robertson, P.C. Burns and A Aprahamian, Irradiation-Driven Restructuring of UO2 Thin Films: Amorphization and Crystallization, ACS Applied Materials & Interfaces. ACS Appl. Mater. Interfaces, 13, 35153−35164 (2021)
J.M. Roach*, K.V. Manukyan, A. Majumdar*, S. Dede*, A.G. Oliver, P.C. Burns, A. Aprahamian, Hyperstoichiometric Uranium Dioxides: Rapid Synthesis and Irradiation-Induced Structural Changes, Inorg. Chem. 60, 24, 18938–18949, (2021).
R. Kelmar, K.V. Manukyan, A. Simon, A. Aprahamian, Preparation and Characterization of Isotopically Pure Mo Targets for Nuclear Science Measurements, Nuclear Instruments and Methods A. 1034, 166763, 4 pages (2022).
S. Dede*, K.V. Manukyan, J.M. Roach*, A. Majumdar*, P.C. Burns, and A. Aprahamian, Irradiation-induced amorphization of UO2 films prepared by spraying-assisted combustion synthesis, Applied Surface Science. 603, 154437 11 pages (2022).
A. Majumdar*, K.V. Manukyan, W. Tan, S. Dede*, J.M. Roach*, A. Couture, P.C. Burns, A. Aprahamian, Neutron Capture of UO2 Targets Prepared by Spin Coating Assisted Combustion Synthesis, Nuclear Inst. and Methods in Physics Research, A 1045 167551 6 pages (2023).
J.M. Roach, K.V. Manukyan, S. Dede, P.C. Burns, A. Aprahamian, Combustion synthesis of Eu2O3 nanomaterials with tunable phase composition and morphology, Journal of Solid State Chemistry 326, 2023, 124235 (8 pages)
S. Dede, S.D. Essenmacher, P. Gastis, K.V. Manukyan, S.A. Kuvin, H.Y. Lee, J.M. Roach, P.C. Burns, A. Aprahamian, Electrospraying deposition and characterization of potassium chloride targets for nuclear science measurements, Nuclear Inst. And Methods in Physics Research, A1055 (2023) 168472 (6 pages).
S. Dede, K.V. Manukyan*, J. M. Roach, D. Robertson, P.C. Burns, and Ani Aprahamian, Irradiation-enhanced Interactions at UO2/Al2O3/Al Interfaces, J. Phys. Chem. C 2023, 127, 20, 9850–9857
A. Majumdar, K.V. Manukyan, S. Dede, J.M. Roach, P.C. Burns and A. Aprahamian, UO2 target preparation with spin coating assisted solution combustion synthesis, EPJ Web of Conferences 285, 03004 (2023) https://doi.org/10.1051/epjconf/202328503004
Two PhD dissertations, 14 Invited Talks, Seminars, and Colloquia, 13 Oral presentation, 23 poster presentations
Products

## Slide 27
The fundamental aspects of SCS of actinide oxides have been obtained.
Simple and efficient SCS-based methods of thin target preparation have been developed.
A large number of targets have been prepared, fully characterized, and tested.
Conclusions

## Slide 28
Aprahamian, Ani
Burns, Peter
Sigmon, Ginger
Szymanowski, Jennifer
Cabanas Noah (ND)
Dede, Stefania (TA&M and ND, now LLNL)
Majumdar, Ashabari (ND)
Roach, Jordan (ND, now ORNL)
Acknowledgments
LANL collaborators
Bredeweg, Todd
Couture, Aaron
Gastis, Panos
Kuvin, Sean
Lee, Hye Young

## Slide 29
Thank you

## Slide 30
Thermodynamic modeling of SCS reactions









Calculated adiabatic temperature (Tad) and composition of equilibrium products as a function of  (C2H5NO2/UO2(NO3)2) molar ratio and the number of water moles (n).
UO2(NO3)2 + C2H5NO2 + nH2O system

## Slide 31
Mechanistic investigations of SCS: UO2(NO3)2 + C2H5NO2 + H2O system
Visual representation of the precipitated complex structure obtained from reactive solutions (A), hydrogen bonding represented by black dotted lines between Gly-1 (B) and Gly-2 (C) ligands with neighboring chain structures.

## Slide 32
Elemental uniformity of oxides
Th0.25U0.75O2
UO2:1%Ni

## Slide 33
Ion-irradiation-induced structural changes