## Slide 1: Fusion Energy Sciences: Tritium Production Session Introduction and Overview
Paul Humrickhouse
February 24, 2024

## Slide 2: Overview
Tritium breeding- why and how much is required to support fusion?
Breeding blanket materials:
  Breeder materials
  Neutron multipliers
  Structural materials
  Coolants
  Other materials
  Blanket concepts
Discussion Topics

## Slide 3: The need for tritium breeding
The D-T fusion reaction is the most achievable
But tritium decays with a 12.3 year half-life, and therefore has no natural supply
Small amounts produced by fission reactors can supply short-pulse research devices
But 55.6 kg T/GWf-yr is required for sustained operation
This will require that it use the fusion neutrons to breed its own tritium supply, with a tritium breeding ratio (TBR) > 1

## Slide 4: T breeding from Li
Fusion neutrons can produce lithium from both naturally occurring isotopes:
  n + 6Li → 4He + T + 4.785 MeV
    Large cross section at thermal energies
    Exothermic: produces additional energy!
  n + 7Li → 4He + T + n’ - 2.5 MeV
    Produces tritium and a neutron
F. Hernandez, Fusion Engineering and Design 137 (2018) 243-256.
It is advantageous to enrich in 6Li to an extent (typically 40-90%) that depends on the blanket concept and other materials present

## Slide 5: Neutron multipliers
TBR = 1 is achieved when every fusion neutron produces a triton from lithium
The multitude of other structures and components necessarily present in a fusion reactor will also absorb neutrons
This can be compensated for by incorporating neutron multipliers, elements that undergo (n,2n) reactions
Good multipliers have a high (n,2n) cross section and low total absorption cross section- Be and Pb are primary candidates
Beryllium is a superior multiplier but has drawbacks (toxicity, supply chain, U impurities)
F. Hernandez, Fusion Engineering and Design 137 (2018) 243-256.
M. Nakamichi, in Comprehensive Nuclear Materials 2nd ed (2020).

## Slide 6: Candidate breeder/multiplier materials
Breeders
  Liquid Metals:
    Lithium (Tmelt = 180 ºC)
    Pb84.3Li15.7 (Tmelt = 235 ºC)
  Solids: separate breeder and multiplier
    Ceramic breeders: Li2TiO3, Li4SiO4
      Others with less favorable absorption/neutron activation possible
    Multipliers:
      Be (metal)
      Beryllide intermetallics: Be12Ti, Be12V, Be12Cr
        Others with less favorable absorption/neutron activation possible
  Molten Salts:
    FLiBe [2LiF + BeF2] (Tmelt = 459 ºC)
    FLiNaBe [LiF + NaF + BeF2], (Tmelt = 305 ºC)
Solid ceramic breeders
F. Hernandez, IEEE Transactions on Plasma Science, 2018
Beryllide intermetallic multipliers
R. Gaisin, Fusion Engineering and Design 161 (2020) 111862.

## Slide 7: Can we achieve TBR > 1(+ε)?
Clearly yes in idealized configurations
Whether achievable in a fusion reactor is a question of design integration…
Multipliers need to offset neutrons lost through penetrations and absorption in all other components and materials,
  e.g. FW, blanket structure, divertor, pellet injectors, heat & current drive components, diagnostics, etc.
L. El-Guebaly, in “Fusion Energy and Power: Applications, Technologies and Challenges” (2015)
These go higher with multiplier addition

## Slide 8: Neutron activation considerations
When considering other elements in breeder, multiplier, or structural materials, neutron activation is a primary consideration
= V alloy, Li2O
= RAFM steel, PbLi
= RAFM steel, Li4SiO4
= SiC composite, PbLi
= RAFM steel, PbLi
= SiC composite, Li4SiO4
M. Zucchetti, Fusion Engineering and Design 136 (2018) 1529-1533.
P. W. Humrickhouse, Fusion Science and Technology (2024, submitted)
All D-T fusion reactors will create significant quantities of radioactive material
Avoidance of long-lived waste and high decay heat (active cooling) requires low-activation materials
  Many common alloying elements (Ni, Co, Mo, Nb, etc.) need to be avoided

## Slide 9: Structural Materials
The need to reduce short (decay heat) and long (waste) term activation has driven the development of structural materials for fusion
Three primary candidates:
  Reduced-Activation Ferritic/Martensitic (RAFM) Steel
    Most mature option, likeliest for near-term deployment; examples:
    F82H (Fe-8Cr-2W-0.2V-0.04Ta)
    EUROFER-97 (Fe-9Cr-1W-0.2V-0.12Ta)
  Vanadium Alloys
    V-4Cr-4Ti
  Silicon Carbide (SiC) composites

## Slide 10: Other materials
Coolants
  Solid breeders require a coolant
  Liquid breeders can in principle also act as a coolant, but have some drawbacks for this purpose
    High pressure drops due to magnetohydrodynamic forces (liquid metals) or high viscosity (molten salts) at high flow rates
    Other undesirable properties such as low thermal conductivity in molten salts
  In both cases, primary coolant candidates are:
    Helium
    Water
Tungsten
  Tungsten appears in many components in and around the breeding blanket:
    Plasma facing materials in the divertor
    Armor on the FW/blanket
    Conducting shells used to stabilize the plasma
    Shielding
  Its effect on breeding may be mixed; it’s a strong thermal absorber but can also multiply at high energy*
*B. Sorbom et al., Fusion Engineering and Design 100 (2015) 378-405.

## Slide 11: Blanket Concepts
Blanket concepts pair breeder/multiplier with structural and other materials and coolants based on their compatibility
  PbLi, solid breeders typically paired with RAFM steel structure and helium or water coolant
    These are the most studied designs
  Lithium traditionally paired with vanadium
    It may help getter impurities (O, H, T) that would otherwise significantly impact vanadium
    Poor or questionable compatibility with other candidate structural materials
  Material solution for FLiBe unclear
    High melt temperature (459 ºC) leaves little/no temperature window for operation with RAFM steel (< 550 ºC)
    Corrosion compatibility with all materials a concern
US Design – Dual Cooled Lead Lithium (DCLL)
M. Abdou et al. / Fusion Engineering and Design 100 (2015) 2–43
JA DEMO Design – Water Cooled Ceramic Breeder (WCCB)
Y. Someya, 2018 US-JA Workshop

## Slide 12: Discussion topics for the session
Fusion reactors are anticipated to breed the tritium needed to fuel energy production. However, quantities of this isotope will be needed during reactor startup, and it may be in short supply. Are there production processes or reactor materials that can be used to establish a source of tritium for fusion energy applications?
Which nuclear data are necessary to support testing and operation of liquid blankets? Ceramic blankets?
What are the uncertainties and sensitivities to tritium breeding ratio?
Is the accuracy of nuclear data sufficient to predict activation of breeder blankets?
Nuclear reactions will contribute to chemical changes in breeder blankets. Can nuclear cross sections be used to accurately predict transmutation of materials in blankets?