## Slide 1
Andrew S. Voyles
13 June 2018 – Program Review for NSSC2 – TA1
REBCO and BSCCO fast neutron irradiations at the LBNL 88-Inch Cyclotron
Lee A. Bernstein
Department of Nuclear Engineering
University of California – Berkeley
Nuclear Science Division
Lawrence Berkeley National Laboratory
http://nucleardata.berkeley.edu

## Slide 2
Thick target deuteron breakup has been known as an effective source of fast, forward focused neutrons and was even considered for 239Pu production in the 1940s*
Thick target deuteron breakup (TTDB) neutron beams on light targets are also strongly forward focused (the neutrons follow the direction of the deuteron beam)
10+ barns/sr
Low-Z targets are particularly good since they have the lowest dE/dx and therefore the longest effective target thickness
*Thanks to Ian Thompson (LLNL)

## Slide 3
We’ve quantified our Thick Target Deuteron Breakup Neutron Source (TTDBNS) using both Time-of-Flight* and foil activation
Mounted Foil Holder
*K.P. Harrig et al., Nuclear Inst. and Methods in Physics Research, A 877 (2018) 359–366
Our goal was to develop a physics-based
model of neutron production
Time-of-Flight (TOF)
Double Time-of-Flight*
Neutrons scatter off a target cell neutron scintillator and into an array of scatter cells allowing for energy determination down to ≈0.5 MeV without contributions from temporally adjacent beam pulses.
Foil Activation
Arrays of activation foils are located at defined angles with respect to the breakup target and the spectrum is determined via spectral decomposition.

## Slide 4: Jon Morrell* developed a combined 5 parameter model that describes the double-differential TTDB neutron production cross section
Shape & Magnitude
1 parameter each
1R. Serber, Phys. Rev 72, 11 (1947)
2C. Kalbach Phys. Rev. C 95, 014606 (2017).
3Meulders (1975) - 16, 33, 50 MeV
4Saltmarsh (1977) - 40 MeV
P(En,𝛳) from R. Serber1 (Phys. Rev. 72, 11 (1947)
Pre-equilibrium cross section from Kalbach2
Talys Maxwell-Boltzmann evaporation
One flat background parameter
Slowing (ded/dx) from SRIM
Fit yields to measurements and literature data3,4
Jon Morrell
Our Results were just published: J.T. Morrell et al., Phys. Rev. C 108, 024616 (2023). https://doi.org/10.1103/PhysRevC.108.024616
*UCB Ph.D. 2021, now at LANL

## Slide 5: We benchmarked the model for 40 MeV deuterons on a thick Be breakup target
=1.4x1011 n/s/cm2 @ 1 cm
=2.0x1010 n/s/cm2 @ 10 cm
=2.2x105 n/s/cm2 @ 10 m
40 MeV deuterons*
50 MeV deuterons*
=7.5x1012 n/s/cm2 @ 1 cm
=1.2x1011 n/s/cm2 @ 10 cm
=6.7x105 n/s/cm2 @ 10 m
*Assumes 20 µA beam and 0°
Spectral variation as a function of angle allows for simultaneous measurements

## Slide 6: TTDB neutron beams are available at two caves at the 88-Inch cyclotron*
Cave 0 (This talk)
High-level cave capable of running up to 1.5 kW of beam power (ASE limit).
Breakup in Vault or Cave.
Max flux : 1012 n/s/cm2
*The 88-Inch Cyclotron: A one-stop facility for electronics radiation and detector testing. M.Kireeff-Covo et al.,. Measurement, 127, (2018), p. 580-587.https://doi.org/10.1016/j.measurement.2017.10.018 .
Cave 5 (See J.A. Brown’s talk)
“TOF Quality” flight path from 7-22 m.
Irradiation Jig
GENESIS

## Slide 7: REBCO and BSCCO Irradiation “Volunteers” at the 88-Inch cyclotron (20 hours @ a total integrated charge of 0.2 Coulomb)
Abby Lee
(GS)
Elan
Park-Bernstein
(UG)
Chris Reis
(GS)
Lee
Bernstein
Andrew
Voyles (Staff)
BSCCO
samples
REBCO
BSCCO
BSCCO

## Slide 8: There is significant variation in flux across the different REBCO strips due to their proximity to the deuteron beam
REBCO Strips in HEIFER
Gafchromic Overlay
Elan is developing a Monte-Carlo integration code to calculate the spectrum over each REBCO strip
Approximately ½ of each foil is in-line with the deuteron beam
REBCO
Hastelloy (mostly Ni)

## Slide 9: REBCO Low Energy (14° < q < 68°)
57Co
56Co
58Co
137Cs from
138Ba(n,pn)
0.2 A•s irradiation @ Ed=40 MeV

## Slide 10: REBCO Low Energy (14° < q < 68°)
56Co
88Y
88Y
59Fe
59Fe from
62Ni(n,a)
60Co from
63Cu(n,a)
40K (bg)
0.2 A•s irradiation @ Ed=40 MeV

## Slide 11: How do our measured conversion fractions compare to predictions from our neutron model?
Chart: Neutron Energy (MeV)
58Ni(n,pn)57Co | 2.8619e-08 | 0.00012157 | 0.0054643 | 0.030669 | 0.079667 | 0.14822 | 0.23297 | 0.32401 | 0.41187 | 0.48815 | 0.55772 | 0.61673 | 0.66627 | 0.70954 | 0.74136 | 0.7647 | 0.78035 | 0.7884 | 0.79409 | 0.7927 | 0.78725 | 0.77875 | 0.7686
Can assay H production from 56-58Co
(n,p) data above 20 MeV is essential
He production can be calculated
IFMIF & FPNS use 40 MeV deuterons
This energy might be too high!
VERY Preliminary !!!
q1 | q2 | 56Co (x1000) ppb | 57Co (ppb) | 58Co (ppb)
80 | 81 | 0.68 | 0.04 | 0.12
76 | 79 | 1.34 | 0.07 | 0.19
79 | 80 | 1.16 | 0.06 | 0.16
70 | 75 | 2.68 | 0.14 | 0.34
14 | 68 | 61.52 | 1.72 | 2.12
1.46
1.81
ENDF +
Simple Geometry
Similar values (0.7 ppb) were seen in the BSCCO from 107Ag(n,2n)105Ag

## Slide 12: Chris Reis is spearheading Gas Production/Materials Characterization at UC Berkeley with Hosemann Nuclear Materials Group and LBNL’s Molecular Foundry
Work at the Molecular Foundry was supported by the Office of Science, Office of Basic Energy Sciences, of the U.S. Department of Energy under Contract No. DE-AC02-05CH11231.

## Slide 13: US-Japan High Energy Physics Collaboration to aid with superconductivity measurements using VTI Probe at IRCNMS
US-Japan HEP collaboration LBNL Leads Chris Reis, Tengming Shen, et. al coordinating with KEK collaborators Toru Ogitsu, Masami Iio, et. al to assess radiation effects on superconductivity
15.5 Tesla Variable Temperature Insert (VTI) specially designed for hot samples to be used at International Research Center for Nuclear Materials Science (IRCNMS)
Changes to Critical Current, Critical Temperature, n-value, Irreversibility field, etc., are key parameters to be assayed.
Members of the US Magnet Development Program
Notes: IRCNMS - International Research Center for Nuclear Materials Science
VTI - Variable Temperature Inserts

## Slide 14: Conclusions
Future plans
Perform cryogenic (LN) irradiations using a new jig being designed by the Hosemann/Prestemon group
Test a new high-intensity Beryllium target developed with a corporate partner (NorthStar)
Irradiate NIF final stage optics as part of the new IFE-STARFIRE collaboration
Summary
Several ppb of the Ni in the sample were transformed to Co during a short low-intensity run, making H in the process. Helium production would be similar.
Lots of Y reactions products (Is this a big problem?)
A full scale run (x25 integrated charge at 0°) would yield 0.1-0.2 ppm gas production plus lots of displacements and secondary particle production

## Slide 15: Collaborators and Acknowledgments
L.A. Bernstein1,2, C. Gesteland1, P. Hosemann1, Y.-H. Lee1, M. Nair1, E.B. Park-Bernstein1, S. Prestemon2, C. Reis1,2, T. Shen2, A.S. Voyles1
1University of California – Berkeley Department of Nuclear Engineering
2Lawrence Berkeley National Laboratory
This work has been performed under the auspices of the U.S. Department of Energy by Lawrence Berkeley National Laboratory under contract No. DE-AC02-05CH1123 and the US Nuclear Data Program
Mehul Nair
Tengming Shen
Chase Gesteland
Peter Hosemann
Soren Prestemon