## Slide 1: 20 T – Cos(𝛳) Designs
G. Vallone1, P. Ferracin1, V. Marinozzi2
03-August-2022
1LBNL, 2FNAL
General MDP Meeting

## Slide 2: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 3: Introduction
We want to compute the mechanical stresses for 20T cos(ϑ) design
  CT I: 4 Bi2212 layers
  CT II: 2 Bi2212 layers
We select CT II as best ($) design
CT I
CT II

## Slide 4: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 5: Magnetic Field
ANSYS magnetic model
  20 T central field at I = 13 kA, with the iron yoke
  Results consistent with Roxie model
  Used to extract e.m. forces for mechanical study
B, T
No Iron
B, T
With Iron

## Slide 6: Magnetic Model Results
Reasonable Lorentz stress in all layers
Assumed mechanical limits:
  Bi2212 (layer 1, 2): 125 MPa
  Nb3Sn (layer 3 to 6): 175 MPa
Layer | Bpeak | jo | Lorentz Stress
/ | T | A/mm2 | MPa
1 | 20.2 | 305 | -81
2 | 18.1 | 305 | -119
3 | 16.0 | 215 | -137
4 | 13.0 | 215 | -133
5 | 11.7 | 398 | -144
6 | 11.0 | 398 | -128

## Slide 7: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 8: Modeling assumptions
Coil modelled as linear elastic
Rigid structure around the outer coil
Rigid winding poles, no prestress
Frictionless contact on the intercoil insulation
Glued contact on the interlayers
Rigid
Structure
Separation
Allowed
Intercoil
Frictionless
Contact
Interlayer
Bonded Contact

## Slide 9: Rigid Structure
Max stress, mid plane:
  Radial: 183 MPa, Azimuthal: 353 MPa
  Inner radius stress due to coil deformability
Lorentz stress on layer 1 was only 80 MPa, but bending…
Radial
Stress
Azimuthal
Stress

## Slide 10: Rigid Structure, Intercepting (Fixed intercoil)
Intercepting structure - intercoil fixed (u=0)
  Removes bending and accumulation of radial forces
140 MPa radial, 155 MPa azimuthal
With perfect interception between coils, layer 2 has to be stress managed
  Radial+azimuthal stresses exceed limits
Radial
Stress
Azimuthal
Stress

## Slide 11: Rigid Structure, Intercepting (Fixed intercoil+interlayer)
Intercepting structure – intercoil and interlayers fixed (u=0)
Even with perfect interception between layers, layer 2 has to be stress managed
101 MPa radial, 147 MPa azimuthal
Radial
Stress
Azimuthal
Stress

## Slide 12: Result Summary - Intercepting
In red stresses that are over conductor limits
Rigid intercoil + interlayer close to Lorentz stress

## Slide 13: Rigid Structure, Layer 2 Stress Managed
If we stress manage L2, do we need to do the same on L1?
  Is the additional stiffness from stress management enough to remove the stress peaks in L1?
  Model with L2 in stainless steel (coil and spacers)
179 MPa radial, 302 MPa azimuthal
Layer 1 has to be stress managed
  Azimuthal stresses exceed limits
Radial
Stress
Azimuthal
Stress

## Slide 14: Result Summary – Stress Management
We can repeat the exercise ‘stress-managing’ only some layers (x means stress managed)
Stress managed solutions show that in reality we might be able to stress manage only layer 1, 2, but layer 3 is very close to the limit
  Field is low, but stress might become higher when outer structure and stress management are not ‘ideal’
  On the other hand, coil 3 can work with no stress management

## Slide 15: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 16: Steel Intercoil – Magnetic Field
5 mm thick stainless steel intercoil shim/structure
Current ramped up to get back to 20 T
  From 13 kA to 13.45 kA
  Lower margin but this is a ‘mechanical’ test
Old
New
Design 2, I = 13.5 kA, B = 20 T |  |  | 
Layer | Bpeak | jo | Lorentz Stress
/ | T | A/mm2 | MPa
1 | 20.3 | 317 | -84
2 | 18.1 | 317 | -123
3 | 15.5 | 223 | -139
4 | 12.8 | 223 | -136
5 | 11.5 | 413 | -148
6 | 10.8 | 413 | -134
Design 1, I = 13.0 kA, B = 20 T |  |  | 
Layer | Bpeak | jo | Lorentz Stress
/ | T | A/mm2 | MPa
1 | 20.2 | 305 | -81
2 | 18.1 | 305 | -119
3 | 16.0 | 215 | -137
4 | 13.0 | 215 | -133
5 | 11.7 | 398 | -144
6 | 11.0 | 398 | -128

## Slide 17: Case A – Steel ‘Open Rings’
Intercoil shims open at 90°
Azimuthal: 331 MPa, Radial: 173 MPa
  Does not solve the bending problem on the first layer
  Similar results with closed rings (shells)
Radial
Stress
Azimuthal
Stress

## Slide 18: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 19: A test with an SMCT ‘Design’ - Assumptions
A ‘test’ design obtained adding 5 mm thick stainless steel spars to the CT design
  Mandrel = spar + wedges (ribs)
  Frictionless contacts between coil and mandrels
  Frictionless contact between mandrels
  Layer 5 and 6 impregnated, with no stress management
Rigid
Structure
Interlayer
Bonded Contact
Frictionless
Contact

## Slide 20: A test with an SMCT ‘Design’ - Results
Limit stresses exceeded on the inner coil upper right edges
Coil 2 and 3 are ok
Eqv.
Stress
Eqv.
Stress

## Slide 21: A test with an SMCT ‘Design’
The high stresses are due to radial forces and contact with the second layer spar
This result suggests that we need more radial support
Eqv.
Stress

## Slide 22: SMCT Designs – Mid-plane rib
Adding a mid-plane ‘shim/rib’
High stresses in layer 1 and 2
  The rib does not solve the issue
Layer 3 to 6 are fine
Eqv.
Stress
Eqv.
Stress

## Slide 23: SMCT Designs – Aligned Wedges
Aligned wedges near the mid-plane
Inner coil still not working
Eqv.
Stress
Eqv.
Stress

## Slide 24: SMCT Designs – Shared Mandrel
New design with a shared mandrel for layer 1 and 2 (an idea by Sasha)
Stresses are worse in this configuration, but probably this is due to this particular coil design
Eqv.
Stress
Eqv.
Stress

## Slide 25: Design Comparison
None of the proposed designs solves the stress issues in the inner coil
  Probably we need more ribs in the first 2 layers
  A magneto/mechanical optimization might help
Test
Mid Plane Rib
Aligned Ribs
Shared Mandrel
seqv.,Pa

## Slide 26: Design 19b – Equivalent Stress
Much better
  Spikes in LTS coils might be solvable
  LTS coil is not within the desired limits
    Not clear why
HTS
LTS

## Slide 27: Design 19b – Total Displacement
Still not clear, to be investigated
Seems that the stress peaks are due to the larger wedges near the pole region
HTS
LTS

## Slide 28: Design 21 – Equivalent Stress
Much better for the HTS coil!
  Layer 1 is almost all fine
LTS also almost fine
HTS
LTS

## Slide 29: Design 21 – Total Displacement
To be discussed
Last week solution was with rigid layer 3
HTS
LTS

## Slide 30: Design 22 – Equivalent Stress
Similar results in LTS layers
Smaller region where the limits are exceeded
  Peak value is lower (176 MPa vs 246 MPa), with finer mesh (contacts did not work otherwise)
We are very close
HTS
LTS

## Slide 31: Design 22 – Total Displacement
For reference
HTS
LTS

## Slide 32: Design 23 – Equivalent Stress
Reinforced layer 3
LTS is fine
HTS still has a small region not working
  Could be fixed playing with the spar thickness? E.g. decreasing t1/t3 and increasing t2
  Might be interesting investigating it with a cable model/different material model
HTS
LTS

## Slide 33: Design 23 – Total Displacement
For reference
HTS
LTS

## Slide 34: Design 23b – Equivalent Stress
Improves field quality with modifications to layer 1
Stresses are similar
Deviates a bit from a CCT design
  In reality the field quality of CCT is not captured in 2D
HTS
LTS

## Slide 35: Design 23b – Total Displacement
For reference
HTS
LTS

## Slide 36: Design 24 – Equivalent Stress
Reinforced layer 4
LTS is almost fine
HTS is fine!
HTS
LTS

## Slide 37: Design 24 – Total Displacement
For reference
HTS
LTS

## Slide 38: Design 23c – Equivalent Stress
New cable for layer 5/6
Slightly worse – layer 5/6 are softer
HTS
LTS

## Slide 39: Design 23c – Total Displacement
For reference
HTS
LTS

## Slide 40: Design 25 – Equivalent Stress
New cable (width <) for coil 2, coil 3 as design 23
Similar to 23c
HTS
LTS

## Slide 41: Design 25 – Total Displacement
For reference
HTS
LTS

## Slide 42: Design 26 – Equivalent Stress
Coil 2 and 3 = design 25
Coil 1, new cable (from 20.65 mm to 18.59 mm)
Similar to 23c
HTS
LTS

## Slide 43: Design 26 – Total Displacement
For reference
HTS
LTS

## Slide 44: 23c/25/26 Comparison
Profile very similar, slight change in actual peak stress
It seems that the stress peaks are not a function of the cable thickness but just of the block number/position
25
26
23c
26
25
23c

## Slide 45: Design History
Test 1
Mid Plane Rib
Aligned Wedges
Shared Mandrel
Coil 1
2 Turns
Layer 1
3/2/1 Turns
Coil 1
CCT / 1 Turn
Layer 3
5 Blocks
Layer 3/4
5 Blocks

## Slide 46: Design 27 – Magnetic Field
Central field 19.85
  Double checked v26, B1 = 19.84
  Keeping it like this for fair comparison

## Slide 47: Design 27 – Equivalent Stress
Changes
HTS
LTS

## Slide 48: Design 26 – Total Displacement
For reference
HTS
LTS

## Slide 49: 26 vs 27
HTS
LTS
v26
v27

## Slide 50: Design 27b – Equivalent Stress
HTS same
LTS is better now
HTS
LTS

## Slide 51: 27b vs 27
v27
HTS
LTS
v27b

## Slide 52: Design 28 – Equivalent Stress
New geometry, optimized for quench protection
  Layer 5/6: wider cable
  LTS ok, HTS with larger peak stress but similar peak stress area
    Should we check this region with a strand submodel?
HTS
LTS

## Slide 53: Design 28 – Total Displacement
For reference
HTS
LTS

## Slide 54: Design 28 – Debonded – Equivalent Stress
Design 28, layer 5/6 debonding from the pole (no prestress scenario)
Same stress in HTS, new spike due to coil 5/pole 6 contact
  Might be removed aligning pole turns of layer 5 and 6
HTS
LTS

## Slide 55: Design 28 – Debonded – Total Displacement
For reference
HTS
LTS

## Slide 56: Comparison
Similar mechanical performances for design 28
Debonding effect on layer 5 can likely be reduced/removed by prestress
28, debonded
28
26 (ASC2022)

## Slide 57: To Do
Stresses in the structure
  Add wedge stress / stress from ribs flows into them
Fix stresses in spar 1
  Check the impact of spar 1 thickness on the stress (adding material towards the aperture)
  Add pocket on the pole symmetry (can remove b.c.)
  Ellipse shaped spar might also improve
Understand peak stress in pole turn layer 1

## Slide 58: Stress Management Structure
A good amount of radial stress flows trough the aligned ribs
  They seem to work as intended!
Equivalent stress high
  Peaks mostly in the corners, but critical region at innermost spar inner radius (1600 MPa, azimuthal)
    We probably need to increase a bit the spar thickness
  Still, we would need a strong steel to withstand these stresses
Layer 1 spar

## Slide 59: Index
Introduction
Magnetic model results
Mechanical model results
  Rigid structures and stress management
  Thick intercoil study
  SMCT Study
Conclusion

## Slide 60: Conclusion
Solution with rigid intercoil shims shows that layer 2 requires stress management (both radial and azimuthal)
Solution with ‘stress-managed’ layer 2 shows that also layer 1 needs stress management
  Layer 1 sees high azimuthal stresses even when introducing thick intercoil shims
  Layer 3 is very close to the stress limits, might also need stress management
  Layers 4, 5 and 6 seem feasible also with no stress management (with a rigid structure around)
Thick steel intercoils do not provide enough stiffness to reduce the stresses in a CT design
Mixed SMCT and CT designs are being considered
  No viable solution for the moment, optimization in progress

## Slide 61: Extra

## Slide 62: Rigid Structure and Coil
Coil modelled as linear elastic, E = 1e4 GPa
  ~226 MPa radial, 195 MPa azimuthal
  REMOVE
Radial
Stress
Azimuthal
Stress

## Slide 63: Rigid Structure, Intercepting (Rigid intercoil)
Coil modelled as linear elastic, E = 20 GPa
Intercepting structure, rigid intercoil (E=1e7 GPa)
~127 MPa radial, 248 MPa azimuthal
Should try with thicker intercoil
IN EXTRA / Non funziona il modello (contatti?)

## Slide 64: Case 0 – Rigid Intercoil
Rigid 5 mm thick intercoil shells (locked on x=0)
Azimuthal: 163 MPa, Radial: 154 MPa
Not super promising – reality will be worse

## Slide 65: Case B – Steel Shells
Intercoil shims closed at 90° (shell design)
Azimuthal: 325 MPa, Radial: 167 MPa
  Similar to open rings and more complicated to assembly / not worth considering

## Slide 66: Case C – Steel Collars – Coil Impregnated
Intercoil shims closed at 90° (shell design)
Coils impregnated together
Still does not work

## Slide 67: SMCT-CT hybrid: v17
2 layer HTS, 4 layer LTS
Strands: 0.9 – 1.1 – 0.8 mm, 40 – 44 – 35
Cable width: 20.65 – 26.82– 15.51 mm
Stabilizer/Superconductor: 3 – 1 – 1.2
Coil width: 158 mm
Current: 14200 A
Peak field: 20.8 – 16.26 – 13.36 T
Margin: 84.4 – 85.3 – 85.6 %
Jcu on LTS: 1479 A/mm2

## Slide 68: SMCT-CT hybrid: v18
2 layer HTS, 4 layer LTS
Strands: 0.9 – 1.1 – 0.8 mm, 40 – 44 – 35
Cable width: 20.65 – 26.82– 15.51 mm
Stabilizer/Superconductor: 3 – 1 – 1.2
Coil width: 158 mm
Current: 14200 A
Peak field: 21.2 – 16.23 – 13.09 T
Margin: 84.9 – 85.2 – 84.3 %
Jcu on LTS: 1479 A/mm2