## Slide 1: 20 T Hybrid Magnet – Cos(θ) Design
M. D’Addazio, P. Ferracin, V. Marinozzi, G. Vallone

## Slide 2: Design criteria of 20 T hybrid magnet
Coil and magnet parameters
  Free coil aperture (diameter) 50 mm
  Operational bore field 20 T
  load-line fraction @ 1.9K: Iop/Iss <= 87 %
  2D Geometrical harmonics bn<3 units for n<10 (at Rref=17 mm)
Quench protection
  All coils powered in series
  Maximum hot spot temperature 350 K
Mechanics
  Maximum Nb3Sn coil stress <180 (<150) MPa at 1.9 (293) K
  For the HTS <120 MPa

## Slide 3: Magnetic Analysis - I
Layer 1-2: HTS (Bi2212)
Layer 3-4: LTS1; layers 5-6: LTS2 – Both Nb3Sn
Strands [mm]: 0.9 – 1.1 – 0.8
Turns[-]: 36 – 40 – 44
Cable width [mm]: 18.59 – 24.38 – 19.50
Stabilizer/Superconductor [-]: 3 – 1 – 1.8
Coil width [mm]: 143
Current [A]: 13500
Peak field [T]: 20.45 – 15.95 – 13.6
Margin [%]: 87 – 84 – 87
Jcu on LTS [A/mm2]: 950
Version 28

## Slide 4: Magnetic Analysis - II
Version 28 |  |  | 
Layer | Bpeak | Jo | Lorentz Stress
/ | [T] | [A/mm2] | [Mpa]
1 | 20.3 | 360 | -110
2 | 18.0 | 360 | -138
3 | 15.8 | 229 | -128
4 | 13.7 | 229 | -129
5 | 13.2 | 379 | -175
6 | 12.0 | 379 | -145
Assumed Mechanical Limits:
  Bi2212 (layer 1, 2): 125 MPa
  Nb3Sn (layer 3 to 6): 175 MPa
Notes: Dati simulazione magnetico G. Vallone con versione v28 (struttura infinitamente rigida)

## Slide 5: Magnetic Analysis - III
Version 28
Bbore [T] = 19.99
Bpeak [T] = 20.35, 15.82, 13.18
Margin [%]: 80.3, 80.8, 78.5
Notes: Margin diversi, probabilmente differenza Ansys-Roxie (verificare)

## Slide 6: Mechanical Analysis – I
Equivalent Stress
Infinitely Rigid Structure
Collar
Poles
Spare + ribs
Wedge
Version 28

## Slide 7: Mechanical Analysis – II
Equivalent Stress
Infinitely Rigid Structure

## Slide 8: Mechanical Analysis - III
Thickness:
Collar – 25 mm
Pad – 50 mm
Yoke – 320 mm
Shell – 80 mm
Key x2 – 10x40 mm
Characteristic:
Friction: 0.2
Layers 1 – 4: Spar + ribs
Layers 5 – 6: Pole + Wedges
Interference: 2 mm on the horizontal key  first attempt for the max allowable stress in the shell
Shell
Yoke
Pad
Collar
Collar
Poles
Spare + ribs
Wedge
Version 28
Mechanical Structure
Infinitely Rigid Structure

## Slide 9: Mechanical Analysis - IV
Coils Boundary Conditions:
Layers 1 – 4: outer node radially coupled to the rib
Layers 5 – 6: all the nodes are coupled to the wedges
Mechanical Structure

## Slide 10: Mechanical Analysis – V
Equivalent Stress
HTS
LTS
Pre-stress
EM forces
Cool down

## Slide 11: Mechanical Analysis – VI
Equivalent Stress
Pre-stress
EM forces
Cool down
Mandrel

## Slide 12: Mechanical Analysis – VII
Equivalent Stress
Pre-stress
EM forces
Cool down
Layers 5-6: Poles and Wedges

## Slide 13: Mechanical Analysis – VIII
Equivalent Stress
Pre-stress
Cool down
EM forces
Pad
First Principal Stress
First Principal Stress

## Slide 14: Mechanical Analysis – IX
Equivalent Stress
Pre-stress
Cool down
EM forces
Yoke
First Principal Stress
First Principal Stress

## Slide 15: Mechanical Analysis – X
Equivalent Stress
Pre-stress
Cool down
EM forces
Shell

## Slide 16: Results summary
Comments on the mechanical structure model:
Corner effects in HTS and LTS coils
Limits are exceeded in the mandrel (bending)
Spikes near the keys in both pad and yoke

## Slide 17: Next Steps
Mechanical structure optimization:
Influence of the interference
Influence of the key position
Dimensions of the mechanical structure