## Slide 1: Development of a 15 T Model Dipole for a Very High Energy Hadron Collider
A.V. Zlobin
APT seminar
17 April 2018

## Slide 2: Outline
Introduction
15 T dipole magnet design and parameters
  Magnetic and mechanical analysis
  Conductor R&D
  Magnet fabrication status
Conclusion

## Slide 3: Introduction
During past two decades Nb3Sn accelerator magnet technology has made significant progress from short demonstration models to long prototypes
  HL-LHC: 11-12 T magnets with ~20% margin
Future needs
  affordable for mass production 16 T dipole (FCC)
11 T dipole MBH for LHC collimation system upgrade
150-mm aperture IR quadrupoles MQXB for HL-LHC

## Slide 4: Open questions and goals
Open questions
  long training
  conductor degradation
  cost
US-MDP goals

## Slide 5: Challenges and motivation
The base for success: better design and analysis tools, new materials (Nb3Sn wires), advanced technologies

## Slide 6: Cos-theta coil
Coil: 60-mm aperture, 4-layer graded coil
Cable:L1-L2: 28 strands, 1 mm L3-L4: 40 strands, 0.7 mm
Insulation: 0.15 mm thick
Mechanical structure:
  Thin StSt coil-yoke spacer
  Vertically split iron laminations
  Aluminum I-clamps
  12-mm thick StSt skin
  Thick end plates and StSt rods

## Slide 7: Cable Development and Test
Final cable cross-section parameters have been selected
  PF~87%,
  Ic degradation <5%,
  RRR>100
HT optimization to achieve optimal Jc and RRR
SS core

## Slide 8: Magnet Conductor and Mechanical limits
Magnet conductor limit:
Bap=15.3T @4.5K
Bap=16.7T @1.9K
100% SSL
87% SSL
300K
Seqv=133 MPa
4K
Seqv=176 MPa
4K+15T
Seqv=168 MPa
Magnet design limit is determined by the mechanical constraints and it is 15 T!
Jc(4.2K, 12T)~2600 A /mm2

## Slide 9: Coil magnetization effect and its correction
Peak values of b3=-48 and b5=+8 units @ B~1.4 T.
LHC MB b3~-7 units
LHC MBH b3~-25 units
50-75 deg
Geometrical b3=-0.8 and 0.375 mm thick iron strips

## Slide 10: Magnet tooling
Reaction/impregnation (2 sets)
  L1-L2
  L3-L4
Reaction fixture
Impregnation fixture
Yoking tooling

## Slide 11: 15 T dipole: Mechanical Stricture Components
Iron Laminations
AL I-Clamps
Fillers
Axial Rods
End Plates
StSt Skin
All structural components are available

## Slide 12: 15 T dipole: Coil Components
Cable (FNAL)
Traces (LBNL/FNAL)
L1/2 parts (CERN)
Ti and Glidcop wedges
4 sets: Ti poles and spacers, SS saddles
L3/4 parts (FNAL)

## Slide 13: Coil fabrication process
Coil winding and curing
Coil epoxy impregnation
Coil reaction
Coil instrumentation
Coil fabrication time ~3 months
Coil (Layer ) | Coil # | Winding, curing | Reaction, witness samples | Instrumentation, epoxy impregnation | Instrumentation
Inner (L1-L2) | 1 | complete | complete | in progress | 
 | 2 | complete | in progress |  | 
 | 3 | Not started |  |  | 
Outer (L3-L4) | 1 | complete | complete | complete | in progress
 | 2 | complete | in progress |  | 
 | 3 | complete |  |  | 

## Slide 14: Mechanical Models
Goals:
Validate the results of mechanical analysis
Development of the coil assembly plan and pre-stress targets
Test all structural components, tooling and instrumentation

## Slide 15: Conclusions
15 T dipole is a challenging and important MDP milestone to understand limits of Nb3Sn accelerator technology
  break the 14 T “wall”
15 T dipole demonstrator has been developed
  optimized coil design
  innovative mechanical structure
Magnetic and mechanical analysis is complete
  large persistent current effect in Nb3Sn accelerator magnets was effectively reduced to the acceptable level
  Design conductor and mechanical limits well understood
Fabrication of 15 T dipole demonstrator is in progress
  important contributions from CERN - great integrated international effort
Magnet test is expected in September 2018

## Slide 16: Acknowledgment
FNAL: E. Barzi, J. Carmichael, V.V. Kashikhin, S. Krave, I. Novitski, C. Orozco, S. Stoynev, D. Turrioni, G. Velev, A.V. Zlobin, A. Rusy, L. Ruiz, S. Jonhson, J. Karambis.
LBNL: S. Caspi, M. Juchno, M. Martchevskii
CERN: D. Schoerling, D. Tommasini
FEAC/UPATRAS: C. Kokkinos.