## Slide 1
Quench Antenna Data on Telene Undulator - First Look
J. DiMarco, E. Barzi, D. Turrioni
31Jan 2024

## Slide 2
Instrumented a Telene-coated Nb3Sn-wire undulator with standard ‘quadrupole-bucked’ QA
First used on Undulator #1, Run 3, 08 Dec2023
Quench events shown here are 65, 66, 85, 86, 87, 88

## Slide 3
QA locations on telene undulator run3

## Slide 4
QA apparently sees the quench in the cable, even though not ‘Rutherford-type’ with inter-strand current redistribution
Half-coil difference
Note that HC diff signal is pretty flat before quench

## Slide 5
Q65
Q66
Q85
Q86
Q87
Q88
Different Q-start here
Training quenches
plateau quenches
‘fall-back’ quench
quenchTrigger t=0
Note: 10 numbers (5 signals, 5 blank) per file

## Slide 6
Plateau quench with HC diff signal becoming ‘noisy’ just before quench

## Slide 7
Unlike plateau quenches, coil with QA1 is earliest in this ‘fall-back’ quench
HC diff is noisy again

## Slide 8
QA3 (and QA2) is seeing excursions and seeming to recover
Unlike the plateau quenches, QA1 is seeing some more ‘spike-like’ activity early
QA4 is also seeing early activity at about the same time as QA1 – note that these are top and bottom of the same section of coil
QA1 is the first to quench, unlike plateau quenches

## Slide 9
Undulator #2, Run 1, 23Jan2024

## Slide 10
Note: there are 39 quenches, but files 8, 34, and 38 are missing. 10 numbers (5signals, 5 blank) per file
False trips

## Slide 11
First training quench
Spike features on QA1
QA5 later than QA2

## Slide 12
2nd training quench – slower development
QA5 ~same time as QA2

## Slide 13
Quench at plateau
Spike features on QA2, QA3
QA5 again lags a bit

## Slide 14
Last quench at plateau
QA5 LEADS QA1 and QA2

## Slide 15
Three of the quenches had some sort of early start – QA activity peaks at ~-7ms before t0

## Slide 16
Start is at -13ms

## Slide 17
Summary and next steps:
Seem to be able to detect quench related pick-up signals even with non-optimized QAs
Detailed differences can be seen between events, and potentially, perhaps with some improvements, can be used to understand something more about quenches in the undulators.
Analysis will continue, including trying to tie QA observations with acoustic ones.

## Slide 18
Back-up slides