## Slide 1: Nb3Sn - Coil Composite and Training Status and Goals
G. Vallone
07/02/2024 - MDP Modeling Group

## Slide 2: Outline
Introduction
Coil Composite
      Stiffness
      Stress/Strain Limits
  Training

## Slide 3: FE Coil Models
Key ingredients required for coil modelling:
Modelling strategy
    To have a reasonably sized model we need several simplifying assumptions
Constitutive equations (material model)
    Connect stress/strain inside the simplified model
Strength limits
    Depending on the modelling strategy, the definition of these limits might be different

## Slide 4: 2D - Available Modelling Strategies
Two modelling strategies developed: ‘strand model’ and RVE model
Both the strand model and RVE model match the mechanical measurements, with no calibration necessary
The RVE model provides the same ‘average’ results, but does not allow to correctly evaluate local peaks
‘RVE’ Model
Strand Model
G. Vallone et al., SUST 2020

## Slide 5: 3D RVE Model - Status
Modeling at the strand level not easy in 3D
We have a set of assumptions/tools available to extend the RVE model in 3D
    Anisotropic yield strength criterion
    Anisotropic work-hardening rule (‘generalized Hill’)
    Element (material) coordinate system definition
  The model was tested on MQXFA, but for the moment the agreement between (longitudinal) measurements/computations is not great
G. Vallone et al., IEEE Trans (2023)

## Slide 6: Coil Composite Tool
We should compute the coil properties for each magnet design
      These are a function of the strand/cable design
  We had developed a tool in python/ANSYS that could do this, but it was never released…
      It is missing only an interface to be used for at least certain ‘design’ families
Cable Parameters
Strand Parameters
Python
Interface
APDL
APDL
Material
Other Formats…

## Slide 7: Mechanical Loads in Nb3Sn Coils
Mechanical loads in Nb3Sn coils can be divided in three regions, based on the effect they produce in the coil composite:
    Region #1: only elastic strains are introduced in the coil composite
    Region #2: loads introduce plastic deformations in the copper matrix, locking residual elastic strains in the filaments and thereby affecting their electro-magnetic performance irreversibly
    Region #3: critical load configurations that introduce local failures in the coil, in the form, for example, of broken filaments or insulation damage
We are working on a framework that can predict the boundaries of these regions starting only from meas. on longitudinally loaded strands

## Slide 8: Strain/Stress Limits - Region 1 and 2
In Region 1: Elastic and Region 2: Plastic, the strain/stress limits coincide with the acceptable critical current reduction
    This can be predicted using the strain function coupled with multi-scale modeling in the ‘loading’ regime
    The same approach can be extended to Region 2, unloading, at least in 2D using measurements performed on strands under transverse pressure
      This should not be necessary with more advanced modeling strategies
    The approach can be applied with RVE strategies to 3D models
      This can be only as good as our constitutive equations…

## Slide 9: Stress/Strain Limits – Region 3
Region 3 is the most complicated, as coil failures can be very different in nature
    Multi-scale models might predict correctly the onset of radial cracks
    Measurements show significant ‘load’ interaction
    Unclear relationship between radial and longitudinal cracks, being explored
G. Vallone, J.F Croteau et al., IEEE Trans. 2024

## Slide 10: Coil Composite - Summary
  What we have:
    2D strand, RVE models validated against measurements
    3D RVE models, non-validated
    2D critical current ‘predictions’ in regions 1, 2
      Extended to 3D, but not validated
    A failure model, tested on a limited set of loading conditions
What we are missing (at least…):
    Improve 3D RVE models
    Check validity of strain function approach in 3D
    Collect (a lot) more data on ‘failure’ of Nb3Sn as function of different loading conditions

## Slide 11: Outline
Introduction
Coil Composite
      Stiffness
      Stress/Strain Limits
  Training

## Slide 12: CCT Training Model
CCT training model:
    Elasto-plastic material model for the conductor, extracted from RVE models
    Cohesive Zone Model at the cable/mandrel interface
    Energy released by debonding + frictional sliding computed at each step
    Magnet ‘quench’ condition checked at each step
Debonding
Energy
Mandrel
Cable
Failed Interfaces
Sliding Energy

## Slide 13: CCT4 - Quench Conditions Zoo
Model results depend on the assumption on the quench condition
    Not clear what is the ‘correct’ assumption
    The model produces ‘events’ at the ‘correct’ current, then the physics behind the thermal energy release is unclear
      We need some experiment to better understand what is happening…

## Slide 14: Conclusion
Failure of bonded interfaces can be modeled using cohesive elements
We proposed an iterative modeling approach to simulate training
Model results suggests that CCT training might be due to debonding and consequent sliding at the interfaces
    This is consistent with recent ’wax’ results
Comparing the released energy ’patterns’ we see some similarities…
Tested on subscale magnets
Training Simulation
Python/APDL

## Slide 15: Training - Status
What we have:
    We proposed an iterative modeling approach to simulate training
    Model results suggests that CCT training might be due to debonding and consequent sliding at the interfaces
    We have some comparison with available Strain Gauge, AE and Quench antenna data
    Tested on subscale magnets
What we are missing (at least…):
    Quench condition validation/change with dedicated experiments
      Work in progress!
    Validation on other magnets (e.g. MQXF?)
    Testing on ‘future’ magnets (e.g. SMCT)