## Slide 1: Updates on 20 T working group activities
P. Ferracin
MDP General Meeting
July 17th, 2024

## Slide 2: Outline
Introduction of 20 T working group
Key results presented at the Collaboration Meeting and recent work/analysis
  20 T design study
  Hybrid magnets development

## Slide 3: Acknowledgement (20 T working group)
Members US MDP 20 T working group
  LBNL: D. Arbelaez, L. Brouwer, M. D’Addazio, L. Garcia Fajardo, J.L. Rudeiros Fernandez, M. Juchno, S. Prestemon, T. Shen, R. Teyber, G. Vallone, X. Wang
  FNAL: G. Ambrosio, M. Baldini, E. Barzi, S. Gourlay, V. Kashikhin, V. Marinozzi, I. Novitski, G. Velev, A. Zlobin
  NHMFL: L. Cooley, D. Larbalestier
  BNL: K. Amm, M. Anerella, J. Cozzolino, R. Gupta, F. Kurian, B. Yahia
European Contributors
  Emmanuele Ravaioli (CERN)
  Douglas Martins Araujo (PSI)
  Etienne Rochepault (CEA)

## Slide 4: Introduction Bi-weekly meetings (but recently weekly…)
66 meetings so far
  https://conferences.lbl.gov/category/100/

## Slide 5: Introduction Goals of working group
Conceptual design of a 20 T hybrid HTS-LTS magnet
  Comparative analysis of different design options for a 20 T hybrid
    Cos design and its stress-management options
    Block-type coil design (block with flared ends)
    Common-coil design (block with racetrack coils)
Review and follow-up of current work on hybrid magnets
  Collect and organize information to provide inputs for 20 T hybrid design and feed-backs to hybrid program

## Slide 6: US Magnet development program roadmap
Road-map updated in 2020
  and to be updated again in by the end 2024
https://arxiv.org/abs/2011.09539

## Slide 7: Motivations of a 20 T hybrid design Previous work
2005, P. McIntyre, et al., 24 T hybrid for LHC tripler (TAMU)
2011, 2014, E. Todesco, et al., 20 T hybrid for LHC upgrade (CERN)
2015, G. Sabbi, et al., 20 T hybrid for SPPC China and FCC (LBNL)
2016, Q. Xu, et al., 20 T hybrid for SPPC China (IHEP)
2018, J. van Nugteren, et al., 20+ T HTS for LHC upgrade or FCC (CERN)
2020, D. Martins Araujo , et al., towards 20 T FRESCA2+Feather (CERN)
2021, J.S. Rogers, et al., 18 T hybrid (TAMU)
2022, P. Ferracin, et al., 20 T hybrid demonstrator (US MDP)
2015, R. Gupta, et al., 20 T hybrid for LHC upgrade (BNL)

## Slide 8: Motivations of a 20 T hybrid design
Relevant to…
  FCC-hh
    “high-field superconducting magnets: 14-20 T”
  Muon colliders
    Collider ring dipole
      Large aperture (100-160 mm), 12-16 T
        Similar to the outsert of a 20 T hybrid
    IR quadrupole magnets
      “…with a peak field of 20 T, also associated with, large apertures, up to 300 mm”

## Slide 9: Motivations Summary
Hybrid magnets development
  HTS/LTS hybrids are a very effective tool to perform R&D on a broad spectrum magnets similar to those considered for FCC-hh or Muon Colliders
  So far, it is also an economically viable option to explore the very high field
    16+ T range
  It forces HTS and LTS teams to work together on integrated designs
20 T design study
  Very effective way of perform studies/analysis on a broad spectrum magnets similar to those considered for FCC-hh or Muon Colliders
  On a side note (but still important)
    It is a very interesting and fun problem for magnet designers
  Excellent case study for students and Postdocs
    It contains almost everything: different SC materials…different cable geometries…magnetics… mechanics…quench detection and protection…..

## Slide 10: Outline
Introduction of 20 T working group
Key results presented at the Collaboration Meeting and recent work/analysis
  20 T design study
  Hybrid magnets development

## Slide 11: Key results presented at the Collaboration Meeting Current 20 T reference cross-sections
Three options considered (CT, BL, CC), for now focusing mainly on an HTS coil made with Bi2212 cable
Iterative process on going
  Magnetic analysis  Margin and field quality
  Mechanical analysis  stress in HTS and LTS coils (and the structure)
  Quench protection  Non-SC/SC ratio, strand-cable design, CLIC, dump…..
  …. And back and forth
More focus on CT and CC, less on BL so far
HTS
LTS
HTS
LTS
HTS
LTS

## Slide 12: Key results presented at the Collaboration Meeting Optimization process

## Slide 13: Key results presented at the Collaboration Meeting 20 T Mechanics

## Slide 14: Key results presented at the Collaboration Meeting 20 T Quench protection (1 m long magnet)
Hot-spot temperature | Peak voltage to ground | Peak CLIQ current
242 | Not optimized yet | 5670
Hot-spot temperature | Peak voltage to ground | Peak CLIQ current
313 | 501 | 4329
Hot-spot temperature | Peak voltage to ground | Peak CLIQ current
286 | 570 | 3810
Block-coil
V1
Common-coil
V5
Cos-theta
V28_137

## Slide 15: Key results presented at the Collaboration Meeting 20 T Summary
For now, CT and CC most analyzed: for 1 m, they meet the criteria (still some work on the corner peaks)
More work required on BL for fair comparison
Mechanics: stress management required in all directions; still very high stress in the mandrel/ribs
Quench protection seems ok for 1 m magnets in all 3 designs
  For longer new solutions to be considered

## Slide 16: Recent work/analysis Update of CT design
Fine tune and overall improvement in most of the aspects (margin/efficiency, mechanics, QP)

## Slide 17: Recent work/analysis Hybrid vs stand-alone
We started to look not only at the hybrid conditions but also at the stand-alone ones
Example with the current CT
  When operating at 20 T (87% of Iss), how much field is provided by HTS and LTS?
    6 T given by HTS and 14 T given by LTS
  When operating in stand-alone (87% of Iss), which bore field would the HTS and LTS generate?
    9 T for the HTS and 15 T for the LTS

## Slide 18: Recent work/analysis Minimum HTS vs minimum coil size
When operating at 20 T (87%)
  6 T given by HTS and 14 T given by LTS
In stand-alone (87%)
  9 T for the HTS and 15 T for the LTS
When operating at 20 T (87%)
  9.5 T given by HTS and 11.5 T given by LTS
In stand-alone (87%)
  11 T for the HTS and 13 T for the LTS
However, the current CT design is only one of the possible options

## Slide 19: Recent work/analysis Minimum HTS vs minimum coil size
The main difference between the two approaches is that
  In one case we minimize the HTS coil
    Focus on cost (assuming HTS more expensive than LTS)
  In the other case we minimize the overall coils size
    Focus on size (work in progress)

## Slide 20: Recent work/analysis Minimum HTS vs minimum coil size
On paper both approaches are valid and achievable, but one has to make a choice
This is likely the explanation (again, work in progress) of the CT_vs_CC issue
  CC has 50 % more HTS than CT but significant less LTS

## Slide 21: Recent work/analysis Hybrid vs all HTS
Let’s look at the load-lines: all with a Je below 600 A/mm2  all HTS?

## Slide 22: Recent work/analysis Hybrid vs all HTS
A third option can be considered: all HTS
  Still to be fully analyzed, but ok in term of margin
Hybrid
Minimum HTS
Hybrid
Minimum overall coil
Hybrid
All HTS

## Slide 23: Recent work/analysis Hybrid vs all HTS
All HTS option: we are not yet taking advantage of the area where LTS is better than HTS
  Only marginally with the CC
Are we limited by the old “rule of thumb”?
  “Accelerator magnets operate with a Jo not much higher than ~500 A/mm2  Je not much higher than ~750 A/mm2”

## Slide 24: Recent work/analysis Seminar at CERN (remote)
Among the feedbacks-comments
  The approach has been so far a very traditional one
    CT, BL, CC with Rutherford cables
    Large and expensive coils/magnets
  How about exploring new options (new paradigm)?

## Slide 25: Recent work/analysis New design study options: REBCO
“Advanced”
  STAR 6-around-1 cable or CORC
    “Familiar” cable but more work needed
“More advanced”?
  Twisted stack
  Aligned stack
    Take advantage of tape anisotropy

## Slide 26: Next steps for the 20 T analysis
For the hybrid designs with Bi2212
  Explore the 3 options: minimum HTS, minimum overall coil, all HTS
  Always consider the stand alone fields
    Relevant for future colliders
      10 T all HTS…..16 T large aperture LTS
For the more advanced hybrid designs with REBCO
  Conceptual designs of REBCO hybrid magnets which meets the criteria
    Major questions marks on mechanics (limited stress) and quench protection

## Slide 27: Outline
Introduction of 20 T working group
Key results presented at the Collaboration Meeting and recent work/analysis
  20 T design study
  Hybrid magnets development

## Slide 28: Key results presented at the Collaboration Meeting Hybrid magnets activities

## Slide 29: Recent work/analysis Qualification of test facility upgrade
Upgrade of the LBNL test facility specifically to test hybrid magnets
  Challenge: two independent facilities (PS, quench protection, header) in one facility
Successful test of REBCO insert (CORC demountable joint samples) inside CCT5
  First, 4.8 kA in the REBCO insert without back-ground field  qualification new PS and QP
  Then, 2.4 kA in REBCO in 6 T background field  full qualification of the facility  ready for Bin5-CCT5

## Slide 30: Recent work/analysis Hybrid work
Several options under consideration for “C4”
  Next steps: comparative analysis and “prioritization”

## Slide 31: Recent work/analysis Overview of hybrid magnets
CCT5-Bin5
30 mm
9-10 T
COMB-SMCT
100 mm
11-12 T
11T-Bi SMCT-SMCT
15 mm
14-16 T
CCT6-BiCCT1-2
40 mm
16-18 T
CCT5-C4
30 mm
11-12 T
Next steps: timeline and more precise field estimate

## Slide 32: Appendix

## Slide 34: Design criteria
Coil and magnet parameters
  Free coil aperture (diameter) 50 mm
  Operational bore field 20 T
  load-line fraction @ 1.9K: Iop/Iss <= 87 %
  2D Geometrical harmonics bn<3 units for n<10 (at Rref=17 mm)
Quench protection
  All coils powered in series
  Maximum hot spot temperature 350 K
Mechanics
  Maximum Nb3Sn coil stress <180 (<150) MPa at 1.9 (293) K
  For the HTS <120 MPa

## Slide 35: Design criteria: some comments
Size
  No limits or constraints set (request from the working group)
  So far the goal has been to minimize coil size, but not significant effort has been devoted to minimize the structure (next step)
Quench protection
  We focus for now on a 1 m long magnet, with CLIC/dump.
  But we start considering also the issue of protecting a long accelerator magnet
Mechanics
  Good knowledge of mechanical properties and limits of Nb3Sn, recent interesting results from Twente on Bi2212 cables  the assumptions seem reasonable
  Much less knowledge on REBCO CORC/STAR stress limits and properties

## Slide 36: Design criteria: Wires and cables
Nb3Sn
  0.7 – 1.1 mm strands
    Typical properties of 127 or 169 (Bruker-OST) RRP stacks
  Rutherford cables: 8-26 mm wide, 1.3-2.0 mm thick
Bi2212
  Isotropic, round, multifilamentary
    Bruker-OST architecture 19 × 36, 37 × 18 or 55 × 18 for 0.8 mm diameter wires
  On paper, possible same strand and Rutherford cable dimensions as Nb3Sn
REBCO
  CORC (ATC LLC) cable and STAR (AMPeers) wires:
    Tapes around Cu former
      Diameter from 1.3 to 3.6 mm
  6-around-1 STAR cable

## Slide 37: Superconducting materials: Je and Jo
Assumptions for magnetic analysis
  Je = Strand current / strand area
    Je_LTS = 875 A/mm2 (1.9 K, 16 T, 5% degrad.)
      3000 A/mm2 Jc (4.2 K, 12 T, virgin)
    Je_HTS = 740 A/mm2 (20 T)
      Bi2212 value
Nb3Sn and HTS cross at 16.5 T
CORC/STAR wire still lower in Je (600 A/mm2, 20 T)

## Slide 38: Current reference cross-sections Cos-theta
Coil inner diameter 60 mm
  Internal support structure
Design constraint: double-layer coils
6 layers, with cables 15 to 22 mm wide
  2 layer HTS, 4 layer LTS
HTS: CCT-like or “single turn” SMCT
LTS: SMCT design + CT
Field quality and margin in spec
je= 450-600 A/mm2, jo= 300-400 A/mm2
OR coil: 165 mm
HTS
LTS

## Slide 39: Current reference cross-sections Cos-theta
4 out of 6 layers with stress management
  Result of several iterations
First two layers (HTS) with a CCT-type design
  Single cable in grove, with ribs and spar
Second two layers (LTS) with SMCT-type design
  Single block in grove, with ribs and spar
Last two layers traditional CT
Coil stress in spec
  but very high stress in the mandrel (Inconel or Nitronic?)

## Slide 40: Current reference cross-sections Block
Coil inner diameter 70 mm
  Internal support structure
Design constraint
  double-layer coils
  HD2/FRESCA2 style coil
3 double-layer coils, with 15 mm wide cable
Field quality and margin in spec
je= 450 A/mm2, jo= 300 A/mm2
OR coil: 130 mm
  Less efficient than CT (50% more HTS, 15% more LTS), but less optimized

## Slide 41: Current reference cross-sections Block
10 mm thick winding pole
  FRESCA2 style
Coils vertically separated by horizontal plates
  Vertical stress management
HTS and LTS separated by vertical ribs
  Horizontal stress management
Stress not yet in spec
Challenges: “insertion” of HTS coil inside LTS coils, grading and splicing

## Slide 42: Current reference cross-sections Common-coil
Coil inner diameter 50 mm
  No internal support structure
Single layer coils allowed : splice in the central pole
  So, more vertical and horizontal flexibility
4 layers, with cables 16 mm to 20 mm wide
  1 layer HTS (plus pole coils), 3 layer LTS
Field quality and margin in spec
je= 550-650 A/mm2, jo= 400-450 A/mm2
OR coil: 110 mm
  ~50% more HTS than CT, but ~50% less LTS
    Overall smaller coil, but at the expense of larger HTS coil
  CT vs CC similar to Case II vs Case I

## Slide 43: Current reference cross-sections Common-coil
No internal structure in innermost layer
Coils vertically separated by horizontal plates
  Vertical stress management
HTS and LTS separated by vertical ribs
  Horizontal stress management
Stress almost in spec
Challenge: pole turns
  Avoidable with asymmetric coils

## Slide 44: Current reference cross-sections Quench protection (more than 1 m length)
Without new solutions, hard to go beyond 3-4 m
Longer lengths protectable with ESC (Energy Shift with Coupling)

## Slide 45: Nb3Sn outserts Canted-Cos: CCT5 and CCT6
CCT5
  Tested in 2019
  8.5 T in 90 mm ap.
  Ready to be used
  as outsert
CCT6
  Mandrel under fabrication
  LD1 (HD2) and MQXF cable
  Design: 15 T (1.9 K, 80% Iss) in 120 mm aperture

## Slide 46: Nb3Sn outserts Stress Management Cos (SMCT)
SMCT
  Stress management at the conductor-block level
  Target: 11 T in 120 mm aperture
  Coil tested in mirror, both with and without inner coil of the MDPCT1

## Slide 47: Nb3Sn outserts Stress Management Cos (SMCT)
SMCTM1
  14.3 kA, 87 % Iss reached in 24 quenches
  12.7 T conductor peak field
  No memory after thermocycle
SMCTM1b
  Highest current was 11.46 kA, 82 % Iss
  14.5 T conductor peak field in the inner coil

## Slide 48: Nb3Sn outserts Summary
in scale
CCT5
90 mm
8.5 T
CCT6
120 mm
15 T
(design)
SMCT
120 mm
11 T
(design)

## Slide 49: Outline
Introduction and motivations
  US Magnet Development Program and the 20 T working group
  Why hybrid and why 20 T
20 T design
  Design criteria
  Preliminary considerations based on sector coils
  Current reference cross-sections
Overview of hybrid activities
  Nb3Sn outserts
  HTS inserts
Conclusions

## Slide 50: Bi2212 inserts Canted-Cos: Bin5, BiCCT1, and BiCCT2
Bin5
  1.6 T in 31 mm aperture
  Successfully tested in stand alone
  Ready to be tested in CCT5
BiCCT1
  5 T in 40 mm aperture
  Coil wound and ready for reaction
  To be tested in CCT6
BiCCT2
  7 T in 40 mm aperture
  12 mm cable fabricated
  To be tested in CCT6

## Slide 51: Bi2212 inserts Stress Management Cos (SMCT)
Bi2212 SMCT
  1-2 T in 15 mm aperture
  Winding test performed with plastic parts
  Fabrication of Inconel 3D printed mandrel in progress
  To be tested in a 4L (CT from 15T magnet + SMCT coil)

## Slide 52: REBCO inserts Canted-Cos (“C” series)
C2: stand-alone test in 2020
  2.9 T in 65 mm aperture
  Fundamental step towards development CORC CCT inserts
Next step: C3
  Target: 5 T in 60 mm aperture
  Under fabrication

## Slide 53: REBCO inserts The COMB (Conductor on Molded Barrel) series
COMB insert
  Target: 2-3 T in 100 mm aperture with CORC wire
  To be tested in SMCT after stand alone test
  Test with STAR wire at both 77 K and 4.5 K
    1.5 T bore field reached

## Slide 54: Bi2212 and REBCO inserts Summary
in scale
SMCT
15 mm
1-2 T
(target)
BiCCT1
40 mm
3 T
(target)
BiCCT2
40 mm
5 T
(target)
Bin5
31 mm
1.6 T
COMB
100 mm
2-3 T
(target)
Bi2212
REBCO

## Slide 55: Overview of planned MDP hybrid magnets
CCT5-Bin5
30 mm
9-10 T
COMB-SMCT
100 mm
11-12 T
11T-Bi SMCT-SMCT
15 mm
14-16 T
CCT6-BiCCT1-2
40 mm
16-18 T
CCT5-C4
30 mm
11-12 T

## Slide 56: Outline
Introduction and motivations
  US Magnet Development Program and the 20 T working group
  Why hybrid and why 20 T
20 T design
  Design criteria
  Preliminary considerations based on sector coils
  Current reference cross-sections
Overview of hybrid activities
  Nb3Sn outserts
  HTS inserts
Conclusions

## Slide 57: Conclusions
US MDP pursuing an LTS-HTS hybrids magnets program towards 20 T
  Excellent tool to perform R&D on various materials and magnets
20 T design study
  Coil size ranging from 120 to 160 mm OR depending on design options and assumptions (HTS vs overall)
  Stress management required in particular in the innermost layers
  Up to 3-4 m length can be protected, beyond new solutions required
Large aperture Nb3Sn outserts under development with stress management concepts
  CCT: “5” is ready, “6” under develop.,
  SMCT first coil being tested in mirror configuration
HTS inserts
  Successful test of Bi2212 Bin5
  Both REBCO CCT and COMB insert designs validated with CORC and STAR wires
First hybrid test (9-11 T field level) expected in 2024

## Slide 58: Appendix

## Slide 59: Motivations of a 20 T hybrid design
…also….the “4 T step”
  8 T
    Nb-Ti “limit” (LHC)
  12 T
    Nb3Sn (HL-LHC)
  16 T
    Limits of Nb3Sn
  20 T
    HTS

## Slide 60: Current reference cross-sections Optimization process

## Slide 61: Critical current versus transverse stress
Chart: average transverse stress [MPa]
| 10.019986663489492 | 19.972634592337041 | 29.903326541877416 | 39.888676028668662 | 50.006113571162103 | 59.949970910804616 | 69.934716131811228 | 79.698056627015262 | 90.003236648046126 | 99.983804599953729 | 109.85769540693157 | 119.93797270893079 | 129.92657964134418 | 139.92524114286164 | 149.85772006985431 | 159.91658125610417 | 169.84619221677559 | 179.92918275056479 | 189.94101747086168 | 199.87366886030671
pressure applied | 1 | 1.0009 | 1.0022 | 1.0021 | 1.0004 | 0.99722 | 0.99586 | 0.9953 | 0.9919 | 0.98757 | 0.9864 | 0.98331 | 0.97966 | 0.97675 | 0.9723 | 0.96593 | 0.96068 | 0.95455 | 0.94707 | 0.93934
unloaded to 10 MPa | 1.001 | 1.0025 | 1.0011 | 0.99536 | 0.99858 | 0.99678 | 0.99277 | 0.99413 | 0.99085 | 0.98429 | 0.98176 | 0.98127 | 0.97879 | 0.97162 | 0.96828 | 0.9637 | 0.95449 | 0.95091 | 0.94336
Chart: average transverse stress [MPa]
| 10.045113099029052 | 20.021794793255058 | 29.975497264251342 | 39.956086136228443 | 49.972307982720253 | 60.002780711478451 | 69.898001660618846 | 79.868671034121576 | 90.024450725337545 | 100.02554545601674 | 110.00583476535391 | 119.98183510271123 | 129.98350510168112 | 139.91418838238221 | 150.00919051663405 | 159.95168952943004 | 169.98168974422381 | 179.95886124762399 | 189.90078556954299 | 199.87760550763213
pressure applied | 1 | 0.99721 | 0.99492 | 0.99353 | 0.99033 | 0.99005 | 0.988 | 0.98161 | 0.97948 | 0.97416 | 0.96682 | 0.96125 | 0.95331 | 0.94499 | 0.94082 | 0.92632 | 0.91534 | 0.90358 | 0.8888 | 0.87463
unloaded to 10 MPa | 0.9973 | 0.99611 | 0.99365 | 0.99078 | 0.99009 | 0.98812 | 0.98407 | 0.98014 | 0.97567 | 0.96785 | 0.9642 | 0.95658 | 0.94684 | 0.93963 | 0.93045 | 0.92087 | 0.90625 | 0.89539 | 0.87598
Applied field 11 T, data normalized to initial Ic of 2.70 kA (sample 3), and 4.07 kA (sample 4)
Measurement sequence:
  10 MPa
  20 MPa
  10 MPa
  30 MPa
  10 MPa
  40 MPa
  etc.
5% degradation reached at: 170-200 MPa in sample 3 and 120-150 MPa in sample 4
Ba = 11 T
Sample 3: LBNL1109 (Dec 2022)
Sample 4: LBNL2002 (June 2023)
Ba = 11 T

## Slide 62: Appendix

## Slide 63
CCT5_Bin5: coil_OR_329
CCT5_Bin5: magnet_coil_OR_76
CCT6-BiCCT2 : coil_OR_158
CCT6_BiCCT2 : magnet _OR_430

## Slide 64: Magnetic analysis “Traditional” Cos (without stress management)
See talk from V. Marinozzi
6 layers, with cables 13 mm to 21 mm wide
  Double-layer coils with internal splice and not graded
Two options considered
  4 layer HTS, 2 layer LTS or 2 layer HTS, 4 layer LTS
Field quality requirements met
  Margin to be optimized
Quench protection addressed (J in Cu)
Stress requirements partially addressed
  Accumulated   150-160 MPa
  Accumulated r approaching 200 MPa
Bi2212
Nb3Sn
Nb3Sn

## Slide 65: R&D towards Nb3Sn outserts Canted-Cos: subscales
Development of sub-scale CCT for material/training study
  5.5 T in 50 mm aperture
  Focus on impregnation material
Sub_2 to Sub_6: from Mix-61 to wax
  Excellent training (no training) performance
  Stable plateau and holding
Currently under development: Sub_7
  Filled wax
    Based on PSI box test, same training performance as wax, better mech properties
    Better candidate for higher stress outsert magnets
  Coil fabricated, magnet assembly in progress, test expected in the summer