## Slide 1: Design of a 20 T cosθ dipole hybrid magnet
Cross section update
M. D’Addazio
10/28/2024

## Slide 2
Main conductor parameters |  |  | 
 | L1-L2 | L3-L4 | L5-L6
Superconductor/Stabilizer | Bi2212/Ag | Nb3Sn/Cu | Nb3Sn/Cu
Number of strands (-) | 32 | 50 | 50
Strand diameter (mm) | 0.90 | 0.80 | 0.70
Cu/noCu or Ag/noAg ratio(-) | 4.00 | 0.90 | 2.00
Cable width (mm) | 14.87 | 22.16 | 19.39
Cable average thickness (mm) | 1.70 | 1.52 | 1.33
Insulation thickness (mm) | 0.15 | 0.15 | 0.15
Summary of the main parameters
Coil and magnet parameters
  Free coil aperture (diameter) 50 mm
  Operational bore field 20 T
  Load-line fraction at 1.9 K ≤ 87%
  2D geometrical harmonics < 3 units for n<10
  ( = 17 mm)
Mechanics
  Maximum Nb3Sn coil stress <180 MPa at 1.9 K
  Maximum Bi2212 coil stress <120 MPa

## Slide 3
Thickness:
  Stain. Steel Collar – 25 mm
  Iron pad – 130 mm
  Iron yoke – 170 mm
  Aluminum shell – 70 mm
  Overall diameter: 1.12 m
Structure design
The structure still needs to be optimized in terms of key position and shape of the iron components.
Notes: Separation and sliding are allowed in the coils.
Bonded only the thin interlayers that represent the insulation in layers 5 and 6.
For the wedges, the nodes are coupled (cpintf).

## Slide 4: Azimuthal prestress
In these plots, the thickness of the iron pad and yoke is considered equal to 300 mm and the shell thickness is equal to 70 mm.
The dashed black line shows that with an azimuthal prestress of 100% of the EM forces is possible reaching a value of the stress comparable to the considered limit.

## Slide 5: Equivalent stress – HTS
Prestress | Cooldown | Energization
51 MPa
52 MPa
122 MPa
For the HTS conductors:
The peak stress after energization is equal to 122 MPa and the maximum is concentrated in a small corner of layer 1.
Stresses at prestress and cooldown are below the limit.

## Slide 6: Equivalent stress – LTS
Prestress | Cooldown | Energization
68 MPa
124 MPa
186 MPa
For the LTS conductors:
The peak stress after energization is equal to 186 MPa and the maximum is located in the corner of the third block of layer 3.
The peak stresses are also verified during pre-stress and cooldown.

## Slide 7: Equivalent stress – Mandrel L1-2
Prestress | Cooldown | Energization
473 MPa
743 MPa
1430 MPa
The stress management design is used in layers 1 – 4.
Bending in the spar of layer 1.
Stress linearization procedure still under evaluation for the ribs.

## Slide 8: Equivalent stress – Mandrel L3-4
Prestress | Cooldown | Energization
482 MPa
1060 MPa
2210 MPa
The stress management design is used in layers 1 – 4.
Stress linearization procedure still under evaluation for the ribs.