## Slide 1
Alessio D’Agliano, PhD student 11/05/2024
Bi-2212 Multiscale Modeling Update

## Slide 2: LTS/HTS Hybrid Dipole Analysis – Current Degradation
Bolt – SS304
Shell – SS304
Clamp – Aluminum
Yoke – Iron
Coil L3, L4 – Nb3Sn
Coil L1, L2 – Bi-2212
Poles – Titanium
Wedges – Brass
Mandrels – Inconel 718
Impregnation – G10
Skin – SS304
Gr.Ins. – Kapton
Bi-2212 is the best superconductor in terms of JC at a high external magnetic field, but it’s prone to stress and strain-induced current degradation. The FEM analysis performed on the hybrid cos-theta coil (linked with .py code) investigates this aspect.

## Slide 3: LTS/HTS Hybrid Dipole Analysis with Current Degradation
From: “Reversible effect of strain on transport critical current in Bi2Sr2CaCu2O8+x superconducting wires: a modified descriptive strain model”, N Cheggour, X F Lu, T G Holesinger, T C Stauffer, J Jiang and L F Goodrich
Strain ε (left) and stress σ (right) current degradation laws were implemented in the simulation code to evaluate the overall decrease of current in the magnet.
The strain-induced current degradation is straightforward. The stress-induced current degradation is possible to obtain translating stress state in the Rutherford cable under applied transverse pressure.
From: “Transverse pressure dependence of Bi-2212 Rutherford cables” Anna Kario presentation at US-MDP Collaboration meeting 2024
Bi-2212 Rutherford cable under transverse pressure (11 T), University of Twente
Strain/stress criteria, ANSYS output:

## Slide 4: Stress-Induced Bi-2212 Current Degradation Law
From: “Transverse pressure dependence of Bi-2212 Rutherford cables” Anna Kario presentation at US-MDP Collaboration meeting 2024
From ten-stack Analysis:
Transverse Pressure Bi-2212 Stress State
From measurements (University of Twente):
Transverse Pressure Curr. Degradation
What we have:
From Hybrid Magnet Analysis:
Bi-2212 Stress State Curr. Degradation
What we want:
Half Bi-2212 ten-stack model with applied transverse pressure and stress results at 100 Mpa.
Mechanical results from the hybrid dipole configuration must be interpret accordingly to the current degradation law. The blue line is the one use in Python code.

## Slide 5: LTS/HTS Hybrid Dipole Analysis – Current Degradation
Curves for the Hybrid LTS/HTS Cos-theta Dipole
Considering the most conservative ε criteria, the average current degradation is around 23.6 % (24.5 % at 8 kA and 22.6 % at 6 kA). In all the other ε/σ criteria, the analysis gives as results an IC degradation from 1.6 % (εeqv criteria) to 2.5 % (σint criteria).
Progressive Current Degradation at Different Current Initial Values

## Slide 6: Hybrid Dipole with Homogeneous Cable Model
Same structure, same pre-stress, same current powering of heterogeneous model hybrid dipole analysis.
Homogeneous cable model, anisotropic material properties for both Bi-2212 and Nb3Sn cables, proper elem-CS.
Hom. model results underestimate the critical current degradation: 0.75 % (εeqv criteria), 0.6 % (εint criteria).

## Slide 7: Conclusions
Consistent amount of simulation were performed using stress and strain Von Mises and Intensity criteria, for both homogeneous and heterogeneous models starting at different critical currents.
The heterogeneous model was necessary to study the current degradation accurately, huge difference with homogeneous model.
The current degradation is modest in all configuration except with strain intensity criteria.
Map more points of the analysis, current degradation with different criteria and various initial IC for both cable models.
Consider to reproduce University of Twente measurement set-up on ANSYS, to be able to translate in a more consistent way the transverse pressure current degradation effect into the stress-state induced one.
Finalize 3D Bi-2212 Rutherford cable model on APDL.
Take away concepts:
Next steps: