## Slide 1
Igor Novitski
January 30, 2019
Fermi National Accelerator Laboratory
15 T Dipole Prestress and Implementation

## Slide 2: 15 T Dipole Magnet design
1 – 4-layer Nb3Sn coil
2 –coil-yoke stainless steel spacer
3 – iron yoke laminations
4 – alignment key
5 – aluminum I-clamp
6 – iron filler
7 – stainless steel welded skin
8 – stainless steel axial rod
9 – stainless steel pusher plate
10 – bullet
2
4
1
7
9
10
8
3
6
5
February 8, 2018
15 T Dipole Mechanical Analysis and Mechanical Model Tests
1100 mm
Weight=2362 kg
612 mm

## Slide 3: Design and Conservative coil pre-stress
300K
Seqv=133 MPa
Limit 150 MPa
4K
Seqv=176 Mpa
Limit 200 MPa
4K+15T
Seqv=168 Mpa
Limit 200 MPa
Location | Yoking-clamping | Skin welding | Cooling-down | Bmax = 14 T
IL Pole | 60 | 113 | 150 | ~5
IL MP | ~15 | ~40 | ~75 | 143
Conservative pre-stress: Smax at all steps <150 MPa
Design coil pre-stress

## Slide 4: Coil Interfaces were analyzed and optimized by appropriate radial shims
HFM-CL1-002 230mm from RE
HFM-CL1-003 230mm from RE
Coil SS 230
L2 OD by 80 mic smaller
L2 OD by
96 mic smaller
HFM-CL2-004 201mm from RE
HFM-CL2-005 218mm from RE
L3 ID by 88 mic smaller
L4 OD by
80 mic smaller
L4 OD by 187 mic smaller

## Slide 5: Coil Block was shimmed to the design radial size and wrapped with GI

## Slide 6: Coil Block Yoking

## Slide 7: Coil Massaging and 1st Yoke Clamping

## Slide 8: Coil pre-stress after 1st clamping (SGs)
from RE
Coil pole azimuthal stresses before/after clamping
- LE cross-section: 32-84(33 avr.)/25-36 (24 avr.)MPa
- RE cross-section: 36-94(56 avr.)/30-43 (48 avr.)MPa
Pre-stress reduction after spring-back ~30%
Coil pre-stress is smaller than expected 60 MPa due to larger clamp size by ~4 mills.
It has to be compensated by additional radial shim ~5 mills Kapton.

## Slide 9: Iron Lamination Side Gap measurement
Data shows that we can use uniform radial shim in the straight section.
The shim is gradually reduced to 0 at coil ends.

## Slide 10: Yoke Removal

## Slide 11: Radial shim installation and expected outside yoke gap

## Slide 12: Expected gap sizes based on MM Measurements
February 8, 2018
15 T Dipole Mechanical Analysis and Mechanical Model Tests
These gaps will be measured and compared with expectations.

## Slide 13: Skin welding
Skin SGs welding history
Stress, MPa
Skip welds under the press
and hand welds on a table

## Slide 14: Gap Control Procedure Mirror Magnet
after Skin Loading
AL Clamp
after Clamping

## Slide 15: Magnet Ends Load

## Slide 16: Final assembly
Lead insulating spacers
Stand-off plate
G10 splicing plates
G10 cover plate

## Slide 17: Conclusions
To reduce the risk of coil damage during assembly the target prestress was limited by 150 MPa. It limit the target field during the first test by ~14 T.
Target coil pre-stress is defined for each assembly step including yoking, clamping, skin welding and cooling-down.
Assembly of 15 T dipole demonstrator is at the iron clamping stage
  the first clamping has been done and the second one with a larger radial shim is in the progress
  The goal is to reach ~60 MPa in the coil IL
The pre-stress during skin welding will add ~ 50 Mpa and we will achieve our target of ~115 Mpa
The level of maximum coil pre-stress after cooling-down will be controlled by the adjustable gap shims based on the gap measurements after welding

## Slide 18: Shim Plan was developed based on FEA
Yoke-Skin Rad interference
d Skin and skin thickness
Clamp-Yoke
interference
Pole slot
Mid-Plane shims
Shell-Yoke Rad
interference
Clamp-Skin Rad
interference
Coil-Coil Rad
interference
Yoke-Yoke
gap taper
Filler-Yoke interference
FEA | FNAL | FEAC
MP Shim L1/2 | 0 | 0
MP Shim L3/4 | 0 | 0.06
Shell-Yoke radial | 0 | 0.025
Yoke-Skin Radial | 0.3 | 0.6
Yoke-Yoke Gap t/b | 0.375 0.275 | 0.42 0.36
Yoke-Clamp interference | 0.3 | 0.4
Skin weld | 0.4 | 0.4
Filler-Yoke interference | 0.1 | 0