## Slide 1: Can we detect signs of training in solenoids? If so, what can we learn from them? Part one: Solenoid fabrication
By: Charlie Sanabria
and Sofía Jiménez Viñolo

## Slide 2: First Prototype
38.1 mm
45.47 mm
2b = 14.65 mm
a2 = 21.70 mm
a1 = 19.05 mm
Expected number of turns = 20 x 4 = 80
Wire length ≈ 10.24 m
Wire + insulation Ø = 0.73 mm
Drawing prepared by
Ray Hafalia
OFHC Cu current leads
Alumina washers
Alumina-coated Stainless steel mandrel
Centering cone (G-10) for testing
Notes: Boron nitride sheets?

## Slide 3: Wire properties and stress calculations
Diameter | 0.6 mm
Non-Cu% | 56.5%
Average RRR | 200
B (T) | Ic (A)
8* | 504
9* | 420
10* | 349
11* | 289
12 | 238
13 | 194
14 | 156
*
Extrapolated using the Pong-Ekin scaling spreadsheet
“Medium Jc” RRP wire critical current (bold values provided by vendor).
“Medium Jc” RRP wire properties
Hoop stress
2b = 14.65 mm
a2 = 21.70 mm
a1 = 19.05 mm
B (T) | Stress on OD (MPa) | Stress on ID (MPa)
8 | 177 | 155
9 | 166 | 146
10 | 153 | 134
11 | 140 | 122
12 | 126 | 110
13 | 111 | 97
14 | 96 | 84
Wire purchased by ASC
Notes: Boron nitride sheets?

## Slide 4: Stress calculations at 9 T
Hoop stress
Displacement
ID
OD
146 MPa
172 MPa
2b = 14.65 mm
a2 = 21.70 mm
a1 = 19.05 mm
72.1 µm
Simulations by L. Brouwer
Sliding surface

## Slide 5: Winding (1 of 4)
Magnetic break inside aluminum payoff spool.
Back tension constant and capable of unwinding.
2.75 lbs. of tension.
Payoff spool
Magnetic break

## Slide 6: Winding (2 of 4)
March 6th 2019
Mica
layer
Sharp turn.

## Slide 7: Winding (3 of 4)
8 mm x 5 mm mica pieces

## Slide 8: Winding (4 of 4)
Winding speed: ~3.7 RPM
number of turns: 18, 17, 17, 17
Acoustic sensor will go on top of the mandrel
No voltage taps between layers
One pair of voltage taps will be added after HT.

## Slide 9: Heat treatment (1 of 2)
Standard “Medium Jc” RRP heat treatment.
Recipe:
210°C/48h + 400°C/48h + 570°C/24h + 660°C/50h
Starting date: Friday 8th, 2019
Wrapped with a fiberglass sheet.
Inside tube furnace with flowing argon.
210°C
400°C
570°C
665°C

## Slide 10: After heat treatment (2 of 2)
Actual measurement [units] | Value
Ramp Rate to 210°C [°C/h] | 44.5
210°C temperature [°C] | 210.8
Time at 210°C [h] | 47.3
Ramp Rate to 400°C [°C/h] | 53.3
400°C temperature [°C] | 399.2
Time at 400°C [h] | 47.7
Ramp Rate to 570°C [°C/h] | 57.2
570°C temperature [°C] | 573.3
Time at 570°C [h] | 24.0
Ramp Rate to 665°C [°C/h] | 55.0
665°C temperature [°C] | 666.4
Time at 665°C [h] | 59.3

## Slide 11: Current status and future plans
Potting and instrumentation in progress.
Testing early April.

## Slide 12: Improvements for next prototype
Target turns were not met. Coating thickness or solenoid dimensions could be adjusted.
New mandrel design
Stronger washers?
Prototype 1
Prototype 2
Interlayer voltage taps… any ideas?
Cost reduction alternatives:
  Leads can be broken in two pieces.
  Mandrel could be 3D printed.

## Slide 13: Names?
STEP coils (Solenoid Training Experimental Project)
SISTER coils (Small Inexpensive Solenoid Training ExpeRiment)
T(r)IPS coils (Training and Interphase Probing Solenoid)
ETCIE coils (Experimental Training Coil Interphase Exploration)
ISETIE coils (Inexpensive Solenoid Experiment for Training and Interphase Exploration)
The little coil that could…