## Slide 1
Ramesh Gupta
Brookhaven National Laboratory
BNL experience related to
HTS accelerator magnets
MDP Videoconference on May 15, 2019

## Slide 2: BNL at USMSP
BNL is glad to join US magnet development program…
Funding is in place in May FIN plan, which means we can start working soon.
Key memorandum is being signed, if not done already.
The initial scope of work for this year was planned to do (a) quench studies on CORC cable and (b) magnetization studies of HTS tape coils (field primarily parallel to the wider face), both in the background field of BNL 10 T common coil dipole.
A detailed plan for will be presented in a future presentation for your feedback. We are already in discussion with LBL and ACT.
The purpose of this presentation is to review previous BNL HTS magnet programs related to accelerators. We are open to sharing experimental data for better scientific understanding.

## Slide 3: HTS Dipole and Quadrupole Magnet Programs at BNL for Accelerators
Hybrid Dipole with CORC® Cable (Phase II SBIR)
High field hybrid collider dipole (Phase II STTR)
Overpass/Underpass HTS dipole (Phase I SBIR)
Curved dipole with the ReBCO tape (Phase II SBIR)
High radiation HTS Quadrupole for FRIB (FRIB/DOE)
Bi2223 HTS tape common coil dipole (DOE)
HTS magnet for NSLS (BNL Project)
HTS quadrupole for RIA (funded by DOE)
Bi2212 Rutherford cable Common Coil Collider Dipole (DOE)
Cosine theta dipole with 4 mm YBCO/ReBCO tape (SBIR)
Cosine theta dipole with 12 mm YBCO/ReBCO tape (SBIR)
BNL can make a significant contribution to the US MDP for developing high field HTS accelerator magnet technology with the above and other high field HTS solenoid programs

## Slide 4: Overview
The goal of this presentation to (re)familiarize everyone with some of these programs to help collaboration to benefit from that experience

## Slide 5: Cosine Theta Coil with 4 mm HTS Tape - SBIR Phase I (1)

## Slide 6: Cosine Theta Coil with 4 mm HTS Tape - SBIR Phase I (2)
No measurable degradation

## Slide 7: Kapton-Ci Insulation on ReBCO Tape (and Making a NbTi Type Cured Coil)
77 K tests show no degradation in conductor performance
Part of an same STTR

## Slide 8: Cosine Theta Coil with 12 mm HTS Tape - SBIR Phase I (1)

## Slide 9: Cosine Theta Coil with 12 mm HTS Tape - SBIR Phase I (2)
No measurable degradation

## Slide 10: HTS Curved Coil with Cryo-cooler (SBIR Phase II with Muons, Inc.)

## Slide 11: SBIR on CORC Cable with ACT (Phase I and Phase II)

## Slide 12: CORC Cable Test at BNL (Phase I SBIR with ACT)

## Slide 13: Measurements at the original V-taps

## Slide 14: Measurements at the additional v-taps on the leads (data recorded with fast logger every 100 microsec)
77 K Test to ~3000 A

## Slide 15: HTS Coil with Bi 2212 Rutherford Cable (React & Wind)
Several Bi2212 cable racetrack R&D coil built and tested at BNL.
  Minimum bend radius 70 mm; Cable thickness ~1.6 mm.
    Bending strain 1.4% or 0.7% depending on whether the wires in the cable are sintered or not.

## Slide 16: Bi2212 Ruther Coils and Magnets
Five Accelerator Type R&D Magnets
HTS from Showa
Cables made at LBL
All React & Wind

## Slide 17: Bi2212/Nb3Sn Hybrid Dipole
6
6
7
7
(Magnet DCC014)
(Magnet DCC012)
(Magnet DCC008)
HTS/LTS Hybrid Magnets (background field provided by Nb3Sn)

## Slide 18: Freeway Overpass/UnderPass (or clover-leaf) Ends
ASC2002
HTS test coil wound in Phase I with e2P/BNL SBIR
BNL
ASC2018
CERN

## Slide 19: Demonstrations of the Overpass/Underpass in Phase I
12 mm wide tape
No degradation
SBIR with e2P
77 K Test Results

## Slide 20: PBL/BNL STTR on HTS/LTS Hybrid Dipole
A unique feature of BNL’s common coil dipole: large open space for inserting & testing “coils” without any disassembly (rapid around, lower cost)
STTR Phase II for (1) Demonstration and protection of High field HTS/LTS hybrid dipole (2) measurement of field parallel and perpendicular field quality
BNL Nb3Sn common coil dipole DCC017 without insert coils
Empty space
HTS coils inside Nb3Sn dipole - early experience of HTS/LTS hybrid dipole
Insert coils in Empty space
Original structure
New structure
New HTS coils with the existing Nb3Sn coils and become part of the magnet

## Slide 21: Retest of Nb3Sn Common Coil Dipole After a Decade
Current (A)
~9.5T@10kA
Short Sample: 10.8 kA/10.2 T (reached during 2006 test)
Retest: No quench to 10 kA/9.5 T (>92% of quench, leads limited)
A reliable magnet for test facility

## Slide 22: HTS Quench Protection

## Slide 23: HTS Coil Quench Test in HTS/LTS Hybrid Dipole Structure
Chart: Hybrid Dipole Field (T)
| 5.477777777777777 | 6.79
 | 0 | 756
 | 0 | 741
 | 0 | 712
 | 0 | 682
 | 0 | 656
 | 0 | 800
 | 0 | 500
 | 0 | 635
 | 0 | 500
 | 0 | 500
 | 0 | 500
 | 0 | 500
Encouraging Results:
HTS coils were ramped to quench, just like LTS coils
No degradation in HTS coils despite a number of quenches
Significant demonstration. 8.7 T may be the highest field HTS/LTS hybrid dipole magnet

## Slide 24: Operation of HTS Coils
Chart: 
HTS coils operated like LTS coils
Significant voltage in HTS coils: >0.2 Volts

## Slide 25: HTS and LTS Currents (just before and after the quench)
Chart: 
Chart: 
Separate power supplies and separate energy extraction for HTS and LTS coils
HTS and LTS coils have different inductances and different characteristics
LTS Common Coil Current (A)

## Slide 26: Magnetization studies in high field at 4 K in magnets made with the HTS tapes (Hall probe measurements)
A select data presented in a couple of slides.
A significantly more data available.

## Slide 27: Test Run at 4 K (in 2 T background field from Nb3Sn coils)
Additional field from the HTS coils in up and down ramp
(offset to start from zero to start up-ramp)
PBL/BNL STTR
field perpendicular configuration

## Slide 28
Decay of Trapped Field
(after the final run to ~8.7 T hybrid field @ 4 K)
Flux creep

## Slide 29: Summary and Conclusions
With it’s vast and unique experience with various HTS, BNL can provide a strong contribution to US high field Magnet Development Program, particularly in the area of HTS magnets
With a unique team experienced in large scale magnet productions in partnership with industry for superconducting colliders, BNL can help develop HTS magnets that industry can build
BNL common coil magnet provides immediately a unique fast turn around, low cost magnet development test facility
BNL can make unique and significant contributions by providing answers to key basic science and technology within a year

## Slide 30: Extra Slides on FRIB Quench Studies

## Slide 31: Protection of HTS Magnet During an Operational Accident Near Design Current
175A
185A
Design: 210 A in SP Coils
Ringing in power supply made situation worse
90mV

## Slide 32: Snap Shot of the Event (Quench?) that Triggered the Shut-off
Fast data logger:
One point/msec
Large inductive voltage in individual coils (ramp)
Small quench detection threshold (2 mV) kept during the ramp by monitoring difference voltage
Diff
voltage
No degradation in coil performance after the event

## Slide 33: Event (Quench?) while ASC Coils were held at 382 A (design: 310 A) at ~50 K (design: 38 K)
Current (A)
Coil Voltages
(mV)
Zoom
Slow logger:
One point/sec
Shut-off
Shut-off
Events prior
to Shut-off
Coil Voltages
(mV)

## Slide 34: Snap Shot of the Event in ASC Coils (individual and difference voltages)
Difference Voltage
Fast data logger
One point/msec
Shut-off
This and previous event appear to be the sign of flux jump
This exceeded quench threshold, triggered shutoff & energy extraction
Event at (a)12 K above the design temperature and (b) at 24% above design current
No degradation in coil performance observed

## Slide 35: Operation Well Beyond the Quench Detection Threshold Voltage (~ mV)
Operated at about two order of magnitude beyond the quench detection threshold. No degradation in coil performance observed.
Test temperature: ~67 K
(ASC to 150 Amp; SP to 100A)