## Slide 1: Ian’s selected review on Cu RRR
Ian Pong (ipong@lbl.gov)

## Slide 2: References
IEC 61788
Various papers by Fickett, including his 1974 MSE review
Munday et al. 1982 J. Phys. F: Met. Phys
N. J. Simon et al. NIST Monograph 177
ITER experience IEEE 2010, 2012 Jewell, Pong et al.
AUP experience Cryogenics 2024 Pong et al.

## Slide 3: RRR Definition
Residual Resistance Ratio – as defined by IEC 61788
Also typical usage:
  LT
    Cu at 4.2 K
    Nb-Ti wire at ~10 K (just above TC)
    Nb3Sn wire at ~20 K (just above TC)
  RT
    Often 273 K - 308 K, definition 293 K
    Correction formula available

## Slide 4
Pong et al. Cryogenics (2025)

## Slide 5: IEC 61788-4
Formerly 61788-4 (Nb-Ti) and 61788-11 (Nb3Sn); since 2016 (4th edition) just 61788-4
Resistance, not resistivity
For composite superconductors under TC 90, scope:
  “monolithic structure”
  RRR < 350
  Rectangular or round cross-section, area < 3 mm2
  For Nb3Sn, after HT

## Slide 6: RRR Notable Details
Resistivity can change when the dimension gets close to the mean free path
Impurities at concentration much below chemically detectable levels can still impact electrical conductivity considerably, that’s why RRR is an important SC QC
“Chemical purity” vs. “electrical purity”
Magneto-resistance effect (applied B impacts RRR)
Microstructure effect (annealing condition impacts RRR)
~17 K - 20 K resistance rise depends on RRR

## Slide 7
Hopkins et al. MSE A (2007)

## Slide 8
Simon et al. NIST Monograph 177

## Slide 9: Heat Treatment
Recovery and recrystallization: RT resistance may not be much affected, but LT resistance may decrease markedly (dislocations annihilate, grains grow  RRR increases)
An important factor: furnace impurity (line of sight from heating elements, environmental residue from retorts, etc.) – easy fix: quartz tube and/or glass fibre
Atmosphere: trace oxygen may help by oxidizing ferromagnetic impurities, reducing their ability to scatter electrons at LT and thereby boosting RRR

## Slide 10: Oxygen Annealing
CuO black, Cu2O “red”
Redox – can be reversed (reduction is slower)
Impurity must have a greater affinity for oxygen than Cu
Oxidation is internal (not surface) because of a much higher oxygen diffusion rate in Cu than impurity diffusion
  Experiment: oxidize, remove surface, reduce
A small effect: oxide + interstitial oxygen

## Slide 11: Nitrogen annealing
Some reported Nb3Sn HT in pure N2 improves RRR
Some reported no change
Possibly depends on the concentration of trace oxygen

## Slide 12: Some numbers
Oxygen solubility in Cu increases with T (i.e. oxide would precipitate on cooling)
Ref.: 400 at. ppm O ~ 0.01 wt% O2
Commercial “oxygen free” typically <0.04 wt% O2 (Cu2O)
Cu2O not considered to have a significant effect on RRR of the relatively pure Cu we would typically care
Oxygen diffusion depends on T and t – but typical Nb3Sn HT is fine

## Slide 13: A few more numbers
OFHC typical RRR >100
“Five nines” (99.999%, or 5N) typical RRR ~1,500
In very high purity Cu (RRR ~10,000), e- mean free path ~0.4 mm at 4 K and size effect contribution to LT resistance of wires may be considerable to that of bulk
In very high purity Cu (RRR ~10,000), 0.15 at. ppm Fe may contribute just as much (0.15 nΩ.cm)
Notes: λ=mvF​​/ne2ρ

## Slide 14: IACS
The International Annealed Copper Standard resistivity should not be confused with the IEC RRR
IACS is for 20°C, mostly power transmission
A resistivity value is defined, and industry typically give conductivity values solely as a % of the IACS figure

## Slide 15: C101
Copper alloy 101, or UNS C10100
A.k.a. OFE or OFHC
~99.99% (four nines, 4N)

## Slide 16: Iron
Fe  FeO  Fe3O4  Fe2O3
0.1% Fe oxidized copper alloy can become magnetic
Ferromagnetism of the oxide magnetite depends on the size of the oxide particles
Resistivity depends on the volume of the impurity that is oxidized
No simple relationship between Cu resistivity and impurity magnetization

## Slide 17: Kondo Effect
Electrical resistance versus T at LT
Minimum before rising again
Related to magnetic impurity in nominally pure metals
As electrical conductivity is related to thermal conductivity by the Wiedemann-Franz law, the same may be observed in thermal properties
Berman and Macdonald Proc. Royal Society (1952)

## Slide 18: Other Effects
Wire processing
  Typically only degrades the initial Cu
  Drawing die cleanliness and wear are known to impact RRR
  Diffusion barrier integrity is critical for Nb3Sn (due to HT)
  Coating (Cr) impurities diffusing into the wire during HT
Wire cross section
  RRR contribution across the wire cross section is not uniform in multifilamentary bundled / restacked wires
  Subelement orientation in rolled wire matters (Baskys et al. IEEE TAS 2023)

## Slide 19: International BM / CC / RR
61788-4 (2016) Nb-Ti:
  Sigma 4.4 on x-bar 178.5  2.44% COV
  Recommend COV <2.5%
61788-4 (2016) Nb3Sn:
  COV 6.07%
ITER:
  COV Nb-Ti (0.8%), Nb3Sn BR (9.7%), Nb3Sn IT (14.1%)
  IO-prep vs. Self-prep – HT isolated from measurement
AUP:
  LBNL RRP® RRR ref COV 0.15%(!!); witness ref COV ~1.3%(!!)

## Slide 20: Summary
RRR for Cu, Nb-Ti, Nb3Sn BR, and Nb3Sn IT have different definitions and different uncertainties (COV)
Microstructure (processing history and HT) impacts RRR
HT controls (time, temperature, trace oxygen, cleanliness) are very important for reliable and repeatable RRR
Oxygen can take out ferromagnetic impurities, reducing their ability to scatter electrons at LT and boost RRR