## Slide 1
MDP bi-weekly meeting
X. Wang, 10 September 2025
C3 update

## Slide 2: Topics for today
Tests we have so far, especially the second test in June
  See Yufan’s talk at MT-29
First look at the short-sample limit at 4.2 K
What’s next

## Slide 3: Magnet design was driven by the 30 mm minimum bend radius of the CORC® wire as of 2018
ID 65 mm, OD 160 mm, 900 mm long
Today’s CORC® wire can be bent to 20 mm radius

## Slide 4: Coils and shell before assembly, November 2024
A. Saravanan designed the mandrels
R. Norris designed the shell
Co-wound two optic fibers with the CORC® wire in each layer
Image courtesy of A. Lin

## Slide 5: C3 has an iron yoke outside the aluminum shell
Designed by L. Brouwer, R. Norris and D. Arbelaez, following Nb3Sn CCT5
25.4 mm thick laminations, 76.2 mm radial thickness, covering 406 mm magnet length
Increased the TF by 30%, from 0.72 to 0.93 T/kA

## Slide 6: The unplanned Stycast in the aperture limited the scope of the first test
Stycast leaked into the aperture and filled ~ 40% of the volume
  Not trivial to quickly remove it
  Impact on magnet/conductor unknown
Live with the Stycast in the first test
  Assess the magnet performance without pushing
  Install a Hall probe in the aperture to verify the dipole field

## Slide 7: The magnet showed a reasonable performance
staircase ramping
simple ramping
Y. Yan
We stopped at 5.75 kA with Layer 1 voltage peaked at 14 µV

## Slide 8: Generated a dipole field of 5.2 T, agreeing with the calculation
Calculation by Y. Yan and L. Brouwer
Dipole field (T)
5.2 T
4.2 K
Dipole TF (T/kA)
4.2 K
Iron contributed 1.1 T,
21% of the total field
First 4.2 K test, March 2025
Measured using a Hall probe

## Slide 9: Removing the Stycast was stressful
Peak strain increased by 200 µε as we got desperate and cut harder
Would it degrade the conductor and magnet performance ?
Fiber in Layer 1 picked up the strain as we started – conductor was strained
3/27/2025

## Slide 10: Questions for the second test
Did removing Stycast in the aperture degrade the magnet?
What’s the field quality?
  Measure with a rotating probe developed by J. DiMarco
Can we push for a higher magnet voltage and dipole field?
Notes: What’s the short-sample prediction?
  Measure the Ic (B) of the wires at 77 and 4.2 K

## Slide 11: 77 K data showed a Ic degradation after removing the Stycast
after removing Stycast
before removing Stycast
Y. Yan

## Slide 12: The degradation, however, was less obvious at 4.2 K
Y. Yan

## Slide 13: We stopped at 105 µV across Layer 1, reaching 6.75 kA at 4.2 K
Y. Yan
06/25/2025: peak current 6.75 kA, Ic = 6741 A at Vc = 100 µV, n = 13
Layer 1 initial voltage increase started at ~3 kA
Slow voltage rise also observed in Layer 4

## Slide 14: The dipole field reached 5.99 T at 6.75 kA
Calculation by L. Brouwer and Y. Yan
Peak I x B force on the conductor ~ 42 kN/m
Iron contribution ~ 1.1 T, 19% of the total field
5.99 T
4.2 K
4.2 K

## Slide 15: Field profile roughly matches that from simulation (w/o magnetization)
B1 TF (T/kA)
Rotating coil developed by J. DiMarco; Measurement system by B. Ghiorso and R. de Leon.

## Slide 16: Stronger persistent-current effect at 77 K than at 4.2 K in the normal sextupole, b3
-11 units at 4.2 K
-33 units at 77 K
Different from C2

## Slide 17: One of the mysteries in the measured multipoles
The trajectory of the multipoles reversed during the down ramp around 2 kA
Current (A)

## Slide 18: Short-sample dipole field for C3 is at least 8 T at 4.2 K
Measured Ic(B, 4.2 K) for Layers 5 and 6
Expect better performance for the inner-layer conductors
ACT will measure the short samples for the other layers

## Slide 19: Two conclusions
Layers 1 and 4 likely degraded before the test
  Measure the short-sample performance at 77 K to confirm
  Search for causes of degradation  learn and share lessons  fewer bugs next time
Can reach 10 T dipole field using today’s CORC® wire based on the HM tapes
  Verify that the conductor will be mechanically sound
  Search for $

## Slide 20: Next – what can we learn from a third test?
Is the magnet still sound?
  Effect of previous test and thermal cycles
Complete the field-quality study
  Maxim: Design cycles to verify if the reverse of the multipole was due to the magnetization effect?
Will repeated current cycling degrade the performance?
  Effect of stress cycles
Can we identify the weak point in the winding?
  Holding current at high current for a longer period and see if the fiber picks the temperature rise
What’s the current limit?
  Push to a higher current without or with thermal runaway
  Maxim: try the MOSFET to shift the current in Layer 1

## Slide 21: Next - dig into the fiber data and validate finite-element modeling
Pole
Midplane
Midplane
Calculation by G. Vallone
Measurement by L. Luo
[Vallone et al., Fri-Mo-Or2-03]
[Luo et al., Wed-Af-Po.08-07]

## Slide 22: We can learn a lot from C3
Data mining just started – hope the funding will be back soon
Keep making better magnets and learn

## Slide 23: Questions / comments
Lance: does the model consider the location of individual tapes?
  No, the model considers the CORC wire as a cylinder carrying uniform current density across the entire cross section of the wire.
George: the data at the center of the magnet at cold includes both magnetization and geometric effect
Steve: can we tell if the degradation occurred before the coil fabrication?
  It’s a good point. We can’t yet.
Ramesh: can we have the leads outside the cryostat to test individual layers?
  Yes, it is a good idea. Vadim did that for the COMB magnet
Vadim: Layer 1 is expected to see the highest field so the voltage rise in this layer is expected.
  Yes. However, Layer 2 has almost identical peak field as Layer 1 but it didn’t generate significant voltage. However, we cannot rule out Layer 1 wire was degraded before coil winding, as Steve mentioned.

## Slide 24: Questions / comments
Maxim:
  The reverse of the multipole can be a result of the change of the magnetization in the conductor.
  The MOSFET switch will be available soon. May use it to bypass the current in Layer 1.
David:
  Can we push the current to the current-sharing regime and check the magnet performance?
Dima:
  Slide 16. Field quality experiment: How close to Ic value was the bias current at 77K and at 4.2K?
  About uniformity. Do you have TapeStar data for Ic(77K, x)? Does nonuniformity suggest layers 1 and 4th layer having problems?
There may be more that I missed