## Slide 1
Status of Recent Quench Antenna applications at Fermilab for CCT5w and HTS tape
19Nov 2025
Presented by J. DiMarco
work in progress…

## Slide 2
CCT5w ‘TAN coil’ QA test

## Slide 3
Second warm bore QA
16 tangential loops around 41mm diameter cylinder; 2-layer pcb, 36 turns total
24-bit, 200 kHz sampling daq
Quench trigger
Signals with
60 Hz filtering
Three types of quench antennas were used:
  Inter-layer QA
  Warm-bore slant QA with 28mm dia.
  Tangential warm-bore QA array with 42 mm dia.
Data taken typically for entire ramp, all tests

## Slide 4
Harmonic multipole sensitive QA have been used to localize quenches radially and azimuthally
- The thought here was to use an array of tangential windings to do the same type of analysis
TAN probe array can give measurement of all low order harmonics (below Nyquist order) – in principle can measure and use any pairs of consecutive harmonics to do this

## Slide 5
Simulated flux in vertices
Field from Line Current doublet
16 vertex QA layout
The TAN analysis works well with the simulated data in determining the location of the quench source

## Slide 6
Measured Flux
Note that symmetric, and not really indicating that part of the coil is closer to the source.

## Slide 7
Analysis does not work!
(Not valid results, not consistent among harmonic pairs…)
Still working on this -
Could be that CCT cable geometry requires a somewhat different analysis (?) …

## Slide 8
HTS REBCO QA test

## Slide 9
36 loop (18 front/back), ~4mm average loop width, 80mm length
REBCO tape
Voltage taps
LN2 bath

## Slide 10
Clear activity here

## Slide 12
Using running average and normalizing by the standard deviation
Some sort of signal – presumably from current redistribution in the tape - is clearly visible about 1-2 s before threshold exceeded

## Slide 13
Can integrate to see signal in terms of flux change