## Slide 1
MDP Work for IR Magnets: EIC Stacks with CTD 1.1 binder
S. Krave, G. Ambrosio
11 February 2026

## Slide 2: Exploration of NbTi cable stacks with intermediate binding
Fermilab is if fabrication a large IR quad for EIC of the key and bladder design and required a rigid cable composite
  This leads to the requirement of epoxy impregnation
  To minimize risk we wish to have a similar process to MQXF
    Intermediate curing stage between layers with a binder
      CTD 1.1 BDR

## Slide 3: Why Binder
Pre- impregnation binder process to set coil layer geometry after winding
The process has been proven in the MCBXF
CTD 1.1 is an epoxy compatible binding system dissolved in a solvent (Acetone or MEK)
  The system appears to be raw B-staged epoxy resin. (Guessing the same system as 101K)
  Cured with heat similar to other binder systems
    Allows drop in replacement to allow same curing process as the Ceramic binder in QXF

## Slide 4: Goal and Steps
Determine mechanical properties of potential insulation systems for EIC
  Handling, Modulus (1-3 directions), CTE, dielectric strength, AC Loss???
Final step: fabrication of accelerator quality coils up to 3.8 m for large aperture magnets (up to 135 mm).
Intermediate steps:
  cable-stacks to demonstrate good quality impregnation, and make samples for measurements of mechanical and electrical properties;
  1-m coils to demonstrate good quality impregnation, and make samples for measurements of mechanical and electrical properties:
Results to be compared with similar samples impregnated with CTD-101k to be used as benchmark

## Slide 5: Cable dimensions
EIC IR quadrupole cable dimensions

## Slide 6: Plans for cable stacks
Make cable stacks exploring insulation and impregnation options:
  Benchmark: S2-glass sleeve (used for HQ) impregnated with CTD-101k
  Using CTD 1.1 BDR
  Prototype using unreacted QXF cable
    Once process is established, use EIC-Like Cable (LHC Inner)
    Value Engineering -Telene
Measure structural properties at RT and 77K:
  Elastic modulus at RT to 75MPa (can be measured at Fermilab)
  Elastic modulus at 77 K (can be measured at Fermilab)
  Thermal contraction RT-77K
  Shear strength at RT and 77K (ASTM D2344) (can be measured at Fermilab with SBS test )

## Slide 7: Stack Configuration
The stacks are shimmed to nominal size (cable plus insulation)
  Fixed cavity not fixed Pressure
  Same constraint as QXF
Prototype stacks of QXF are being fabricated with equivalent constraints

## Slide 8: Sample Prep
Cable is sectioned and insulated
  Then placed in fixed cavity in AL channel
  Shims are made from 3D printed PPS-GF, good to ~200°C
    Super handy, I recommend getting a machine that can use this material
Binder is applied at desired rate. We found that the tooling allows easy distribution applied by disposable pipette
Apply unit volume per square
Dry

## Slide 9
1st set used 6 grams binder per total sample (3g solution, 1.5g solid/meter of cable)
  Missing photo but only ~3mm penetration into stack
Time to update the binder recipe

## Slide 10: Quick wetting test
Just to see behavior…
Glass did not pull mix aggressively from brush
Stayed wet under brush with no additional wicking (6781 S2/ 933HTS)

## Slide 11
Looking at wicking
  1:1 Binder to MEK did not wick substantially away from the brush
  Adding additional Solvent improved wicking to a point
    But did not pull aggressively away from brush.

## Slide 12: Added some Acetone to assist in resin takeup
CTD:MEK:Acetone
1:1:1
Fast wet out, low overall solids density
CTD:MEK
1:1
Spanish Recipe
Low wet out, high solids.
CTD:MEK
1:2
Intermediate wet out, uneven solids distribution
Trying to be more quantitative, we made a simple wicking test: Apply 1ml of solution and track spot size vs time
3 recipes:
  Standard
  Diluted with extra MEK (1 part solids to 2 parts MEK)
  Diluted with Acetone (1:1:1 Solids to Acetone to MEK)

## Slide 13: Summary of test
 | Diametral Distance traveled (to 1/8") |  | 
Time (seconds) | 1:1 Binder to MEK | 1:2 Binder to MEK | Acetone Blend
0.50 | 1.5 | 2 | 3
1.00 | 2.5 | 2.5 | 3.9
1.50 | 2.5 | 3 | 3.9
2.00 | 2.5 | 3.5 | 3.9
2.50 | 2.5 | 3.75 | 3.9
1:1 MEK system had small spot size and did not flow aggressively
1:2 system wicked substantially better
Aceton system drastically improved resin takeup
Normalized resin application rate to grams per square meter
Chart: True Resin Application Rate in 6781 S2 Glass
| 0.5 | 1 | 1.5 | 2 | 2.5
1:1 Binder to MEK | 438.5612 | 157.882 | 157.882 | 157.882 | 157.882
1:2 Binder to MEK | 164.4604 | 105.2547 | 73.0935 | 53.7014 | 46.7799
Acetone Blend | 73.0935 | 43.2506 | 43.2506 | 43.2506 | 43.2506

## Slide 14: For reference: Comparison to MCBXF system
From what I can gather the effective solids application rate in MCBXF per stack procedure was 23 g/m^2 of insulation
solids rate for QXF stack seems to bottom out at 40 g/m^2
  Not unlike MQXF ceramic binder
  Samples with same rate did not wet out MEK only

## Slide 15: Back to stacks:
No Acetone
With Acetone
Samples without acetone exhibited poor adhesion for the same geometry. Added acetone substantially improved adhesion
Same procedure, 2 more dilute Recipes.

## Slide 16: Stack Impregnation
Remove stacks form Curing fixture
Transfer to standard 10-stack impregnation fixture
Pot with selected resin
  101K first

## Slide 17
1st set of samples have been potted with CTD-101K and look very good
  Glass is fully transparent
    Fully wetted
    Good adhesion to cable
      Clear glass with white spots would indicate debonding between insulation and cable, but we do not see this
  Samples with Aceton and Without look nearly identical
Will measure shear strength, flexural modulus and possibly CTE next week.

## Slide 18: Moving forward
Preliminary Conclusion: 1:1:1 recipe provides good handling and impregnation. No reason to suspect issues mechanically.
Re-make 4-stacks to compensate for slightly different unreacted cable conditions
  1st samples used the reacted QXF cable equivalent
Make 10 stacks using the same recipe for compression modulus and Integrated thermal contraction to 77K using the strain gage technique
  Micro-Measurements TN-513-1 (~1 month)
Repeat 4/10 stacks with EIC Cable (4 weeks after cable)
  Likely 1:1:1 recipe
Benchmark against 101 K without binder
Repeat tests using Telene instead of 101 K

## Slide 19: Geometry References

## Slide 20
21.45 mm Outer
EIC Stack Layout
4.29 mm shim
2 x 8.58 mm 4-stack
2x 250 mm
25.27 mm
3.82 mm shim

## Slide 21
21.45 mm Outer
15.4 mm
EIC
4.29 mm shim
2 x 8.58 mm 4-stack
EIC
25.27 mm
25.27 mm
4.93 mm
4.93 mm