## Slide 1: CERN Conductor R&D
International HFM Meeting 2019
Washington, 4-5 December 2019
Amalia Ballarino, CERN
A. Ballarino, M. Benedikt, L. Bottura, A. Devred, D. Tommasini

## Slide 2: CERN Conductor R&D Program
Nb3Sn
HTS
Other Superconductors
A. Ballarino

## Slide 3: Nb3Sn
A. Ballarino

## Slide 4: CERN Conductor Development Program – Nb3Sn
Scope: develop, qualify and procure superconductors with performance meeting requirements of the CERN - magnet - programs
Present reference performance: conductor for 11 T - 12 T magnets (HL-LHC conductor) 
Explore and qualify different wire layouts; ensure availability and continuity of industrial production; sustain requirements of the CERN magnet development program via dedicated studies and conductor procurement
Final target performance: conductor for 16 T magnets (FCC conductor)  Explore, via R&D, possibilities for achieving the FCC conductor challenging targets; bring wire R&D to a level of development that enables starting technological optimization of Rutherford cables. Qualify Rutherford cables first in conductors’ test stations and then in short model coil dedicated programs
A. Ballarino

## Slide 5: CERN Conductor Development Program – Nb3Sn
Timeline: 2017 – 2024
Present reference performance: conductor for 11 T - 12 T magnets (HL-LHC conductor)
Final performance: conductor for 16 T magnets (FCC conductor)
2017
Dec 2024
HL-LHC Performance
FCC R&D
Dec 2021
R&D Implemented in industrial processes
Qualified long lengths of industrial wire
2020
Series HL-LHC
A. Ballarino
Lower cost
Long lengths
Notes: Focus of FCC program on Nb3Sn - need to provide input to the physics community in a relatively short time (when series procurement of HL-LHC conductor started)

## Slide 6: CERN Conductor Development Program – Nb3Sn
Conductor procurement: 2017 – 2024
 1.4 tons ( = 1.1 mm, 1 mm, 0.7 mm) of HL-LHC wire procured in 2019
500 kg per year as from 2020 ( 2.5 tons total) of the most promising wires developed in the framework of the program
R&D Wire (20 km – 50 km per R&D contract)
A. Ballarino

## Slide 7: CERN Conductor Development Program – Nb3Sn
Started in 2017 - collaboration agreements initiated in 2017 and 2018
Launched an international effort aiming at providing feedback on the possibility of reaching beyond state-of-the-art HL-LHC Nb3Sn high-field performance (Jc @ 16 T). Defined an intermediate milestone: achievement of HL-LHC performance;
Fostered Nb3Sn conductor development in industry. Investigated potentials and interest of future suppliers;
Promoted advanced activities (material science, studies and characterization) in laboratories and institutes world-wide
Program implementation
A. Ballarino

## Slide 8: CERN Conductor Development Program
Japan
Korea
Russia
Europe
Europe
Europe
Switzerland
USA
Europe
Europe
USA
Participants: industry, supported by national laboratories, laboratories, institutes and universities worldwide
Fermilab
INFN
A. Ballarino

## Slide 9: Nb3Sn wires – Targets
Production of about 20 km of wire by each of the industrial partners
*Processes shall enable scalability and show potentials for low cost large scale production
FCC
HL-LHC
*
A. Ballarino

## Slide 10: To-date results from industrial partners
A. Ballarino

## Slide 11: Nb3Sn development in Russia - Achievements
Distributed barrier wire developed during a 2-year programme with TVEL
12 km of 1 mm diameter wire supplied, with > 1 km average piece length
  Non-Cu Jc > 1100 A/mm2 (16 T, 4.2 K)
New wire design under development in a further 2-year programme
Wire cabled at CERN (trial Rutherford cable, 50 m long, 40-strand). Wire from two billets
RRR  180, Ic degradation < 2 %
TVEL Wire -  = 1 mm
Rutherford cable – 40 strands
A. Ballarino

## Slide 12: Nb3Sn development in Japan - Achievements
Joint CERN-KEK programme developing:
  Distributed tin wires with JASTEC
  Tube type wires with Furukawa
JASTEC: achieved Non-Cu Jc of 1000–1100 A/mm2 in piece lengths > 100 m with a final deff of  55 μm (reduction of deff from 267 µm, in 2018, to 65 µm)
  Rolling tests to assess suitability for cabling:
    RRR > 150, no Ic degradation after 15% rolling 
    Wire suitable for cabling
0.8 mm
Wire from Jastec
Wire round and 15 % rolled
A. Ballarino

## Slide 13: Nb3Sn development in Korea - Achievements
J. Kim, FCC Week 2019

## Slide 14: Nb3Sn development in Korea - Achievements
Four-year programme started with KAT in 2017
Developing common barrier wires with distributed Sn-Ti
  Achieved Non-Cu Jc  1000 A/mm2 (16 T, 4.2 K) for first trials tested
  6 km of latest trial wire (192 M) recently supplied (unit lengths from 100 m to 750 m)
Optical micrograph of 1mm diameter KAT wire from 6 km delivery
KAT, wire design evolution
A. Ballarino

## Slide 15: Nb3Sn Wire Industrial Development - Summary
A. Ballarino
S. Hopkins

## Slide 16: FCC Conductor Workshop – 5-6 March 2018, CERN
7 companies, two universities and two national research institutes
A. Ballarino

## Slide 17: FCC Conductor Workshop – 5-6 March 2018, CERN
“After a short project time, industrial Nb3Sn wires with Jc values between 850 and 1’100 A/mm2 at 4.2K/16T have been reached, i.e. approaching the level specified for HL-LHC”
“The cost target is ambitious: from the present review it seems difficult, but realistic, as was considered by more than one participant in a reasonable timescale”
“It is recommended that the short model coil programme should be extended to run in parallel with the period foreseen for the production of long model magnets, to allow the validation of results achieved by the conductor development programme”
A. Ballarino

## Slide 18: FCC Conductor Workshop – 5-6 March 2018, CERN
“The project is structured logically, with a staged approach and clearly defined intermediate steps (Jc, RRR, Deff, robustness and cost). We support a procurement of wires satisfying HL-LHC performance for use as well for cable qualification as in magnet R&D, also to demonstrate a solid interest in the result”
“Wire diameter and effective filament diameter specifications have been defined in combination with magnet design. It is acceptable to retain 60 microns as an intermediate specification, but it is urgent to conduct a study to define requirements. An integrated conductor programme considering cabling degradation, stability and margin issues should be established”
“The panel supports to test the Internal Oxidation approach and to consider processes compatible with this technique”
A. Ballarino

## Slide 19: Beyond state-of-the -art performance
A. Ballarino

## Slide 20: HL-LHC
Ispec= 632 A (12 T)
L. Cooley
Ispec= 632 A (12 T)
B. Bordini
Total procurement  30 tons
RRP 108/127
B. Bordini
PIT 192 Bundle Barrier
A. Ballarino

## Slide 21: FCC Jc Target
FCC Jc target vs HL-LHC performance
Needed: 7000 tons - 9000 tons superconductors
A. Ballarino

## Slide 22: Internal Oxidation Process at Fermilab
Chart: B (T)
| 16 | 16.3 | 16.7 | 17.2 | 17.600000000000001 | 18.100000000000001 | 18.7 | 19 | 19.5 | 20.100000000000001 | 20.5 | 21 | 21.3 | 22 | 22.6 | 23 | 23.4 | 24.3 | 25
 | 1740 | 1620 | 1480 | 1310 | 1170 | 1040 | 864 | 770 | 654 | 554 | 460 | 377 | 336 | 228 | 164 | 130 | 102 | 43 | 10.8
 | 1600 | 1430 | 1260 | 1090 | 932 | 767 | 717 | 607 | 512 | 407 | 343 | 274 | 212 | 179 | 89.7 | 32.6 | 8.12
HL-LHC | 2449.7876 | 2025.3774 | 1659.0942 | 1343.0963 | 1071.1715 | 838.3126 | 640.4232 | 474.1082 | 336.5197 | 225.2452 | 138.2209 | 73.6666 | 30.035 | 5.9716
 | 2700.1785 | 2224.1245 | 1816.6222 | 1451.0127
 | 2240 | 1866.9244 | 1554.461 | 1278.4237
FCC Target | 3430.7603 | 2836.4028 | 2323.4482 | 1880.9147 | 1500.1025 | 1173.9995 | 896.869 | 663.9562 | 471.2729 | 315.4406 | 193.5689 | 103.165 | 42.062 | 8.3628
FCC Target
HL-LHC
Internal Oxidation
Multi-filamentary wires
Record Jc in multi-filamentary ternary APC wires: Jc (16 T, 4.2 K) > 1500 A/mm2
X. Xu et al, arXiv:1903.08121, 2019
Fermilab, Hypertech, Ohio State University
Nb-1wt%Zr -7.5 wt% Ta
Birr = 27 T
Bc2 = 27.8 T
A. Ballarino

## Slide 23: Nb-Ta-Hf at Florida State University
5.8 T
Ta-Hf at FSU
Mono-filamentary wires
Ta-Hf at Hypertech
Multi-filamentary wires
Balachandran et al., FCC Week 2019
S. Balachandran et al., Supercond. Sci. Technol. 32 (2019) 044006
A. Ballarino
Notes: Here we show that addition of Hf to Nb4Ta can significantly improve the high field performance

## Slide 24: Internal Oxidation at University of Geneva
2019 Data
CERN-UNIGE Collaboration Agreement
A. Ballarino

## Slide 25: Beyond state-of-the-art performance
Collaboration Agreement with Florida State University
Meeting organized by KEK, in Japan, in spring 2019 (KEK, CERN, ASC)
Jastec and Furukawa studying implementation of Nb-Ta-Hf in industrial R&D billets (as part of the on-going FCC collaboration agreement)
Collaboration Agreement with Fermilab – to be finalized in early 2020
R&D on APC billets produced with the internal oxidation process, study of process industrialization, electro-mechanical studies and characterization of APC wires
Collaboration Agreement with the University of Geneva – CHART 2 (with contribution from Suisse National Foundation for Science)
    Production of R&D billets (monocore and multi-filamentary) with the internal oxidation process
    Collaboration Agreement with Bruker
        Internal oxidation process in PIT conductor
A. Ballarino

## Slide 26: Challenges to be addressed
Mechanical properties
  Optimization of wire layout
  Optimization of cable layout/impregnation
  Stability
    Wire
    Cable
    Field quality
      Wire’s filaments size
    Qualification in high-current and high-field test stations
      Wire
      Cable
A. Ballarino

## Slide 27: High-field test stations
CERN, Superconductors Laboratory
  15 T and 16 T solenoids for wires/tapes’s characterization (1.9 K and 4.5 K);
  Fresca (9.6 T, 50 kA, 1.9 K and 4.5 K) and Fresca 2 as from 2021 (13 T, 50 kA, 1.9 K, 4.5 K and Tvariable) for LTS and HTS cables’ characterization
  University of Geneva
  21 T, Tvariable, 2 kA
  University of Twente
    15 T, 2 kA for wires’s characterization (4.5 K)
    11 T, 50 kA, 4.5 K for cables’ characterization (electro-magnetic press)
    LNCMI, Grenoble
    10 T, 3 kA ( = 298 mm), 4.5 K and Tvariable
    20 T, 1.5 kA ( = 128 mm), 4.5 K and Tvariable
    30 T, 1.5 kA ( = 38 mm), 4.5 K and T variable
A. Ballarino

## Slide 28: HTS
A. Ballarino

## Slide 29: REBCO
Very high in-field electric performance (Je(4.2 K, 20 T) > 1000 A/mm2)
We do not need more Jc !
Questions to be addressed for use in accelerator magnets:
  Use of large tapes in accelerator magnets;
  Development of cables for accelerator magnets (stacks, CORC, Roebel,…);
  Quench detection and quench protection aspects (in tapes, cables and coils);
  Technological aspects, e.g. impregnation and electrical joints
  Questions to be addressed at the level of tape production:
    Achievement of controlled, homogeneous and reproducible electro-mechanical properties along the full length, e.g. internal resistance and copper stabilizer electrical resistivity. Needed feedback to tape manufacturer
  Feasibility of long lengths and cost reduction
A. Ballarino

## Slide 30
L. Rossi
EuCARD2/ARIES have triggered a international collaboration also beyond EU laboratories

## Slide 31: REBCO
Develop technical specification for procurement of tape. Interface with tape manufacturers to understand potential difficulties and limitations
Qualify tapes from different manufacturers
Develop, study qualify cable layouts suitable for accelerator magnets. CERN experience: stacks of tapes (developed dedicated cabling machine), round cables (CORC type), and Robel cables (produced at KIT and characterized at CERN)
Develop and qualify cables for demonstration coils (undulators, wigglers, high-field magnets)
A. Ballarino

## Slide 32: Other materials
A. Ballarino

## Slide 33: MgB2 for Power Transmission Lines
120 kA @ 25 K
18 kA @ 25 K
7 kA
@ 25 K
120 kA @ 25 K
Received 480 km of wire (ULs up to  3 km)
Additional 650 km for HL-LHC series production
Low-field applications (developed wire with ASG)
Medium-field applications (Collaboration Agreement with SPIN and ASG)
A. Ballarino

## Slide 34: Iron Based Superconductors
SPPC: 100 km circumference, 12 T
Baseline: iron based Superconductor
Strand | diam. | cu/sc | RRR | Tref | Bref | Jc@ BrTr | dJc/dB
IBS | 0.802 | 1 | 200 | 4.2 | 12 | 3800 | 111
Conceptual design with expected Je of IBS in 2025
Y. Ma, D. Wang et al
Collaboration Agreement with SPIN
A. Ballarino
BaFe2As2 (122) PIT
FeSexTe1-x (11) Coated Conductor
Focus on powder synthesis
Focus on substrates development
Target Jc:  1000 A/mm2 (16 T, 4.2 K)
122 Pellet
Invar 36 substrate

## Slide 35: Conclusions
Focus of the CERN conductor development program is on Nb3Sn. Program, targets and timeline are in line the with the magnet program. They will provide feedback to the HEP community on the feasibility of the FCC targets. To-date, effort, results and response from the world-wide community are extremely encouraging
HTS is explored via a small coils magnet program. Conductor study and development (REBCO tape and cables) are re-launched for better understanding potentials and limitations for future use in accelerator magnets
MgB2 wire/cables for power transmission lines is now an established technology. This wire technology is applicable also to low-field magnets
Potentials of MgB2 and iron-based superconductors for higher fields are investigated via dedicated R&D conductor programs
A. Ballarino

## Slide 36: Thanks for your attention !