## Slide 1
Lance Cooley
US Magnet Development Program / US Conductor Development Program
National High Magnetic Field Laboratory / Florida State University
Conductor Procurement, Research, and Development Roadmap
Draft – October 30, 2019

## Slide 2: Mission statement for CPRD
The Conductor Development Program has been active since the mid 1990s --- we have sustained and adapted this program for present needs
Mission 1: Define research opportunities for university, LDRD, and SBIR programs
  This Roadmap should be the important focal point of discussions
Mission 2: Invest in developmental magnet conductors
  Direct procurements of best-effort R&D conductors, typically at 10 kg scale and higher
  Acquisition of emerging conductors by agreement or procurement
Mission 3: Maintain a viable inventory of conductor for foreseen magnet R&D
  Present inventory is low, ~90 kg of long-length Nb3Sn plus ~200 kg short lengths
  100-200 kg procurements of Nb3Sn wire are needed
  20 kg procurements of Bi-2212 are needed

## Slide 3: Status: 27 Aug 2018 Summary to MDP-TAC
Conductor roadmap approved October 17, 2017; Updated August 27, 2018
  Request: dedicated annual set-aside of ~$0.5M for conductor R&D (not incl. procurements)
Nb3Sn baseline: 150/169 RRP at 1.0 mm dia. 3.6:1 Nb:Sn, Ti doped (aka the Hi-Lumi sub-element) with reactions favored at 680 °C to drive up Hirr
    We made a procurement of 90 kg using ECAE niobium
    Hi-Lumi 108/127 RRP at 0.85 mm diameter – spool ends are made available to MDP
Nb3Sn R&D: research opportunities  invest in research billets when ready for 10 kg scale
  HyperTech Research tube-type conductor – pending evaluation for cabling damage
  Fermilab High-Cp conductor – pending next stage development with HTR and B-OST
  APC – both internal oxidized (Zr) and retained cold work (Ta+Hf) – pending next stages and alloy development
Bi-2212: support implementation in magnets
  Present high-Jc conductor is stable (but sole supply), US-based, and configurable
REBCO: monitoring other programs, esp. CORC implementation in CCT
  Tailoring contact resistance and uniformity of very thin conductors are key topics

## Slide 4: TAC and Steering Group Recommendations for CPRD
TAC: Provide a prioritized plan for conductor procurement in potential funding scenarios.
  Renewed MDP roadmaps will define procurement needs
TAC: Continue to leverage SBIR and non-HEP R&D efforts on conductors, and clearly identify synergies that can directly support the 20T HTS roadmap.
  Indeed a variety of funding mechanisms are being pursued on this front.
    Recent Early Career Award of Xinchen Xu (FNAL) provides strong support for Nb3Sn R&D
    CERN is providing support through ASC
    Fusion Energy Sciences (FES) has supported a significant fraction of the C3 REBCO magnet conductor needs.
    Added value from NHMFL/ASC core grant, which supports furnace development, Bi2212 magnet development, REBCO tape characterization, conductor optimization and magnet protection design and analysis
    Many SBIRs
ESG: Provide a prioritized plan for managing a dedicated conductor set-aside
  The plan will emerge from the discussions spurred by these slides

## Slide 5: Conductor Procurement under CPRD
Conductors for procurement are > 2 kg scale (prefer 10 kg), > 100 m (prefer 1km)
R&D conductors are, at present, not “procurement variants” (unlike past CDP actions). Focus is on bringing emerging ideas to fruition
Emerging conductor “threshold”: less than 2 kg, pieces less than 100 m
  Emerging conductors are evaluated continually, engagement is vibrant
    Dramatic advances can bring them into the roadmap when suitable
  Pnictides, no, so far they are being watched …
  Present state of advanced Nb3Sn is just emerging above 2 kg
  REBCO - Present state of CORC “strands” is ~10 m; challenges are apparent

## Slide 6: Challenges for the CPRD Roadmap for the next 5 years
Very dynamic, and much activity is not directly supported by CPRD. How to keep CPRD in the nexus? (Should CPRD be the nexus?)
  CERN: investments in conductor development worldwide
    Also teamed with FSU to support procurement of Nb-Ta-Hf alloys
  Fusion Energy Sciences: re-starting programs with focus on REBCO
  Fermilab Early Career and Laboratory-Directed Research activities
  University R&D grants, synergistic programs at MagLab and elsewhere
  SBIR: Multiple companies have received awards relevant to CPRD
Technical challenges are difficult
  Nb3Sn APC: need to obtain new alloys, demonstrate their ductility, incorporate them in production-like conductors
  Nb3Sn High Cp: same challenges as stated in the bullet above
  Bi-2212: Keep the conductor pipeline full, reduce conductor cost (other suppliers may be emerging)
  REBCO: Identify and confront key aspects required for a magnet conductor

## Slide 7: CPRD Management & Advisory Committee
MDP
CDP / CPRD manager operates under advice from a committee generally composed of members from stakeholder labs
  Present committee: MDP G6 plus J Minervini, E Hellstrom
  Needs: a) balanced MDP representation; b) expertise in all conductor aspects; c) connections to broader conductor activities
  Is a different advisory committee needed?
Decisions have to be made in full awareness of other activities
FNAL
LBNL
BNL
SBIR
STTR
CERN
B-OST, Luvata, SuperPower
CPRD
Topics
Funds
ASC
LDRD
ECRA
Fusion

## Slide 8: Nb3Sn Roadmap: APC and High-Cp development Both RRP and PIT designs are possible
CPRD half billets – optimized
CPRD half billets
10 kg
Industrial pilot – CPRD?
2 kg
University & ECRA
The same general timeline applies to Zr, Ta-Hf, and high-Cp conductors
2020
2021
2022
2023
2024
Get alloys
Demonstrate ductility
Demonstrate reactions
Small restacks
Alloy studies
HT studies
Cabling studies
First coils?
40 kg conductor
40 kg conductor
Conductor
$50k
$200k
$200k
Does CPRD become the curator of new alloys?

## Slide 9: Goal: flexible options for Nb3Sn Not necessary to continue any present path
The conductors that emerge from the roadmap are as likely to be an optimal combination of alternatives as much as an evolution of a present form
2020
2021
2022
2023
2024
High Cp
Oxide APC
CW APC
PIT-like High Cp+APC
RRP-like with both internal oxide and CW options
Does CPRD coordinate the locus of ideas?

## Slide 10: Bi-2212: Stabilize production and encourage cost reduction
The conductor itself is more than adequate for magnets
  US-based powder now better than ever
  Long-length wires (2 km)
  Flexible wire manufacturing
    Multiple architectures
  Insulation technology
  Strengthening approaches
  Rutherford cables
  OP reactions are now reproducible
    Scaling to 1 m L x 0.25 m OD

## Slide 11: Bi-2212: path toward stable, consistent magnet conductor
Consistent orders with same specifications over next ~5 years
Encourage in-line QC and contribute to process diagnostics
2020
2021
2022
2023
2024
CPRD billets
10 kg conductor
$150k
MagLab billets
MagLab billets
Lab coil?
MagLab billets
Lab coil? NMR?
MagLab billets
NMR products??
CPRD billets
20 kg conductor
$240k
CPRD billets
20 kg conductor
$200k
CPRD billets
20 kg conductor
B-OST competitor?
$160k
1 m x 250 mm OD
50-bar oven

## Slide 12: REBCO – mostly conductor on round core (CORC), also symmetric tape round wire (STAR), possibly others…
Opportunities:
  THIN REBCO (now 20 µm) permits winding of ~2 mm diameter “strands” with supposedly isotropic, multifilamentary, current-sharing properties
    Only SuperPower makes thin REBCO; standard thickness is 50 µm  5 mm OD cond.
    Tape current density can be huge, > 2kA/mm2 at 20 T, 4.2 K
    Cables of REBCO “strands” on the horizon?
  Hirr >> 20 T at 20 K  Unique opportunity for outside-the-box magnets
    Remove helium piping from the tunnel, cooling by units built into magnet??
  Leverage advances supported by fusion and electric machines

## Slide 13: REBCO – mostly conductor on round core (CORC), also symmetric tape round wire (STAR), possibly others…
Challenges:
  High cost (but improving?)
  Low production rate (but improving?)
  Wide variation of properties
    Critical current 50% batch to batch from same production line
    Critical current 300% from manufacturer to manufacturer
    Contact resistance varies widely
    Physical variations (dimensions, etc…) and mechanical variations (strength)…
  Limited flexibility
  Conductors come with built-in flaws and damage precursors (e.g. slitting cracks)
  Burnout risk, quench modeling, detection & protection,

## Slide 14: REBCO roadmap: target key advances that will make REBCO a magnet conductor by 2025
Focus on achieving status of “magnet conductor” by retiring key obstacles
  (Opinion: present conductors are not yet there, c.f. Bi-2212 c. 2010 VHFSMC)
Drive toward highly reproducible tapes relative to a spec (what is the spec?)
  Requirements: Shape, copper plating, strength, and yes critical current too
    Understand limits of manufacturing of thin conductors and root causes of variations
    Understand and remove flaws that come along with the conductor
  QC, handling requirements, storage requirements
Put highly reproducible conductors into “strands” of consistent design  do consistent “strands” emerge?
  Contact resistance, current transfer, tension, flexibility…
    Do conductors need to be tinned and soldered?

## Slide 15: Having a conductor inventory also facilitates conductor-level and cable-level investigations (which advise next advances in conductor)
Most of these studies are in core R&D, university programs, etc.
Heat treatment studies (e.g. C. Sanabria), conductor potential
Limiting properties (e.g. Tarantini), identification of alloying opportunities
Fundamental behavior beneath opportunities related to APC and high Cp
Strain-dependent measurements, strain cliff (are there more details?)
Cabling damage (RRR & Ic loss; leakage), and characterization of extracted strands
Transverse stress (cable stacks measured under pressure)
Cable tests
SBIR ideas

## Slide 16: Summary
Priorities
Keep the magnet conductor pipeline full (not drawn from $0.5M set-aside)
  Nb3Sn as needed, which has assistance from AUP remnants
  Bi-2212 needs consistent orders
Leverage conductor advances (CPRD = modest; SBIR + others = big bucks)
  Complement Early Career activities
  Kick in at 10 kg to utilize Nb-Ta-Hf from CERN/ASC
Help REBCO to emerge
  Target specific purchases that advance status toward magnet conductor
Feed conductor-level investigations