## Slide 1: Solenoid training test update
Sofia Jimenez Vinolo, Charlie Sanabria,
M. Marchevsky

## Slide 2: First Prototype
45.47 mm
38.1 mm
a2 = 21.70 mm
a1 = 19.05 mm
Expected number of turns = 20 x 4 = 80
Wire length ≈ 10.24 m
2b = 14.65 mm
Wire + insulation Ø = 0.73 mm
Drawing prepared by
Ray Hafalia
OFHC Cu current leads
Alumina washers
Alumina-coated Stainless steel mandrel
Centering cone (G-10) for testing
Notes: Boron nitride sheets?

## Slide 3: Wire properties and stress calculations
Diameter | 0.6 mm
Non-Cu% | 56.5%
Average RRR | 200
B (T) | Ic (A)
8* | 504
9* | 420
10* | 349
11* | 289
12 | 238
13 | 194
14 | 156
*
Extrapolated using the Pong-Ekin scaling spreadsheet
“Medium Jc” RRP wire critical current (bold values provided by vendor).
“Medium Jc” RRP wire properties
2b = 14.65 mm
a2 = 21.70 mm
a1 = 19.05 mm
B (T) | Stress on OD (MPa) | Stress on ID (MPa)
8 | 177 | 155
9 | 166 | 146
10 | 153 | 134
11 | 140 | 122
12 | 126 | 110
13 | 111 | 97
14 | 96 | 84
Wire purchased by ASC
Notes: Boron nitride sheets?

## Slide 4: Stress calculations at 9 T
Hoop stress
Displacement
ID
OD
146 MPa
172 MPa
2b = 14.65 mm
a2 = 21.70 mm
a1 = 19.05 mm
72.1 µm
Simulations by L. Brouwer
Sliding surface
T
T
|F|= IBRa
a/2
R
a/2
a/2
a
F
F = 2T sin (a/2) ~Ta
T = IBR
B (T) | Stress on OD (MPa) | Stress on ID (MPa)
8 | 177 | 155
9 | 166 | 146
10 | 153 | 134
11 | 140 | 122
12 | 126 | 110
13 | 111 | 97
14 | 96 | 84

## Slide 5: Winding
8 mm x 5 mm mica pieces
Winding speed: ~3.7 RPM
number of turns: 18, 17, 17, 17
No voltage taps between layers
One pair of voltage taps will be added after HT.

## Slide 6: Heat treatment
Standard “Medium Jc” RRP heat treatment.
Recipe:
210°C/48h + 400°C/48h + 570°C/24h + 660°C/50h
Starting date: Friday 8th, 2019
Wrapped with a fiberglass sheet.
Inside tube furnace with flowing argon.
210°C
400°C
570°C
665°C

## Slide 7: Coil potting

## Slide 8: Instrumentation
Acoustic sensor
Quench antennas

## Slide 9: Training
9 T
(81% Iss)
(81% Iss)
8.5 T

## Slide 10: AE r.m.s. amplitude as function of current
Quench #3 (375 A, compression)
The rest of the data to be analyzed…

## Slide 11: Epoxy cracks

## Slide 12: Future steps
Analyze the acoustics
Analyze quench antenna data
Repeat test to see if quench memory is preserved
Build a new coil using and instrument it with multiple Vtaps, acoustic sensors and embedded thermometers