## Slide 1
Lance Cooley
US Magnet Development Program / US Conductor Development Program
National High Magnetic Field Laboratory / Florida State University
Conductor Procurement, Research, and Development Roadmap

## Slide 2: Mission statement for CPRD
The Conductor Development Program has been active since the mid 1990s --- we have sustained and adapted this program for present needs
Mission 1: Define research opportunities for university, LDRD, and SBIR programs
  This Roadmap should be the important focal point of discussions
Mission 2: Invest in developmental magnet conductors
  Direct procurements of best-effort R&D conductors, typically at 10 kg scale and higher
  Acquisition of emerging conductors by agreement or procurement
Mission 3: Maintain a viable inventory of conductor for foreseen magnet R&D
  Present inventory ~90 kg of long-length Nb3Sn plus ~200 kg short lengths
  100-200 kg procurements of Nb3Sn wire are needed
  20 kg procurements of Bi-2212 are needed

## Slide 3: Status: 27 Aug 2018 Summary to MDP-TAC
Conductor roadmap approved October 17, 2017; Updated August 27, 2018
  Request: dedicated annual set-aside of ~$0.5M for conductor R&D (not incl. procurements)
Nb3Sn baseline: 150/169 RRP at 1.0 mm dia. 3.6:1 Nb:Sn, Ti doped (aka the Hi-Lumi sub-element) with reactions favored at 680 °C to drive up Hirr
    We made a procurement of 90 kg using ECAE niobium
    Hi-Lumi 108/127 RRP at 0.85 mm diameter – spool ends are made available to MDP
  HyperTech Research tube-type conductor – pending evaluation for cabling damage
Nb3Sn R&D: research opportunities  CPRD invest in research billets when ready for 10 kg scale
  High-Cp conductor – pending next stage development with HTR and B-OST from FNAL LDRD
  APC – both internal oxidized (Zr) and retained cold work (Ta+Hf) – pending next stages and alloy development
Bi-2212: support implementation in magnets
  Present high-Jc conductor is stable, US-based, and configurable
REBCO: monitoring other programs, esp. CORC implementation.
  Tailoring contact resistance and uniform very thin conductors are key topics

## Slide 4: TAC and Steering Group Recommendations for CPRD And considerations for implementing recommendations
TAC: Provide a prioritized plan for conductor procurement in potential funding scenarios.
  MDP roadmaps and their priorities will define procurement needs for each area
    R&D investments underpin future roadmap stages
TAC: Continue to leverage SBIR and non-HEP R&D efforts on conductors, and clearly identify synergies that can directly support the 20T HTS roadmap.
  Nb3Sn R&D (16 T roadmap) has emerged as a priority, it should not compete with conductor priorities on the 20 T HTS roadmap
  Fusion is driving REBCO production
  High-field magnets outside of HEP define additional research areas for REBCO and Bi-2212
ESG: Provide a prioritized plan for managing a dedicated conductor set-aside
  The context here is a dedicated set-aside for R&D to move emerging conductors forward

## Slide 5: Conductor Procurement and R&D thresholds
Conductors for procurement are > 10 kg scale, > 1 km pieces
  Baseline Nb3Sn conductor mentioned previously: 1 mm OD RRP 150/169 (3 km typ.)
  Bi-2212 has stable 10 kg design, beginning procurement-like QC (2 km typ.)
R&D conductors are, at present, not “procurement variants” (unlike past CDP actions). Focus is on bringing emerging ideas to fruition
Emerging conductor “threshold”: less than 2 kg, pieces less than 100 m
  Emerging conductors are evaluated continually, engagement is vibrant
    Dramatic advances can bring them into the roadmap when suitable

## Slide 6: Challenges for the CPRD Roadmap for the next 5 years
Very dynamic activities, and much activity is not directly supported by CPRD. How to keep CPRD in the nexus?
  CERN: investments in conductor development worldwide (e.g. EuroCirCol)
    Also teamed with FSU to support procurement of Nb-Ta-Hf alloys
  Fusion Energy Sciences: re-starting programs with focus on REBCO
  Fermilab Early Career and Laboratory-Directed Research activities
  University R&D grants
  Synergistic projects at MagLab (e.g. 40T-SC) and elsewhere
  SBIR: Multiple companies have received awards relevant to CPRD
Technical challenges are difficult, progress will be slow, support must be sustained
Conductors are expensive; mileage for investment dollar is low

## Slide 7: CPRD Management & Advisory Committee
MDP
CPRD advisory
CDP / CPRD manager operates under advice from a committee generally composed of members from stakeholder labs
  Present committee: MDP G6 plus J Minervini, E Hellstrom
  Needs: a) balanced MDP representation; b) expertise in all conductor aspects; c) connections to broader conductor activities
  Charge: establish and prioritize conductors under R&D set-aside
  Method: proposals solicited from companies
Decisions have to be made in full awareness of other activities
FNAL
LBNL
BNL
SBIR
STTR
CERN
B-OST, Luvata, SuperPower
CPRD
Topics
Funds
ASC
LDRD
ECRA
Fusion

## Slide 8: Nb3Sn Threats and Opportunities
Opportunity: 30% to 100% more pinning at high field, maybe also tolerant of training
  The microstructures for both oxide particle doped material and Hf grain-refined material are different than that of the present RRP baseline; these are gains rooted at the fundamental level for flux pinning
Threat: HTS
  Is there enough time and resources to develop alloys and manufacturing processes before HTS steals the show?
X Xu et al.

## Slide 9: Nb3Sn Roadmap: APC and High-Cp development Both RRP and PIT designs are possible
CPRD half billets – optimized
CPRD half billets
10 kg
Industrial pilot – CPRD?
2 kg
University & ECRA
The same general timeline applies to Zr, Ta-Hf, and high-Cp conductors
2020
2021
2022
2023
2024
Get alloys
Demonstrate ductility
Demonstrate reactions
Small restacks
Alloy studies
HT studies
Cabling studies
First coils?
40 kg conductor
40 kg conductor
Conductor
CPRD could become the curator of new alloys until stable production

## Slide 10: Goal: flexible options for Nb3Sn Not necessary to continue any present path
The conductors that emerge from the roadmap are as likely to be an optimal combination of alternatives as much as an evolution of a present form
2020
2021
2022
2023
2024
High Cp
Oxide APC
CW APC
PIT-like High Cp+APC
RRP-like with both internal oxide and CW options
CPRD should coordinate the locus of ideas

## Slide 11: Bi-2212: Get conductor into magnets
Opportunity: Conductor current density has continued to increase, yet we are still only realizing <1% of theoretical limit
  Continued powder development (A Xu –SBIR; Jiang, Hellstrom)
Challenge: Getting Coil reactions to utilize as much of the available Ic as possible
  Make coils to understand OP HT needs
    Higher Jc powder? Mix / grade?
    Broaden the window?
Threats: 1) cost; 2) Sole supply, will Bruker act to protect its REBCO-based NMR magnets?
Peter Lee - NHMFL

## Slide 12: Bi-2212: path toward stable, consistent magnet conductor
Consistent orders over next ~5 years, drive down costs, inject improvements when opportunities present
Encourage in-line QC and contribute to process diagnostics
Competition is emerging (A Otto – SBIR; WST showed conductor at MT-26)
2020
2021
2022
2023
2024
CPRD billets
10 kg conductor
MagLab billets
MagLab billets
Lab coil? Cryomag. STTR
MagLab billets
Lab coil? NMR?
MagLab billets
NMR products??
CPRD billets
20 kg conductor
CPRD billets
20 kg conductor
CPRD billets
20 kg conductor
B-OST competitor?
1 m x 250 mm OD
50-bar oven

## Slide 13: REBCO – mostly conductor on round core (CORC), also symmetric tape round wire (STAR), possibly others…
Opportunities:
  THIN REBCO (now 20 µm) permits winding of ~2 mm diameter “strands” with isotropic, multifilamentary, current-sharing properties
    Tape current density can be huge, > 2 kA/mm2 at 20 T, 4.2 K  high winding current density possible with CORC
    Cables of REBCO “strands” on the horizon?
  Hirr >> 20 T at 20 K  Unique opportunity for outside-the-box magnets
    Leverage advances supported by fusion and electric machines
    Remove helium piping from the tunnel, cooling by units built into magnet??

## Slide 14: REBCO – mostly conductor on round core (CORC), also symmetric tape round wire (STAR), possibly others…
Threats:
  Only SuperPower makes REBCO on 20-25 µm thick Hastelloy, slit @ 1 to 2 mm widths
  Expensive
Unknowns and Challenges:
  Flaws come with the conductor, implications for I-REBCO (e.g. 32 T) and NI-REBCO are being learned, usually the “hard way”. What happens in CORC? What are the flaws that need attention and development of circumventions?
  Splices in CORC and other cables? Production length is ~200 m…
  Can cables tolerate Ic drop-outs, including those that occur due to strain in operation?
  Contact resistance and uniform cross-section shape – what controls current sharing?
  What is the appropriate level to engage with REBCO? There is enough work to fill a large conductor research program now that magnet technology is blooming

## Slide 15: REBCO – Roadmap
Focus on achieving status of “magnet conductor” by retiring key obstacles by 2024, in no particular order
  c.f. Bi-2212 c. 2010 VHFSMC
Potential areas for CPRD investment:
  Cost reduction, production (rate, length) increase
  Isotropic pinning additives (Y2O3 instead of BZO)
  Reduction of property and shape variations
  Slitting for very thin conductors
  Tailoring of contact resistance, control of handling and environmental factors
  Property grading
  Innovative cable designs, e.g. strengthened core

## Slide 16: Having a conductor inventory also facilitates conductor-level and cable-level investigations (which advise next advances in conductor)
Most of these studies are in core R&D, university programs, etc.
Heat treatment studies (e.g. C. Sanabria), conductor potential
Limiting properties (e.g. Tarantini), identification of alloying opportunities
Fundamental behavior beneath opportunities related to APC and high Cp
Strain-dependent measurements, strain cliff (are there more details?)
Cabling damage (RRR & Ic loss; leakage), and characterization of extracted strands
Transverse stress (cable stacks measured under pressure)
Cable tests
SBIR ideas

## Slide 17: Cost reduction comes with magnet pull
Nb-Ti went from $16/m when current density was 1500 A/mm2 …
to $1/m when current density reached 3000 A/mm2 and magnet demand drove production from ~1 ton per year to 200 tons per year
Nb3Sn: presently few ton per year, but not yet engaged with medical magnets
Will 2212 soon engage with NMR now that Jc is so high?
Will REBCO engage broadly now that magnet technology is blooming?

## Slide 18: CPRD “standard” funding scenario
Keep the Nb3Sn magnet conductor and Bi-2212 magnet conductor pipelines full
  100 kg Nb3Sn annual, $250k
  20 kg Bi-2212 annual, $250k
Make targeted investments in emerging ideas, balanced across portfolio, per discussion and input from the CPRD Advisory Committee
  $250k to $500k annual
  Balanced portfolio: Nb3Sn, Bi-2212, REBCO
  Sustain existing development teams at e.g. Bruker-OST
Total: $1M annual set-aside

## Slide 19: Go Big
We are in a short period where rosy funding scenarios are playing out
  AIP FYI: all P5 project opportunities have been enacted. The “re-baseline” of accelerator R&D from 25% to 18% of program can be reversed.
What can we do with a significant boost?
  Challenge: some things take time, e.g. 12-18 months from alloy order to delivery
    3 years for alloy order to wire R&D order to delivery
  Stockpile conductor to respond to boosted MDP
  Commit raw materials orders, stockpile monofilament of Nb4Ta2Hf and Engimat run 56
  Accelerate getting advanced Nb3Sn into cables and magnets
  Drive competition for cost reduction: Luvata Nb3Sn, alternative Bi-2212 mfg.
  Reduce the need for OP HT for Bi-2212 – remove / reduce bubble sources
  Fund a suite of linked REBCO projects coordinated by a common cable design
    Material for 20 m, 30 conductor CORC solenoids
    32T, 40TSC, LBC projects reveal that REBCO still poses many unknowns for magnets

## Slide 20: Go Bigger and Longer
Nb3Sn RRP will inevitably remain a double-stack  difficult to scale beyond 100 kg without innovation “skunk works” (e.g. cranes in clean restack rooms)
  Mono  sub-element  conductor
ITER style Nb-Ta-Hf is single stack at scale and could be interesting
Nb3Sn PIT is single stack, but continues to have challenges intrinsic to cabling deformation, which subtract 15% or more of Jc  flattened conductors in novel cabling?
Bi-2212 could be a large single-stack billet  possible scale to 400 kg billet? Extrudable
  Long-term cost reduction  $2000/kg (Nb3Sn price): larger scale offsets $$ material
REBCO has cheap raw materials  Will vendors scale to very wide (> 100 mm) foils and very long production lengths?
30-year manufacturing without industry pull  MDP-supported Conductor Institute, aka “skunk works”?
  Ohio State - HTR model? NHMFL-ASC wire shop expansion? NETL Albany partnership?

## Slide 21: Summary
Priorities
Keep the magnet conductor pipeline full
  Nb3Sn as needed, which has assistance from AUP remnants
  Bi-2212 needs consistent orders
Leverage conductor advances, keeping all activities in view
  Complement Early Career activities
  Kick in at 10 kg to utilize Nb-Ta-Hf from CERN/ASC
  Inject other advances as they emerge, e.g. High-Cp, new Bi-2212 powder
Help REBCO to emerge
  Target specific purchases that advance status toward magnet conductor
Supply conductor for basic investigations