## Slide 1: DOE GARD Review of the U.S. Magnet Development Program
Review Closeout
Summary of Preliminary Findings and Comments
Review Committee:
Ruben Fair (Jlab) Andy Lankford (UCI, Chair), Pierre Vedrine (CEA Saclay)

## Slide 2: Nb3Sn Magnet Development
Cos-theta – MDPCTl - quality and impact of the recent scientific achievements
The goals of the first test have been achieved
Some accomplishments
  Bmax = 14.10±0.04 T - a record field at 4.5 K for accelerator magnets
  Graded 4-layer coil design.
  Innovative support structure and magnet fabrication procedure have been developed and tested.
Findings from the recent tests:
  Better understanding of how to improve stress management
  Improved definition of acceptable design stress limits
  Better understanding of the use of diagnostics and the exchange of information and techniques between LBNL and FNAL
The quality and significance of the recent test is high
  as demonstrated by the achieved goals and findings described above.
  as attested by comments of international workshop participants, including:
    Achieved performance gives significant credibility to the FCC target of 16 T.

## Slide 3: Nb3Sn Magnet Development
Cos-theta – MDPCTl - merit, feasibility and impact of the future test plan
The test plans for the immediate future for this magnet, to achieve 15 T, are logical and should provide additional valuable information to improve stress management techniques and to understand quench initiating mechanisms.
The future steps in stress-managed cos-theta are logical and define a valuable line of investigation. It is the first investigation of stress management in cos-theta magnets. However, the full plan is overly ambitious for the coming three to four years, particularly considering that this thrust of MDP must be prioritized against other activities within budget constraints. Funding allowing, it is desirable to accomplish the goals of tasks 2 and 3 within the coming years. Task 5 seems beyond the scope. MDP could consider whether to progress through task 2 on the way to task 3 or whether to move directly to task 3, including cost in these considerations.
The schedule presented from 2020 to 2023 is certainly ambitious but also very aggressive bearing in mind the challenges still to be overcome.

## Slide 4: Nb3Sn Magnet Development
CCT - quality and impact of the recent scientific achievements
The progress in understanding CCT coil configuration has been systematic.
Findings from recent tests:
  Some improvement of early training – change of epoxy mix and interface conditions
  Good use of acoustic emission sensors and development of effective data interrogation methods to understand observed training.
  Better understanding that observed training is due to force and not short sample limit
  Better understanding of how to improve stress management
The quality and significance of the recent test is high as demonstrated by the findings outlined above.

## Slide 5: Nb3Sn Magnet Development
CCT - merit, feasibility and impact of the future test plan
The next steps for this magnet transition to a subscale program for CCT and target specific areas for further investigation, such as:
  Testing of epoxies and interfaces
  Mandrel deformation during heat treatment
  Test of assembly methods
  Test of new instrumentation methods
We agree that this is a sensible approach for the Nb3Sn CCT magnet program.

## Slide 6: Nb3Sn Conductor Development
Recent significant advances in conductor have been accomplished:
Controlling grain size, two techniques
  APC via oxidation – have reached FCC Jc goal in research samples
  Hf – shows potential to reach FCC goal
Eliminated an important constraint on Nb3Sn performance
Impact recognized by interest of the international community
Significant further work is necessary to turn this R&D into magnet conductors.
It was noted by the international workshop that improvements are also desirable in Nb3Sn conductor parameters other than Jc, particularly considering the high Jc now being achieved.

## Slide 7: HTS Magnet Development
Quality and impact of the recent scientific achievements
REBCO
  Good, steady progress on magnets
  MDP seems to be leading REBCO dipole development
Bi2212
  MDP has driven significant performance improvements in conductor
  MDP has achieved record performance in racetrack coils
  Bi2212 is attractive in that it may yield quench-free magnets

## Slide 8: HTS Magnet Development
Merit, feasibility and impact of the future test plan
Committee supports the stepwise approach being followed with both conductors, and supports parallel investigations of both conductors.
The rate of progress has been limited by conductor availability. It would be desirable to fund additional conductor procurement, within an overall balanced MDP program.
Progress on HTS magnets depends upon progress on HTS conductor development. Progress on conductors is currently being accomplished outside MDP. MDP should continue to take advantage of this outside work and maintaining collaborations with university and other efforts. It would be desirable for MDP to foster further conductor development via investment in industry.

## Slide 9: Strategic Planning
Soundness and feasibility of the draft updated roadmap
The strategic plan is described in terms of a “roadmap”.
  It is a comprehensive strategic plan identifying and defining the necessary steps for the next 4-5 years in R&D to provide high-field dipoles for the next-generation very high-energy proton-proton collider.
  The strategic plan reflects a broad perspective on the challenges of high-field magnet R&D and extensive discussion of program optimization.
As a draft, this roadmap does not yet describe a strategic plan that can be accomplished on the timescale outlined within present budget levels, and probably not within foreseeable budgets.
  The elements of the plan need to be prioritized to a degree that can guide budget discussions with the agency.
    These discussions do not require a rank ordering of all program elements.
    Rather, identification of the highest priority elements, along with their budget needs, is needed.

## Slide 10: Strategic Planning
Some further comments:
The long-range and ambitious goals of MDP are appropriate to the GARD program.
The 4-5 year time horizon of the roadmap is appropriate.
  MDP should also maintain the long-term vision laid out in its program goals and its list of 10 driving questions.
At this point, maintaining LTS & HTS parallel R&D paths is critically important.
  We do not know the optimum solution within the multiparameter space. It is premature to choose a preferred path.
  Pursuing LTS and HTS R&D in parallel is within MDP capabilities.
It appears that the roadmap is missing an R&D line on measuring mechanical properties of cables and coils in order to better understand these issues.
The committee encourages MDP to continue to feedback their test results into their modeling and to continue to share their modeling with the rest of the community.
How the many R&D threads come together to inform future steps is not made clear in the roadmap.
The international context in which MDP exists is likely to become somewhat better defined by the report of the European Strategy for Particle Physics Update in early 2020.

## Slide 11: Strategic Planning
Some more further comments:
Collaborative work with CERN on development of test facilities is a positive development, particularly because the High-Field Vertical Magnet Test Facility is much needed by MDP. MDP should work closely with CERN in designing and realizing this facility.
In its planning, MDP considers how to leverage, particularly in the conductor area, R&D in other fields and for other applications. Recent collaboration with FES has provided the opportunity for a much needed high-field vertical test facility.
The strategic plan reflects thoughtful consideration of existing infrastructure and expertise. Moreover, the strategic plan does not restrict itself to R&D activities for which there is existing expertise. Rather it includes priority R&D activities that demand development of important new expertise.
The R&D activities called for in the draft MDP strategic plan, are more complementary to international activities and plans than they are duplicative.
  In fact, when activities appear to be duplicative, they can be seen as largely complementary when viewed more closely.

## Slide 12: Strategic Planning
Some more further comments:
MDP cannot be a fully comprehensive R&D program. For this reason, its strategic plan need not be comprehensive; however, it would be valuable to explicitly account for R&D lines covered by others, particularly by university groups and by international collaborators. (stop here?) Such accounting would help guide worldwide efforts towards a complete global roadmap.

## Slide 13: Management
MDP Management has demonstrated its effectiveness in strategic planning and in implementing a prioritized and optimized program.
Effectiveness of strategic planning
  MDP is at a point in time at which its original roadmap is well advanced and it has assembled a draft roadmap for the coming years.
  The strategic plan of the original roadmap formulated by MDP Mgmt, at the time MDP was established, successfully guided MDP to the significant accomplishments achieved to date.
  The new draft roadmap for the coming years assembled by MDP Mgmt outlines a comprehensive high-field magnet development program.
      It reflects extensive, thoughtful discussion of the needed R&D directions and the best way to accomplish that R&D.

## Slide 14: Management
Effectiveness of implementing a prioritized and optimized program
  MDP Mgmt was effective in establishing a successful R&D program.
  It has also been effective in implementing its strategic plan, as demonstrated by the important accomplishments in each of its thrusts.
  Resource utilization:
    In the context of this review/international workshop, it is difficult to evaluate in detail the effectiveness of resource utilization.
    There is clear evidence of consideration of existing infrastructure and expertise.
    There is no obvious evidence of ineffective or inefficient use of resources.
The interactions among the laboratories appear to be working relatively well, and the laboratories’ managements appear to support and provide resources to the program.
We encourage continued growth in the interactions between individuals from the different laboratories.

## Slide 15: Collaborations
MDP has established numerous collaborations that enhance its effectiveness.
The international workshop in which this review was embedded demonstrated benefits of interactions with R&D programs outside MDP.
A subject to be considered is how MDP could enhance its progress and effectiveness by increased interactions with R&D activities outside MDP, at other US institutions and at institutions abroad.
  The committee does not prejudge the degree or frequency of interaction,
    for instance whether interaction is through workshops, international discussions of a worldwide R&D strategic plan, further collaborations, coordination of programs, etc.
  In the spirit of the international workshop in which this review was embedded, MDP should consider how international experts can help identify, develop, and optimize the required R&D activities.