## Slide 1
Reed Teyber, Maxim Marchevsky, Soren Prestemon - LBNL
Jeremy Weiss, Danko van der Laan – ACT LLC
CableTerminations with Integrated Hall Arrays for Quench Detection

## Slide 2: Motivation
Normal zone detection in HTS cables remains an active area of R&D
In Fusion reactors, coils can operate with fast ramp rates
  Detection problems exacerbated
Seek a non-invasive (outside of reactor), real-time quench detection system
  Supplement voltage measurements

## Slide 3: Motivation
Previous paper by Maxim uses Hall sensors to detect quench in slit ReBCO tape
  “Quench detection method for 2G HTS wire. SUST, 23(3):034016, March 2010“
Monitor current redistribution in terminal using Hall sensor array as proxy for quench detection
  Exploit low current sharing and layered terminal topology in
  Layer quench manifests as axial shift in terminal current
  SBIR with Maxim/LBNL and ACT

## Slide 4: Methods
Experimental setup
  8 layer (16 tapes), ~ 1.2 kA @ 77 K
  PCB with 29 GaAs Hall sensors
  Heater and PM induced magnet quenches
Static and fast-ramped current
  Up to 10 kA/s

## Slide 5: Methods
Experimental procedure
  Ramp current to desired value, turn on heater to induce quench
  Plot change in sensor value (subtract baseline measurement)
Heater
Blue: sensor 0 (inner terminal)
Red: sensor 29 (outer terminal)
Baseline
Current redistribution

## Slide 6: Static quenches
Static current, heater induced quench
  Contours show change in Hall sensor response
  Right y-axis shows sample voltage
Spatial frequencies to consider
  Layer to layer: ~10 sensors
  Twist-pitch: ~3 sensors
  Tape-to-tape: ~1 sensor
Response dominated by global increase in field
  Fits simple model on previous slide
  Periodic, wave-like normal zone propagation at 700 A
    Originating at terminal outside
    Not at helix twist-pitch length scales
  Smaller variations observed on layer-to-layer scale (~10 sensors), as observed at 1000 A
Outer term.
“CORC-side”

## Slide 7: Static quenches
Terminal Hall sensors can be used for real-time quench detection
  Similar magnitude and temporal response as sample voltage

## Slide 8: Dynamic quenches
Explore feasibility of terminal Hall sensor for quench detection in ramped Fusion magnets
  Ramp rates of 1 kA/s, 5 kA/s and 10 kA/s
  Sorenson SGA 10/1200 PSU programmed with PyVISA
  Magnet-induced (left) and heater-induced (right) results
With fast ramps (1-10 kA/s), small variations in tape inductances yield inductive voltage distribution
Non-dimensional time

## Slide 9: Dynamic quenches
Raw Hall sensor signals demonstrate hysteresis loop over current excursion
  Shielding currents induced in copper terminals
Contours show change in Hall sensor plot between no-quench experiment and quench experiment

## Slide 10: Dynamic quenches
Heater induced
Magnet induced
1 kA/s
5 kA/s
10 kA/s

## Slide 11: Discussion
Implementation is ex-situ, and can be implemented with low-cost Hall sensors
Promising quench detection method to supplement voltage measurements
  Real-time quench detection is more challenging with fast ramps, ongoing work
Promising tool to study dynamics
  Small changes in experimental parameters yield large changes in measured results
  Would be helpful to know tape structure in terminal (industrial CT (Xiaorong), inverse Biot-savart optimization from Hall scan)
  Higher current quench experiments (i.e. 4K) would increase SNR, potentially helping resolve tape-level current redistribution

## Slide 12
Extra Slides

## Slide 13: Ramped Quench detection