## Slide 1
Ramesh Gupta
For Superconducting Magnet Division
Brookhaven National Laboratory
Preliminary Results of the HTS/LTS Hybrid Dipole Test
MDP Video meeting on February 19, 2020

## Slide 2: Contributions from
Work presented here and the work being performed now is thanks to many individuals, including:
    Bill Sampson, Shresht Joshi, Anis Ben Yahia, Piyush Joshi, Bill McKeon, Sonny Dimaiuta, Denny Sullivan, Peter Galioto, Pat Doutney, Mike Anerella, John Cozzolino, Ray Ceruti, …

## Slide 3: Fixture inside the magnet
Fixture inside the common coil dipole
HTS coils and samples inside
HTS/LTS Hybrid Dipole
Zoo of leads

## Slide 4: Run Plan for Magnetization Studies (almost everything planned in this slide done, perhaps not always be in the order planned)

## Slide 5: Test Run at 4 K in HTS/LTS Hybrid Dipole (~2 T background field from Nb3Sn coils)
Additional field from the HTS coils in up and down ramp
(offset to start from zero to start up-ramp)
Field perpendicular (2016 SBIR)
Field parallel (2019 MDP)
Field parallel (2019 MDP)
Significant reduction in magnetization from HTS coils when field is primarily parallel to the wide face when compared to primarily perpendicular

## Slide 6: 4 K run – No background field
Magnetization measurement were done prior to this test up current up to 500A at higher temperatures

## Slide 7: 4 K Magnetization Run in Background Field (background field subtracted)

## Slide 8: Quench Protection of HTS/LTS Hybrid Dipole

## Slide 9: Cutout View for Nb3Sn coils at 10 kA and HTS coils at 1 kA (with Nomex insulation and No-insulation)
13.9 T
HTS coils are installed with as low clearances. Horizontal Lorentz forces brings them in contact with the LTS coils

## Slide 10: ANSYS Run Transverse Stress and Strain from Nb3Sn 10 kA, HTS 1 kA
LTS Coils

## Slide 11: Insulated Coil Powered with the common coil (field in NI coil: Nb3Sn field + trapped field)
Nb3Sn coil quenched

## Slide 12: HTS Coil was ramped to the maximum of PS after the quench to check damage from the quench
Nb3Sn coil quenched

## Slide 13: Field and Current Decay (coupling studies)
Field Decay
(quench @ t=0)
Current Decay

## Slide 14: Planned Quenches
All quenches in LTS coils.
HTS coils seems to tolerate quenches from Nb3Sn coils (large energy transfer)

## Slide 15: Extra slides

## Slide 16: HTS Coil in 2 T Field (primarily parallel to the wide face) NI COIL

## Slide 17: HTS Coil in 2 T Field (primarily parallel to the wide face) INSULATED COIL

## Slide 18: 2016 Test (Field Perpendicular)
Chart: Hybrid Dipole Field (T)
| 5.477777777777777 | 6.79
 | 0 | 756
 | 0 | 741
 | 0 | 712
 | 0 | 682
 | 0 | 656
 | 0 | 800
 | 0 | 500
 | 0 | 635
 | 0 | 500
 | 0 | 500
 | 0 | 500
 | 0 | 500
HTS coils with ASC tape
Field primarily perpendicular to the wide side of the tape
HTS coils were ramped to quench, just like LTS coils
No measurable degradation found
Test limited by the current leads of LTS coil

## Slide 19: Feedback of Quenching of HTS Coils on LTS Coils in HTS/LTS Hybrid Magnet (2016)
What happens to HTS coils if LTS coil quench?
Coupling between the HTS & LTS coils