## Slide 1
Paolo Ferracin, Giorgio Ambrosio, Lance Cooley, Ramesh Gupta, Vadim Kashikhin, Alexander Zlobin
US Magnet Development Program
MDP Meeting on
Comparative analysis of magnet design concepts

## Slide 2: Outline
What was presented at the collaboration meeting (in brief)
  Three tasks
Status and plan

## Slide 3: Proposed design studies roadmap
Title: Design studies of LTS/HTS hybrid magnets
  Focus on design of
    Outer (background) coils based on Nb3Sn superconductor
    Inserts based on
      Both with REBCO and Bi2212 superconductors
    Hybrid magnets towards 20 T field level

## Slide 4: Proposed design studies roadmap
Time frame: 2020 – 2023
Methods
  Modeling effort
    “classical 2D/3D” mechanical, magnetic and QH simulations
      Developing new modeling techniques is not part of this task
      However, if new tool/analysis is required  feed-back to Technology area (III), modeling and simulations

## Slide 5: Hybrid program and goals of the design studies (I)
Hybrid program
  “Near term” (~2020-2022)
    CCT5
      8 T in 90 mm aperture
    CCT Bi2212 BIN5 and/or some inner coils from the CCT REBCO C2
      1-2 T field level
    Target hybrid field: ~ 9 T
Goals of the design studies
  Start analysis of challenges specifically of hybrid magnets
    Integration of LTS/HTS, mechanics, protection, powering, diagnostics, test facility…..

## Slide 6: Hybrid program and goals of the design studies (II)
Hybrid program
  “Medium term” (~2022-2024)
    CCT6 and/or SMCT
      11-12 T in 120 mm aperture
    CCT Bi2212 and/or SMCT Bi2212 and/or CCT REBCO and/or COMB REBCO
      Towards 5 T field level
    Target hybrid field: towards 14-15 T
Goals of the design studies
  Evaluate different designs (both LTS and HTS)
  Investigate alternatives (common-coil and blocks)
  Perform a comparative analysis in view of a 20 T hybrid magnet, considering both modelling and experimental results
    Margin, mechanics, field quality, quench protection strategies, fabrication-assembly-loading, performance of previous models, scalability, cost……
    Basically, help converging on all the and/or
  Continue the analysis of challenges specifically of hybrid magnets

## Slide 7: Hybrid program and goals of the design studies (III)
Hybrid program
  “Long term” (~2025 and beyond)
    Target hybrid field: towards 20 T
Goals of the design studies
  How much field from LTS and HTS respectively?
  Which design? How a 20T hybrid may it look like?
  Evaluation high Jc limitations in Nb3Sn
    We are working on very high Jc strands: can we afford it?
      Yes from the stress point of view (CCT and SMCT), but what about QP?

## Slide 8: Outline
What was presented at the collaboration meeting (in brief)
  Three tasks
Status and plan

## Slide 9: Status and plans task 1
Hybrid I
  Bi2212 insert (1-2 T) in CCT5 (8-9 T)

## Slide 10: Status and plans task 1
Hybrid I
  Bi2212 insert (1-2 T) in CCT5 (8-9 T)
Weekly meeting on upgrade of LBNL test facility for hybrid testing
  In that meeting, discussion on interface insert-CCT
    CAD model of FRESCA2-feather received from CERN to check locking system
      Work in progress
Weekly meeting on CCT activities
  Initiated discussion on Bi2212 support structure
    Al or SS shell thickness? Self-supported (most likely) ? Contact between layers and shells
      Never tested before in a 8 T background field
    2D analysis in progress

## Slide 11: An example of the interface insert-outsert

## Slide 12: Status and plans task 2
Hybrid II
  Bi2212/REBCO insert (5 T) in Nb3Sn outsert (~11 T) with 120 mm bore
  Outsert currently under study
    CCT6
    SMCT

## Slide 13: Hybrid II Bi2212/REBCO insert (5 T) in Nb3Sn outsert (~11 T)
Weekly meeting on CCT activities
  Initiated review of CCT6 design
    Which strand/cable? Which spar and ribs (feedback from subscale coils)? Which support structure? Which pre-stress?
    Modelling in progress

## Slide 14: Hybrid II Bi2212/REBCO insert (5 T) in Nb3Sn outsert (~11 T)
Comparative analysis
  How a 11 T, 120 mm aperture design with cos- or block or common coils may look like?
  Preliminary criteria for comparison

## Slide 15: Hybrid II Bi2212/REBCO insert (5 T) in Nb3Sn outsert (~11 T)
Some thoughts on cos-
  From 60 mm (11T magnet) to 120 mm
    Forces linearly increased with aperture
    From 110 to 220 Mpa of Lorentz stresses  even higher peak stresses
  Stress management required
  However….

## Slide 16: Hybrid II Bi2212/REBCO insert (5 T) in Nb3Sn outsert (~11 T)
Some thoughts on cos-
  Still interesting to check FCC design
    Also in that case twice the forces as 11T magnet
Force quadratically increase with field
  16 T to 11 T 
    ~ factor 2 reduction
  60 to 120 mm 
    ~ factor 2 increase
Larger cable?

## Slide 17: Hybrid II Bi2212/REBCO insert (5 T) in Nb3Sn outsert (~11 T)
Some thoughts on cos-
  In parallel, comparative analysis between CCT and SMCT

## Slide 18: Hybrid II Bi2212/REBCO insert (5 T) in Nb3Sn outsert (~11 T)
Some thoughts on block
  FRESCA2 (reached 14.6 T)
    13-15 T in 100 mm bore
    1 mm strand, 40 strand cables
    ~21 mm cable
  Is it conceivable a wider cable, for a 120 mm bore and an 11 T target field?

## Slide 19: Hybrid II Bi2212/REBCO insert (5 T) in Nb3Sn outsert (~11 T)
Some thoughts on common-coil
  So far, apertures for accelerator magnets (small)
  How a 120 mm aperture common coil magnet would look like?
    Like the outsert of a 16 T magnet?

## Slide 20: Hybrid II Bi2212/REBCO insert (5 T) in Nb3Sn outsert (~11 T)
Preliminary criteria for comparison
  Strand/cable design
  Efficiency (quantity of conductor)
  Coil parts
  Coil ends
  Winding
  Coil fabrication tooling (W-C-R-I)
  Lorentz stress / Peak stress
  Assembly-loading
  Support structure
  Scale-up
  Quench protection
Strong/easy
Medium
Weak/difficult

## Slide 21: Also, later….
Hybrid II
  Bi2212/REBCO insert (5 T) in Nb3Sn outsert (~11 T)
    Comparative analysis of insert design
Hybrid III
  Hybrid magnets towards 20 T field level
    Conceptual design
      Review of CERN activities

## Slide 22
Finally, if there is time…..

## Slide 23: FRESCA2c magnetic model standalone
Electric current from the standalone testing perfomed in 2018 at 4.3 K
          11.3 kA meaning an I/Iss ratio of 0.83
          Bore field (B(0.0,0.0)) of 13.4 T
14/03/19 - D. Martins Araujo

## Slide 24: FRESCA2c magnetic model standalone
Max B field on coils
          Outer coil: 13.21 T (80% SS)
          Inner coil: 13.73 T (83%)
Outer
coil
Inner
coil
14/03/19 - D. Martins Araujo

## Slide 25: Case 1 of integration - magnetic model
Electric current of 11.7 kA on FRESCA to have I/Iss = 0.83 at 4.3 K considering 10 kA for FM2:
          Bore field (B(0.0,0.0)) of 17.48 T
14/03/19 - D. Martins Araujo

## Slide 26: Case 1 of integration - magnetic model
Electric current of 11.7 kA on FRESCA to have I/Iss = 0.83 at 4.3 K considering 10 kA for FM2:
          Bore field (B(0.0,0.0)) of 17.48 T
14/03/19 - D. Martins Araujo

## Slide 27: Appendix

## Slide 28: Hybrid program and goals of the design studies (II)
Then, some personal thoughts on the comparative analysis….
    The goal should not be, or does not necessarily have to be
      reaching a consensus on a particular design
        ….historically, as far as I know, this goas has never been achieved before…
    Instead, more realistically, the working group could aim at
      Discussing and reviewing the different designs and listing pluses and minuses or open issues….grounding on “objective” criteria
      Providing inputs to the other areas (in particular area I and area II) to better define their roadmaps and overall directions, and avoid inconsistencies

## Slide 29: An example of comparative analysis from FCC/Eurocircol
Magnets at the limits of Nb3Sn superconductor
Based simply on modelling, the selection is very difficult
  Better if we rely also on experimental data

## Slide 30: Resources needed and possible timeline
Resources
  1.5 Post-Doc full time (0.5 per lab)
  0.5 FTEy for supervision and biweekly meeting of the working group
Timeframes and goals
  About 3-4 years in total
  First six months (by Sept. 2020)
    Review of work so far, by MDP and internationally (FCC/Eurocircol)
      Nb3Sn dipole magnets, HTS inserts, 15-20 T hybrid magnets
    Definition of a list of criteria and preliminary evaluation of MDP designs and/or proposed alternatives, always from the hybrid perspective
    Perform analysis in support of the test of the first hybrid magnet (9-10 T) with CCT5
  First year (by March 2021)
    Design study of second hybrid magnet (14-15 T)
      Based on CCT, SMCT and HTS development results and first hybrid test with CCT5
  Final goal
    Design study of a 20 T hybrid

## Slide 31: An example of the hybrid challenges
FRESCA2 and Feather2
  13-14 T + 3-5 T
  work in progress at CERN
Significant challenges in mechanical integration
  Self supporting insert or in contact with LTS

## Slide 32: An example of the hybrid challenges

## Slide 33: Show how the proposed roadmap builds off of MDP and international efforts to-date
Magnets at the limits of Nb3Sn superconductor
  Eurocircol/FCC design studies: margin

## Slide 34: Show how the proposed roadmap builds off of MDP and international efforts to-date
Magnets at the limits of Nb3Sn superconductor
  Eurocircle/FCC design studies: Jc

## Slide 35: Show how the proposed roadmap builds off of MDP and international efforts to-date
Magnets at the limits of Nb3Sn superconductor
  Eurocircle/FCC design studies: quantity of superconductor
No show-stoppers found in any particular design
  Peak stress <150 MPa at warm and <200 MPa at cold
No final selection (although CT as baseline)final choice