## Slide 1: MDP General Meeting 20 T hybrid magnet and comparative analysis
P. Ferracin, G. Ambrosio, E. Barzi, L. Cooley, R. Gupta, V. Kashikhin, V. Marinozzi, I. Novitski, B. Yahia, A. Zlobin
US Magnet Development Program

## Slide 2: Outline
Definition of the goals of the working group
Design criteria for a 20 T hybrid magnet
Some preliminary estimates of radiuses and dimensions
Overview of current hybrid work
Conclusions and action items

## Slide 3: 1st goal of the working group
Conceptual design of a 20 T hybrid HTS-LTS magnet
  Comparative analysis of different design options for a 20 T hybrid
    Cos design and its stress-management options
      “Traditional” Cos
      Canted Cos (CCT)
      Stress management Cos (SMCT)
    Block-type coil design (block with flared ends)
    Common-coil design (block with racetrack coil)
  Definition of general design criteria: aperture, field, margin…..
  Analysis of challenges specifically of hybrid magnets
    Integration of LTS/HTS, mechanics, protection, powering, diagnostics, test facility…..

## Slide 4: 1st goal of the working group
An example: 16 T dipole magnets for FCC
Ideally the goal should be to carried out the full 2D design and analysis of a 20 T hybrid for all the design options considered
    Cos design and its stress-management options, Block-type design, Common-coil design
In addition, 3D considerations will be included in the comparison

## Slide 5: 1st goal of the working group
The goal of the comparison should not be, or does not necessarily have to be
  reaching a consensus on a particular design
Instead, more realistically, the working group could aim at
  Discussing and reviewing the different designs and listing pluses and minuses or open issues….grounding on “objective” criteria
  Providing inputs to the other areas (in particular area I and area II) to better define their roadmaps and overall directions, and avoid inconsistencies

## Slide 6: 2nd goal of the working group
Review and follow-up of current work on hybrid magnets
This current work can be divided based on the field level
  9-10 T
  11-12 T
  13-14 T
  Beyond 15 T
The goal is to collect and organize information from these programs (responsibility of area I and area II) to provide inputs for 20 T hybrid design

## Slide 7: Outline
Definition of the goals of the working group
Design criteria for a 20 T hybrid magnet
Some preliminary estimates of radiuses and dimensions
Overview of current hybrid work
Action items

## Slide 8: Design criteria for a 20 T hybrid magnet
Previous work within MDP on a 16 T dipole magnet
  GianLuca Sabbi, Alexander Zlobin, MDP General meeting – May 17, 2017
https://conferences.lbl.gov/event/82/

## Slide 9: Design criteria for a 20 T hybrid magnet
Geometrical
  Number of apertures 1
  Free coil aperture 50 mm
Comments
  The common coils will naturally provide 2 apertures
    This will be taken into account on the comparison
  No “strong” constraints on
    Magnet total length (<2 m)
    Magnet straight section (>200 mm)
    Maximum magnet OD
      Reference numbers: 620 mm (FNAL/1.9K), 660 mm (BNL/1.9K), 914 mm (LBNL/4.5K)

## Slide 10: Design criteria for a 20 T hybrid magnet
Operational
  Reference temperature 1.9 K
    4.5 K option can be considered: it would impact the ratio of HTS vs LTS
  Operational bore field 20 T
  Margin on the load-line @ 1.9K >= 15 %
    With respect to round strand Ic including self field and 5% cabling degradation
  Short sample bore field 23.5 T
  Geometrical harmonics at Rref=17 mm and 20 T: bn<5 for n<10
    Magnet straight section
  Target design field 20 T

## Slide 11: Design criteria for a 20 T hybrid magnet
Operational
  Maximum Nb3Sn coil stress >180 (<150) MPa at 1.9 (293) K
  Conditions of coil-pole or rib interfaces at 20 T
    If bonded 20 MPa max. tension
      ‘Corner spikes’ (~1 contact element, 1 mm) neglected
    If separation allowed: Half cable width in contact or < 50 µm max gap
      Conditions may be different depending on the design

## Slide 12: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  Strand diameter 0.7-1.2 mm
  Cu:non-Cu ratio 0.8-2.0
  Non-Cu Jc round strand with self-field
    12 T, 4.2 K 2980 A/mm2
    15 T, 4.2 K 1640 A/mm2
    16 T, 4.2 K 1250 A/mm2
      See next slide for reference fit
  RRR (after cabling) >50
  Ic degradation due to cabling 5%
  Maximum number of strands in cable 60
  Cable Insulation thickness 0.150 mm

## Slide 13: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  Reference Jc(B,T) fit:
  , ,
    where 𝑡=𝑇/𝑇c0; 𝑏=𝐵p/𝐵c2 (𝑡), Bp is the conductor peak field, Tc0 = 16 K, Bc20 =29.77 T, C0 = 223900 T.A/mm2.
  Fit of data from recent (03/2020) RRP 108/127, 1.1 mm diameter, 1.1 Cu/non-Cu

## Slide 14: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  “3000” A/mm2 kind of conductor, round, with self field
Jc round
Jc , 5% deg.
Je , 5% deg.

## Slide 15: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  In general, it would be better to stay within already tested parameters (min, max)
Dimension before reaction; In MQXF, assumed expansion during reaction is 4.5 % (th), 1.2 % (w)

## Slide 16: Design criteria for a 20 T hybrid magnet
REBCO Conductor
  Work in progress
Bi2212 Conductor and cable (input from T. Shen and L. Garcia Fajardo)
  The wire diameter:
    from 0.6 mm to 1.5 mm
  Cable width: basically same possibilities as with Nb3Sn cables

## Slide 17: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable (input from T. Shen and L. Garcia Fajardo)
  Record performance strand RC5/6 about 20% higher than what is currently “comfortably” produced.

## Slide 18: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable
  Maximum Nb3Sn coil stress: <120 MPa (293) K

## Slide 19: Design criteria for a 20 T hybrid magnet
Quench protection
  Nb3Sn
    Maximum hot spot temperature 350 K
    Total time delay 40 ms
    Maximum J in the Cu 1350 A/mm2
    Maximum voltage to ground @ quench 1.0 kV
    Ground insulation design voltage >5 kV
  Bi2212 and REBCO
    Limit criteria to be determined (feedback from Area II and III, experiments, tests…)
      For Bi2212, Tmax= 400-450 K (Supercond. Sci. Technol. 29 (2016) 035010)
  Powering in series

## Slide 20: Outline
Definition of the goals of the working group
Design criteria for a 20 T hybrid magnet
Some very preliminary estimates of radiuses and dimensions
Overview of current hybrid work
Conclusions and action items

## Slide 21: First some references (20 T Bop)

## Slide 22: First some references (“towards” 20 T)

## Slide 23: First some references (“towards” 20 T)
Analytical model from Lucas Brouwer
  Thick shell with cos distribution
4 CCT winding layers,
  2 of Bi2212 and 2 of Nb3Sn
    Field in Nb3Sn is given by self field + stray field from Bi2212 insert
Results: 150-160 mm interface D for B=23.5 T

## Slide 24: Preliminary analysis of coil and magnet dimensions
Sector coil (60) with J = J0 distribution

## Slide 25: Field in at 20 T dipole
Bbore_op = 20 T
Bpeak_op = Bbore_op · 1.04 = 20.8 T
Bbore_ss = Bbore_op / 0.85 = 23.5 T
Bpeak_ss = Bbore_ss · 1.04 = 24.4 T

## Slide 26: Nb3Sn vs Bi2212
With properties describe above Nb3Sn and Bi2212 cross at 14.5 T at 4.2 K and 16.5 T at 1.9 K

## Slide 27: Very…very…preliminary coil size
So, with Jo_op = 385 A/mm2 and Bbore_op = 20 T
  Coil width ~ 75 mm
Very strong assumptions
  constant uniform Jo,
    same cable….
  No spar/ribs…
75 mm should a first order thickness of only the “cable layers” in a cos distribution

## Slide 28: Field in the conductor
At short sample, Bp_ss = 24.4 T  Je_ss = 670 A/mm2  Jo_ss = 452 A/mm2
So, at 85% of short sample  Je_op = 570 A/mm2  Jo_op = 385 A/mm2

## Slide 29: Very…very…preliminary coil size
50 mm aperture
Under the previous assumption (very simple analytical model, no stress management….)
  ID Nb3Sn = 146 mm
  OD Nb3Sn = 200 mm
  75 m total coil thickness
    48 mm thick Bi2212 coil
    27 mm thick Nb3Sn coil
Bi2212
Nb3Sn

## Slide 30: Very…very…preliminary magnet size
20 mm collar
250 mm thick yoke
  However, for a single short model, higher stray field could be accepted
50 mm thick shell
  Fx/t = 200 MPa
OD: 850 mm

## Slide 31: Size comparison
LHC MQXF FRESCA2 ????

## Slide 32: Outline
Definition of the goals of the working group
Design criteria for a 20 T hybrid magnet
Some preliminary estimates of radiuses and dimensions
Overview of current hybrid work
  Both conceptual design and “real” development
Conclusions and action items

## Slide 33: The 9-10 T field level
LBNL
  Bi2212 insert Bin5c_2 (2-3 T stand alone) in CCT5 (8-9 T)
    Test planned in 2021

## Slide 34: The 11-12 T field level
BNL
  Coils wound with REBCO tape or CORC (1-3 T) inside DCC017 common coil Nb3Sn dipole (10.2 T)
Tape perpendicular to field
Tape parallel to field
CORC

## Slide 35: The 13-14 T field level (I)
LBNL
  Bi2212 or REBCO (CCT or COMB) inserts (5-6 T stand alone) in CCT6 (2 or 4 layers, 11 T)

## Slide 36: The 13-14 T field level (II)
FNAL
  Bi2212 or REBCO (CCT or COMB) inserts (5-6 T stand alone) in SMCT (2 layers, ~11 T)

## Slide 37: The 13-14 T field level (III)
BNL
  CORC Coils in DCC017 as part of the STTR Program

## Slide 38: The 13-14 T field level (III) and beyond 15 T
FNAL
  Bi2212 insert SMCT (4-5 T stand alone) in 11T dipole coil and then in SMCT coil

## Slide 39: Conclusions and action items
The goals of the working group have been defined
  Comparison linked to 20T hybrid design
General criteria for the conceptual design defined, especially for Nb3Sn
  Less “rigid” than in previous comparison work
  Many open question on HTS (quench protection, stress)  feedback from Area II and III needed
Preliminary analytical analysis seems to provide “reasonable” general dimensions
Some general comments
  The topics (20 T Bop) seems still rather “unexplored”, or not too crowded
  With Area I and II, MDP has a nice R&D path towards it
Next steps
  Work on REBCO specs and Je
  Define “comparison” criteria
  Continue aperture/thickness/dimension analysis
    Iron, grading
  Move progressively from analytical models to simplified FEM of CT, CCT, SMCT, block and CC designs
  Continue the follow-up of current hybrid program

## Slide 40: Appendix

## Slide 41: 1st goal of the working group
Time frame: 2020 – 2023
Methods
  Modeling effort
    “classical 2D/3D” mechanical, magnetic and QH simulations
      Developing new modeling techniques is not part of this task
      However, if new tool/analysis is required  feed-back to Technology area (III), modeling and simulations

## Slide 42: Design criteria for a 20 T hybrid magnet
Bonded vs separation-allowed
  Test Facility Dipole (by G. Vallone)

## Slide 43: Design criteria for a 20 T hybrid magnet
Bonded vs separation-allowed
  MQXF (by G. Vallone)

## Slide 44: Material limits (by Giorgio Vallone)

## Slide 45: Analysis of coil radius and thickness

## Slide 46: Peak stress
Stress due to accumulated e.m. forces on the mid-plane
  No shear, no bending….