## Slide 1
AE analysis and event clustering
M. Marchevsky
L. Stephey, M. Mustafa LBNL

## Slide 2: New hardware development
Commercial AE system from Physical Acoustics
Self-calibrating acoustic hardware
An FPGA-based system that can stream 8 (and up to 32 after upgrade) channels at 10 Ms/s and simultaneously stream important metadata such as count, energy, frequency, etc. in real time.
New variation of the “old style” two-wire sensor design that used compact SMD components and is modified to enable pulsing the piezo for cross-calibration purposes

## Slide 3: Selecting acoustic events by thresholding
Threshold
HDT
HLT
(hit definition time)
(hit lockout time)
N - number of zero crossings
U
T
t
0
t
0
- Event absolute time
T – Event duration
N - Number of zero crossings
F = N/T - Frequency
U – Event amplitude
U
E = U
rms
2
- Event energy

## Slide 4: Connecting AE amplitude, energy release and temperature rise
A metal ball dropped on the magnet surface, each time reaching progressively lower height hn, until all its energy has been transferred to the structure. Same energy fraction is transferred to the magnet structure at every bounce and En for the n-th bounce can be expressed as =
1. AE voltage in a square in known to be proportional to the energy released in the transient event. This can be verified in a simple experiment
2. Attenuation of the acoustic wave in the material follows a universal behavior:
3. In a number of papers it was demonstrated that integral thermal dissipation is proportional to the cumulative energy of acoustic emission for crack propagation
Using two sensors at the opposite ends of the magnet one can estimate energy release as where is a universal scaling and and are the acoustic sensor voltages
IOP Conf. Series: Material Science and Engineering 208, 012012 (2017)
Specific heat of the conductor at low temperature c(T)~aT, hence:
= ~ = ½(-)
M. Marchevsky et al., Cryogenics, 69, pp 50-57, 2015
https://doi.org/10.1016/j.cryogenics.2015.03.005.

## Slide 5: Magnet memory and two distinct training regimes
“kink” in the training
dependence
Regime I
Regime II
Quench #90
Mechanical memory in the initial quenches (Kaiser effect)
As training progressed, the memory effect is erased
Quench #90
Quench #3
Quench #2
Quench #1
Possible physical mechanism:
Cracks in epoxy develop and percolate
=> slip-stick between grains and parts
CCT5: new non-cracking epoxy was used => Regime I portion of the training curve is eliminated!

## Slide 6: Mechanical events can be reliably identified using acoustics
1 g ball dropped from 7.5 cm height.
Ball drop
Pencil break
by E. Nilsson
When ratio of d1/d3 , where dn is the nth scale of discrete wavelet decomposition is used as an identification criterion, an order of magnitude difference between pencil lead break (events 2-12) and ball drop (event 13-30) is detected on all eight sensors around the magnet (even those that are far away from source)

## Slide 7: Simple event classification approach
Select two fingerprint files: from Quench #1 ramp – label them as “1”, and from Quench #103 ramp – label them as “2”
Split the resulting data into two randomly-selected sub-sets of equal size (2860 pts)
Normalize wavelet scale-specific amplitudes for every event
Apply trained and validated algorithm to the ramp data is has never seen to find out how many events of each type were detected
Q1 ramp: 4711 events of type “1” Q103 ramp: 2860 events of type “2”.
Randomized and took 2860 of each type => 5720 events total in the dataset
Train the Random Forest classifier in Python on the first sub-set against event “type”, then validate its prediction accuracy using the second sub-set
 | Actual type |  | 
 |  | 0 | 1
 | 0 | 1152 | 321
 | 1 | 185 | 1202
Predicted type

## Slide 8: Identifying fraction of “cracking” events in training ramps
Type “1” event fraction
Ramp to quench #
“kink” in the training
dependence
Trained Random Forest model reveals a kink in the event fraction dependence that coincides with the transition from “cracking” regime in the training curve

## Slide 9: Looking at “fingerprints” using spectrograms
“True ”Regime I”?
“True ”Regime II”?
Q1
Q103

## Slide 10: Acoustic event type clustering and sound database
Encoder
Decoder
Latent
Reconstructed spectrograms
First encouraging unsupervised clustering results using deep learning
In collaboration with NERSC

## Slide 11: How different AE events really are in the beginning of training vs end of training?
CCT4 Quench #3
CCT4 Quench #103
We still need a robust physical validation of our clustering results

## Slide 12: Mechanical relaxation after the quench in CCT4
~ 2.5 s
9677 A
10197 A
16266 A
current
current
current
acoustic
acoustic
acoustic
Post-quench slip-stick “aftershocks” – we will apply those to verify clustering and potentially also for supervised training
Cracking
regime
Slip-stick
regime
CTD-101 (4.2 K)
“Mix-61” (4.2 K)
Un-sintering of a Nb3Sn
Rutherford cable (RT)
All slowed down to ~17% of the original sampling rate of 1 MHz
We are building a “sound database” that can be latter used for supervised learning models