## Slide 1: Multi-Scale Modeling of Superconducting Magnets
D. Arbelaez
MDP Modeling Group Meeting
05/19/2020

## Slide 2: Multi-Scale Model Overview
Coil
Cable
Strand
RRP Filament
Obtain the 3D strain state at the filaments for applied macro-scale loads
Determine effective material properties at different length scales
Models range from the cable to strand sub-element scale

## Slide 3: Available Tools
Several tools were developed and are available for use
Cable Models (use regular mesh)
  Cable deformation model
  Stress/Strain analysis on cable
  Effective property calculation (including epoxy in gaps between strands and insulation around cable)
Periodic sub-element model
  Stress/Strain analysis on sub-element
  Effective property calculation

## Slide 4: Cable Compaction Model
Large plastic deformation finite element two phase model
  Elasto-plastic homogeneous phase (strand)
  Non-linear elastic fictitious material phase (void)
Avoids complications with meshing and contact elements
Fictitious void material is modeled with a highly compressible “soft” material
Regular unaligned mesh
Three types of elements
  Strand element (elasto-plastic)
  Void element (non-linear elastic)
  Interface element
    Treated as a void element when the volume of the element is greater than the strand volume inside that element
    Treated as a strand element when the volume of the element is less than the strand volume inside that element
Unaligned Mesh
Strand
Void Space

## Slide 5: Material Properties
Elasto-plastic strand
  Power law hardening curve
  Properties for Copper are assumed
Fictitious void material
  Defined by strain energy function
  Volumetric part is a function of J (ratio of final to initial volume)
  Highly compressible (small stiffness) for moderate values of J
  Stiffens quickly as J approaches zero

## Slide 6: Initial Cable Configuration
Initial cable model
  Number of strands (N)
  Strand diameter (d)
  Initial pitch angle (φ0)
  Smallest repeating unit cell in the axial direction with length
End strand geometry
  Remains in contact with at least on strand throughout unit cell
  Initial angle φ0 and final angle -φ0 with respect to the cable axis
  One possible solution for the axis of the end strand is the intersection of two angled cylinders
Intersection defines the end strand axis

## Slide 7: Deformed Cable Shape
Final cable parameters
  Width of the cable (w)
  Thickness of the cable (t)
  Pitch length (Lp)
  Packing factor
Boundary conditions
  Periodic in the axial direction
  Normal displacement is constrained on the side faces
Parameters for Deformed Cable Example

## Slide 8: von Mises Stress Example

## Slide 9: Sample Cross-Sections

## Slide 10: Homogenization of the “Coil Material”
“Coil Material” microstructure
  Cable
  Interstitial binder (epoxy)
  Insulation layer (S-glass composite)
Homogenized strand properties are used for the cable
Periodicity is assumed in all directions (infinite material)
Consider only linear elastic behavior
Effective properties are extracted by applying six different periodic loading conditions
Insulation
Epoxy
Strand

## Slide 11: Calculated Orthotropic “Coil Material” Properties
Individual Material Properties
  Epoxy (E = 5 GPa, ν = 0.3)
  Insulation (E1 = 14.9 GPa, Et = 6.7 GPa)
  Strand properties varied (E = 126 GPa determined from homogenization of the strand with E = 135 GPa for Nb3Sn)

## Slide 12: Model at the Strand/Filament Scale
Homogenization of a periodic microstructure to determine effective properties
  Periodic assumption is valid only if there is a large number of sub-elements
  Geometry may not be periodic due to deformations
Periodic Microstructure
Periodic Boundary Conditions

## Slide 13: Coupling Between Different Scales
Coupling is for only linear elastic properties
  Trivial coupling between scales since properties are independent of deformation
  Coupling from coil to cable scale and from cable to RRP sub-element/filament scale
Loads are transferred by applying the strain in the larger scale as the average strain over a unit cell in the smaller scale

## Slide 14: Conclusions
Work did not continue on this subject after initial progress but some useful tools were developed
  Cable deformation code
  Effective property calculation code
  Framework is in place for multi-scale analysis
If there is interest these tools can be made available for broader use
  In current form they are not made for outside users and would need some work to make them user friendly