## Slide 1: CCT development using CORC® wires to address several questions
How to make magnets using CORC® wires?
  Develop technology required for high-field applications
What is the magnet performance?
  Field, quench behavior, field quality
  Feedback on conductor performance
What needs to be improved and developed?

## Slide 2: Develop magnets with increasing complexity
C0: first 3-turn coils on printed mandrels
  First experience with CORC® wires, joint fabrication
  Short wires < 2 m
C1: 40-turn two-layer magnet on printed mandrels
  Fabrication: winding with relatively long wire, ~ 10 m, low-Je wire (150 A/mm2 at 20 T, 4.2 K)
  Performance: target 1 T at 4.2 K, quench behavior, field quality
C2: 40-turn four-layer magnet on metal mandrels
  Fabrication: metal mandrel, winding, applying Stycast epoxy. 30-tape wire with higher Je (250 A/mm2 at 20 T, 4.2 K)
  Performance: target 3 T at 4.2 K, quench behavior, field quality
  Feedback for conductor development

## Slide 3: Development of subscale 3-turn coils is very useful
Track the wire critical current after each fabrication step to understand the development
Detect and correct issues before the 40-turn magnet development
Use the 3-turn coil on aluminum bronze mandrel as an example

## Slide 4: Driving questions
What’s the Ic reduction with Al-Br mandrels?
  22% on layer 1 and 27% on layer 3
Any issues with winding on metal mandrels?
  Insulation was scratched off when the wire entered the groove
What’s the impact of applying stycast?
  1% Ic reduction, negligible
What’s the best procedure to apply stycast?
  Apply the stycast when wrapping the fiber cloth

## Slide 5: Two 3-turn C2 coils using Aluminum-Bronze 954 mandrels were made and tested
Both layers had 30 mm minimum bending radius
The central region was sand-blasted. The resulting surface scratched off the wire insulation during the winding of the 3-turn Layer 1
This issue was addressed by polishing the groove with Scotch Brite disk
Layer 1
Layer 3

## Slide 6: Al-Br 3-turn Layer 1
Wire (~ 1.85 m) was cut from Layer 3 commercial order
Three tests at 77 K
  10/1/2018, installed terminals
  10/2/2018, tested before bending
  10/11/2018, tested after winding before applying stycast
  10/16/2018, tested after applying stycast

## Slide 7: Several electrical shorts occurred during the winding with the sand-blasted mandrel
Polyester insulation scratched off when the wire rubbed against the groove
  Sand blast made the surface of the groove rough
We need to minimize the number of shorts
  Multiple shorts may create arc damage to the conductor
  Epoxy may touch the conductor and cause damage during curing
We paused the winding, polished the groove and continued winding with no short observed afterwards

## Slide 8: Used UV glue to help wrapping the voltage-tap wires
The Kapton patch to remove the short

## Slide 9: We painted the coil with Stycast 2850MT with a layer of fiber cloth and then wrapped with heat shrink tapes to control the profile of the Stycast
After painting and wrapping with fiber cloth
The peak surface temperature was around 200 F
Wrapped a layer of heat shrink tape after applying Stycast on top of fiber cloth

## Slide 10: There were local high points after the Stycast cured
We plan to reduce the amount of Stycast by skipping the second round of Stycast for future coils

## Slide 11: Using 10 µV/m criterion, we had 21% Ic reduction after winding, and 1% more after applying stycast, better than the 30% reduction measured on the bluestone 3-turn layer 1
Raw data
Resistive foot removed
Lower contraction of Al-Br (0.324%) compared to Bluestone (0.6%) may lead to less Ic reduction after applying the stycast
The Al-Br is also magnetic which can reduce the peak field on the wire

## Slide 12: V2 after winding: slope of the resistive foot reduced by 85% to 3 nΩ and the n value doubled to 10
Increasing n value after winding was observed in the past
Not clear why the resistive foot reduced

## Slide 13: Applying the stycast did not cause any significant performance degradation
Ic (A) @ 10 uV/m | Before winding | After winding | After stycast
V0 | 682 | 722 | 688
V1 | 938 | 825 | 796
V2 | 1561 | 1240 | 1218
1% Ic reduction after applying stycast could be due to the increased strain on the conductor

## Slide 14: Similar conclusion holds if using the voltage criterion (2 µV), although the performance increased after winding due to the low criterion
Ic (A) @ 2 µV | Before winding | After winding | After stycast
V0 | 341 | 391 | 360
V1 | 564 | 492 | 461
V2 | 918 | 977 | 956

## Slide 15: Al-Br layer 3
Wire was cut from the 3 m long witness sample for the Layer 2 commercial order
10/8/2018, installed terminals
10/12/2018, tested before winding
10/18/2018, wound the coil
10/19/2018, tested at 77 K after winding
10/22/2018, applied stycast
10/23/2018, tested at 77 K after applying stycast

## Slide 16: V(I) of three segments across the conductor showed the current transfer and VI transition of the superconducting wire
Three pairs of voltage taps monitoring the V-I transition
V2
V1
V0

## Slide 17: Wound the coil after applying a Stycast patch to the first reverse bend
Grooves were polished before winding. Only one intermittent short at the pole region was observed during winding
Applied Stycast patch on the lower reverse bend before winding
Applied Kapton tapes inside the exit groove to prevent shorts between the conductor and the groove

## Slide 18: Wire on Layer 3 experienced more handling than that in Layer 1, which may cause additional Ic degradation
Wire came off the groove in the double-bend region
Clamped it down to the groove which did not occur to layer 1 wire
For C2, we modified the mandrel design to remove the reverse bends in Layer 3

## Slide 19: Using 10 µV/m criterion, we had 27% Ic reduction after winding and no impact from applying stycast
Raw data
Resistive foot removed
Using 2 µV voltage criterion, we had 18% Ic reduction after winding and 1% more after applying stycast

## Slide 20: Ic values from two criteria
2 µV voltage criterion
10 µV/m electric-field criterion

## Slide 21: V2 after winding: slope of the resistive foot reduced by 80% to 1.8 nΩ and the n value increased by 50% to 15
This was consistent with Layer 1

## Slide 22: No high point by applying one-pass of stycast

## Slide 23: We gained useful experience for C2 with two 3-turn coils using Al-Br mandrels
We reduced the chances of electrical short between the wire and mandrel during winding.
  The rough edge of the groove scratched off polyester insulation
  Grooves were polished after being sand blasted. This reduced the chances of damaging the insulation
Developed a procedure to co-wind voltage-tap wires
  The wires were stable in the groove next to the wire but we lost one turn. No significant inductive noise was observed during the cold test. Need to verify this with the 40-turn coil
Modified the procedure to apply stycast to ensure the layers can fit into each other
  One pass of stycast when wrapping the fiber cloth. Skipping the second pass when wrapping the heat shrink tape
  Used 1” wide heat shrink tape with 0.5” wide fiber cloth. Seems working. Continue improving the technology with 3-turn bluestone coils
  Heating with 550 F temperature setting on the heat gun seems working. Need to verify with bluestone coils
The Ic reduction ranges from 22% to 27% after applying stycast. Lower than the 30% observed on layer 1 Bluestone mandrel
  Need to verify more on Bluestone coilis
  The impact of Stycast is negligible (1% Ic reduction)