## Slide 1
Stoyan Stoynev for the team
US Magnet Development Program
Fermi National Accelerator Laboratory
MDPCT1b quench locations, quench propagation and links to performance
MDP Meeting, July 22, 2020

## Slide 2: “15 T” Coil connections
COIL 005
COIL 004
-
+
COIL 002
COIL 003

## Slide 3: “15 T” voltage taps
A1
A2
A3
A4
A5
A7
A8
A6
Coil instrumentation (seen from “above”)
A9
B1
B2
B4
B5
B3
B7
B8
B6
C3
C4
C7
C5
C6
D3
D4
D7
D6
D5
D1
D2
C1
C2
Layer 1
Layer 2
Layer 3
Layer 4

## Slide 4: MDPCT1b Training
Ramp #58
Ramp #s
61
62
63
Ramp #75
Ramp #1
Ramp #2
Ramp #45
Ramp #13
Ramp #14
Ramp #6
(it is possible that
degradation goes on)

## Slide 5: Quench patterns

## Slide 6: Quench locations at a glimpse .
28
28
20?
20?
20
11*
*7 of them are RR and TD quenches
3
3
2
2
2
2
2
2
2
The only
non-pole
location
COIL 005
COIL 004
Those colors indicate
quenches in different
non-adjacent segments
(often in different layers/coils)
This color indicates fairly
well known location
This color indicates not so
well known location
Both colors (and only them) can
have associated numbers which are
the numbers of similar quenches

## Slide 7: Quenches
Coil 4 only quenches
Looking at beginning-middle-end of training curve

## Slide 8
4; d6_d7, d7_c7, c7_c6, d5_d6
COIL 005
COIL 004
Known
Ramp 1
(7530 A)
Propagation through d7_c7 (27 cm): 57 ms
Propagation through d6_d7 (27 cm): 9+71 ms
Quench propagation V: 5 m/s and 3 m/s, respectively

## Slide 9
4; c7_c6, d4_d5
COIL 005
COIL 004
Ramp 6
(8497 A)
Less known
9.5 V/s
Most of the quenches don’t give
enough information to determine
the propagation velocity but
one can compare voltage rise
patterns in the same segment(s)

## Slide 10
4; d4_d5, d3_d4
COIL 005
COIL 004
Ramp 58
(8978 A)
14.6 V/s
~Known
No significant differences in
propagation pattern toward the
end of the training curve;
faster propagation at higher current
(factor of ~2).

## Slide 11: Quenches
Coil 5
Three main patterns identified, points of interest on the training curve investigated

## Slide 12: Quenches
Coil 5
Pattern 1
(beginning of training, ramp rate
and temp. dependence quenches)

## Slide 13
5; c6_c7, c5_c6, c3_c4
COIL 005
COIL 004
Known
Ramp 2
(7924 A)
Propagation through c5_c6 ( 54 cm): 16 ms
Quench propagation V: 34 m/s (?)
(more likely C3_C4 is quenching
independently, see later)
Less known
4.4 V/s
6.6 V/s
C5_c6
Ramps
Pattern

## Slide 14
5; c6_c7, c5_c6, c3_c4
COIL 005
COIL 004
~Known
Less known
?
Ramp 86
(8886 A; 4.5 K)
8.6 V/s
?
No significant differences in
propagation pattern between early
training at 1.9 K and RR/TD quenches;
faster propagation (factor of ~2); second quench location initiates earlier.
Could be
resolved
by
acoustic
measurements

## Slide 15: Quenches
Coil 5
Pattern 2
(with the two highest currents)

## Slide 16
5; c4_c5, c5_c6, d7_d6
COIL 005
COIL 004
Ramp 13
(9021 A)
Known
Less known
7.6 V/s
Propagation through c4_c5 ( 30 cm): 6.4 +23.0 ms
Quench propagation V: 10 m/s
15 V/s
8.0 V/s
C5_c6

## Slide 17
5; c4_c5, c5_c6, d7_d6
COIL 005
COIL 004
Ramp 14
(8940 A)
Known
Less known
Similar to ramp #13
C5_c6
Note that the dV/dt decreases by a
factor of two when the adjacent segment
becomes resistive – consistent with
quench propagating in the remaining
segment direction
15 V/s
8.0 V/s

## Slide 18
5; c4_c5, c5_c6, d7_d6
COIL 005
COIL 004
Ramp 62
(10007 A)
Known
Less known
28 V/s
73 V/s
16 V/s
Propagation through c4_c5 ( 30 cm): 1.4 +6.9 ms
Quench propagation V: 36 m/s
C5_c6
Much higher initial expansion,
faster propagation later (factor of ~2+).
C5_C6 dV/dt factor of 3+ higher!

## Slide 19: Quenches
Coil 5
Pattern 3
(with limiting quenches)

## Slide 20
5; c5_c6, c6_c7, c3_c4
COIL 005
COIL 004
Ramp 46
(9831 A)
Known
Less known
?
62 V/s
40 V/s
In this case the quench starts in
the “green” segment and it propagates in
both directions
(two-directional 62 V/s is consistent also
with the one-directional 28 V/s from the
previous slide)
C5_c6
?

## Slide 21
5; c5_c6, c6_c7, c3_c4
COIL 005
COIL 004
Ramp 61
(9980 A)
Known
Less known
?
36 V/s
61 V/s
C5_c6
?

## Slide 22
5; c5_c6, c6_c7, c3_c4
COIL 005
COIL 004
Ramp 63
(9900 A)
Known
Less known
?
62 V/s
34 V/s
C5_c6
?

## Slide 23
5; c5_c6, c6_c7, c3_c4
COIL 005
COIL 004
Ramp 75
(9961 A)
Known
Less known
?
104 V/s
60 V/s
C5_c6
Faster initial quench propagation
in later ramps? Could indicate
locally damaged conductor.
Segment boundary not so cleanly visible anymore in dV/dt.
?

## Slide 24
Ramp 63
(9900 A)
Ramp 68
(9969 A)
C5_c6
C5_c6
C5_c6
Ramp 66
(9913 A)
5; c5_c6, c6_c7, c3_c4
Ramp 64
(9883 A)
Those are all same scales.
From Ramp 66 on the profile changed,
a non-linear initial expansion is visible.
It suggests much higher quench propagation than in other quenches in the
same segment (but different location, see ramp 62 which is also similar to 67).

## Slide 25: Time between first two segments quenching
The time difference relates to “patterns” discussed. It is seen however that for one of the main pattern t changes significantly (after ~ quench #30). The other main pattern (where the limiting quenches are)
shows consistent nearly constant times despite the short non-linear quench/voltage expansion discussed.
Coil 5 times (on the right vertical axis)
are grouped in the main two “patterns”
(denoted C5-a and C5-b) with remaining
ones under another group (C5-rest).
Time ~0 usually indicates quenches in two
non-adjacent segments (often in different layers or coils)

## Slide 26: Summary
Quench velocities can only be determined in small part of the quenches
and they increase at higher currents (as expected)
Voltage rising (dV/dt) patterns are useful to monitor change in behavior
While the propagation speed clearly increases toward high currents,
non-linear/large initial expansions are seen in multiple quenches
toward the end of the training curve (coil 5)
  may indicate degradation “initiation”
  beyond the first milli-second dV/dt are consistent for large part of the
  training curve in the segment we can monitor (5C5_C6)
Ramp rate and temperate dependence quenches
are similar to some early training quenches at 1.9 K