## Slide 1: Costheta cross section (preliminary)
V. Marinozzi
07/28/2020

## Slide 2: Assumptions
Goal: develop a 20 T hybrid costheta cross-section
First layout: 6 layers (4 HTS, 2 LTS)
50 mm aperture
HTS is Bi-2212 rutherford cable, with filamentery strands
LTS is Nb3Sn
No HTS grading
Conductor parameters from existing cable

## Slide 3: Conductor
Quantity | Bi-2212 | Nb3Sn
Strand diameter | 0.8 mm | 0.8 mm
Number of strands | 30 | 30
Cu(stabilizer)/SC | 0.8 | 1.5
Bare width | 13.76 mm | 13.3 mm
Bare height (inner) | 1.4 mm | 1.4 mm
Bare height (outer) | 1.5 mm | 1.5 mm
Insulation thickness | 0.15 mm | 0.15 mm
Jc in SC | 1741 A/mm2 (20 T, 1.9 K) | 1929 A/mm2 (16 T, 1.9 K)
From DCC017
From RC coil (17 strands)
Grey values are preliminary, to be reviewed

## Slide 4: Critical current
Jc in SC obtained by scaling Jc engineering from Paolo slides

## Slide 5: Cross section
Layer 1: 15 turns
Layer 2: 22 turns
Layer 3: 24 turns
Layer 4: 24 turns
Layer 5: 27 turns
Layer 6: 30 turns
Total: 142 turns
85 mm

## Slide 6: Operating field and margin
Operating current | 12300 A
Operating bore field | 19.97 T
Peak field (Bi-2212) | 20.85 T
Margin on the load line (Bi-2212) | 89.14 %
Peak field (Nb3Sn) | 13 T
Margin on the load line (Nb3Sn) | 87 %
Nb3Sn
Bi-2212

## Slide 7: To do
Double check some HTS parameters
Perform field quality optimization
Compute forces (stress management need?)
Computation of quench protection related parameters (inductance, current in stabilizer,...)