## Slide 1: Interfaces
Steven Krave
Fermilab
US Magnet Development Program

## Slide 2: Interfaces are key
Glued or frictionless or something in between.
  We apply these boundary conditions to ensure controlled movement in our modeling in a fashion that matches reality
  In reality we don’t typically do anything to push conditions in any one direction and have uncertainty
  Uncertainty is bad, and leads to unpredictable, erratic performance
  We often rely on manufacturer data and idealized cases to generate a parameter-space for simulation
    This may be useful where these conditions are replicated

## Slide 3: Potential Failure Modes
Interfaces in magnet composites are all a function of adhesion characteristics of the resin and surface properties
Magnet interfaces are so weak that seems unlikely that they directly cause conductor degradation
From: https://www.stevenabbott.co.uk/practical-adhesion/fmodes.php

## Slide 4: Probing Failure
Tensile Adhesion testing
  I’m looking for some useable fixturing
Peel testing
  Useful for flexible substrate
    We have used for mold release testing
      Note, good mold release means had to quantify test data
    Could be cable to cable?
      Would need some tooling but probably not too difficult
Shear testing
  Shear Compression
  Short Beam
  Others

## Slide 5: Example Data
Short Beam Strength per ASTM D2344 of Nb3Sn Subscale Composite 4-stack

## Slide 6: Summary of New Resins tested so Far
CTD 101K with no binder tends to go to ~15 MPa
  Quiet until ~80% ultimate
CTD 155 goes to ~25MPa
  Quiet until ~50% of ultimate
153 goes to ~22 MPa
  Makes noise from 20%
701X goes to ~26 MPA
  Reasonably quiet until failure

## Slide 7: Observations and anecdotal evidence
For QXF we are doing a comparison between a good performing coil and an average performing coil.
  Visual testing and Tg Measurements
    Aside from some small cosmetic differences these don’t seem to build much of a case for difference in performance
  But we had to break them to extract samples
    We found it very easy to extract samples from the better performing coil
    It was rather difficult to extract samples from the poorly performing coil
Worse Performance: Difficult to separate from pole
Better Performance: Easy to separate from pole

## Slide 8: Small scope plans moving forward
We plan on fabricating and testing 4 and ten stacks of reacted Nb3Sn Cable that have been cleaned and measuring shear properties
  Samples had insulation ultrasonic cleaned and rinsed in alcohol
  Cable ultrasonic cleaned in 2% Citranox and rinsed in alcohol
  Clean samples mean clean, clear cable samples
    I have not seen this in any other samples made
    The tech forgot mold release and needed a hammer and chisel to separate the cable sample from the tooling

## Slide 9: Suggestions for potential low friction/ reactable mold releases
Nickel Boron
  Nickel plating with embedded boron
Boron aluminum Magnesium
  High tech coating
Tungsten Disulfide
  Not compatible with epoxy
  Good to over 1000C and compatible with thermoplastics
Boron Nitride
  Seems to work ok, I have made some samples. It’s not as great as traditional mold releases but works. Adheres to the sample. Radiation concerns.