## Slide 1: MDP General Meeting 20 T hybrid magnet and comparative analysis
P. Ferracin, G. Ambrosio, E. Barzi, L. Cooley, R. Gupta, V. Kashikhin, V. Marinozzi, I. Novitski, B. Yahia, A. Zlobin
US Magnet Development Program

## Slide 2: Outline
Parameterization curves
  Nb3Sn
  Bi2212
  REBCO

## Slide 3: Parameterization options in Roxie

## Slide 4: Nb3Sn Critical current density
Reference Jc(B,T) fit assuming 5% cabling degradation:
  ,
  ,
    where 𝑡=𝑇/𝑇c0; 𝑏=𝐵p/𝐵c2 (𝑡), Bp is the conductor peak field, Tc0 = 16 K, Bc20 =29.77 T, C0 = 212705 T.A/mm2.

## Slide 5: Nb3Sn Strand critical current

## Slide 6: Bi2212 Critical current density
Assumption: Stab./non-stab. = 3
Cubic fit from 3 to 30 T
Jc (A/mm2) = a  B3 + b  B2 + c B + d
a | -0.1558
b | +10.655
c | -295.12
d | +5820.1

## Slide 7: Bi2212 Strand critical current

## Slide 8: REBCO Critical current density
Assumption: Stab./non-stab. = 10
Cubic fit from 5 to 25 T
Jc (A/mm2) = a  B3 + b  B2 + c B + d
a | -2.6533
b | +156.61
c | -3287
d | +30926

## Slide 9: REBCO Strand critical current

## Slide 10: Appendix

## Slide 11: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  “3000” A/mm2 kind of conductor, round, with self field
Jc round
Jc , 5% deg.
Je , 5% deg.

## Slide 12: Nb3Sn
Reference Jc(B,T) fit for round wire:
  , ,
    where 𝑡=𝑇/𝑇c0; 𝑏=𝐵p/𝐵c2 (𝑡), Bp is the conductor peak field, Tc0 = 16 K, Bc20 =29.77 T, C0 = 223900 T.A/mm2.
  Fit of data from recent (03/2020) RRP 108/127, 1.1 mm diameter, 1.1 Cu/non-Cu

## Slide 13: Nb3Sn
Nb3Sn Conductor and cable
  Strand diameter 0.7-1.2 mm
  Cu:non-Cu ratio 0.8-2.0
  Non-Cu Jc round strand with self-field
    12 T, 4.2 K 2980 A/mm2
    15 T, 4.2 K 1640 A/mm2
    16 T, 4.2 K 1250 A/mm2
      See next slide for reference fit
  RRR (after cabling) >50
  Ic degradation due to cabling 5%
  Maximum number of strands in cable 60
  Cable Insulation thickness 0.150 mm

## Slide 14: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  Reference Jc(B,T) fit:
  , ,
    where 𝑡=𝑇/𝑇c0; 𝑏=𝐵p/𝐵c2 (𝑡), Bp is the conductor peak field, Tc0 = 16 K, Bc20 =29.77 T, C0 = 223900 T.A/mm2.
  Fit of data from recent (03/2020) RRP 108/127, 1.1 mm diameter, 1.1 Cu/non-Cu

## Slide 15: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  In general, it would be better to stay within already tested parameters (min, max)
Dimension before reaction; In MQXF, assumed expansion during reaction is 4.5 % (th), 1.2 % (w)

## Slide 16: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable (input from T. Shen and L. Garcia Fajardo)
  The wire diameter:
    from 0.6 mm to 1.5 mm
  Cable width: basically same possibilities as with Nb3Sn cables

## Slide 17: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable (input from T. Shen and L. Garcia Fajardo)
  Record performance strand RC5/6 about 20% higher than what is currently “comfortably” produced.

## Slide 18: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable (input from T. Shen and L. Garcia Fajardo)

## Slide 19: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable
  Maximum Nb3Sn coil stress: <120 MPa (293) K

## Slide 20: Design criteria for a 20 T hybrid magnet
REBCO Conductor
  CORC cable
    3.42mm diameter including 30 micron thick insulation.
  STAR cable
    1.3 mm diameter without insulation (#3)
    2.04 mm diameter without insulation (#4)

## Slide 21: Design criteria for a 20 T hybrid magnet
REBCO Conductor
  We use the following parameterization
    Ic(B, 4.2 K) = 10^(*log(B)+c)
  Where

## Slide 22: Design criteria for a 20 T hybrid magnet
REBCO Conductor
  Stress degradation

## Slide 23: Design criteria for a 20 T hybrid magnet
With properties describe above
  Nb3Sn and Bi2212 cross at
    14.5 T at 4.2 K
    16.5 T at 1.9 K
  Nb3Sn and REBCO cross at
    15.0 T at 4.2 K
    17.5 T at 1.9 K

## Slide 24: Design criteria for a 20 T hybrid magnet
Quench protection
  Nb3Sn
    Maximum hot spot temperature 350 K
    Total time delay 40 ms
    Maximum J in the Cu 1350 A/mm2
    Maximum voltage to ground @ quench 1.0 kV
    Ground insulation design voltage >5 kV
  Bi2212 and REBCO
    See next slides
  Powering in series

## Slide 25: Design criteria for a 20 T hybrid magnet
Quench protection
  Bi2212: Tmax= 400-450 K

## Slide 26: Design criteria for a 20 T hybrid magnet
Quench protection
  REBCO