## Slide 1
Xiaorong Wang
REBCO Working Group/MDP
MDP weekly meeting, 9/30/2020
C3 update

## Slide 2: C3 will be a 6-layer CCT magnet aiming at 5 T dipole field using CORC® wires
Magnet ID: 65 mm
OD: 160 mm without external structure
Dipole field transfer function: 0.72 T/kA
Wound with commercial single CORC® wires

## Slide 3: C3 will address several key questions for high-field REBCO magnet and conductor technology
Conductor
  What is the optimal wire architecture to improve the Ic retention?
  How does the minimum Ic specification work?
  What is the actual wire performance?
  What needs to be done for future conductors?
Magnet fabrication
  Is it feasible to work with full-depth grooves?
  What needs to be implemented to address higher Lorentz forces?
  What can we learn to generate higher dipole fields?
Magnet performance
  Can we generate a 5 T dipole field?
  What is the mechanical behavior of the magnet?
  What is the transition behavior when the conductors are impregnated?
  How can we identify the locations of normal zones and understand the causes?
  What is the field quality?

## Slide 4: Conductor availability starts hindering the magnet/conductor feedback loop
Expect to receive CORC® conductors for C3 in Q1 2021
  First CORC® order placed in Q1 2019
  Tape order specified a minimum Ic at 4.2 K, 6 T for the first time
  Tape delivery to ACT has not yet started
In addition to cost, a longer lead-time is a concern for future magnets
  Work with vendors to understand the issues

## Slide 5: Ongoing mechanical analyses provide feedback to the magnet fabrication
aluminum shell
An aluminum shell is necessary to reduce the peak stress on the mandrel from 500 to 250 MPa
Lucas Brouwer

## Slide 6: A single-cell model to evaluate the stresses on conductors with different groove designs
Pole region
Mid-plane region
Mariusz Juchno

## Slide 7: Prepare tests on short CORC® wires to develop the vacuum-pressure impregnation process
Jillian Stern, Tufts University
Does the VPI process degrade the CORC® wires?
What’s the impact of curing temperature and duration?
Compare the wire Ic before and after the VPI process
Apply the successful VPI process on subscale coils, followed by C3

## Slide 8: Next steps
Complete the mechanical analysis for C3 (Q4 2020)
Complete the baseline fabrication plan for C3
  Prove the principle of a new winding concept (Q4 2020)
  Confirm the VPI process on CORC® wires (Q4 2020 – Q1 2021)
  Complete mandrel fabrication and magnet winding plan (Q4 2020)
Make and test the subscale C3 (Q1 – Q3 2021)
  Develop mandrels for the three-turn subscale magnet (Q1 2021)
  Work with vendors to delivery the wire in Q1 2021
Make and test the C3 magnet (Q4 2021 – Q2 2022)

## Slide 9: Additional questions that we are working on
How to identify the locations of first on-set of flux-flow voltages in the coils?
  Explore options of using distributed fiber-optic sensing
  Aim to test ideas with the subscale and C3 magnets
What is the stress limit due to Lorentz forces on bent conductors?
  Test subscale CORC® CCT coils in background fields

## Slide 10: Summary
C3 magnet is the focus of LBNL effort
We are completing the fabrication plan
  Deal with Lorentz forces that become serious
  Use the C2 technology as the baseline plan
  Develop new technologies and introduce them to C3
Conductor availability is a concern
  Work with vendors to confirm the delivery schedule of C3 wire
  Prepare for bigger uncertainty for future magnets