## Slide 1: Stress Modeling Results for CCT5 Relevant to Epoxy Properties
Lucas Brouwer
10/20/2020
MDP Modeling Working Group

## Slide 2: Outline
Last meeting we heard from Steve/Tengming about epoxy and interface strength
From the CCT modeling side, what are:
  interface normal/shear stress distributions
  potential trouble locations
Subscale and diagnostics options for probing impact on training

## Slide 3: Results in a local, cable frame are shown for CCT5
Mechanical model for CCT5 with load steps of
cooldown to 4.5 K
powering to 16 kA (~90% of short-sample)
conductor bonded in channel, layers sliding with friction
convert stress to local frame and output to paraview
mesh information
stress in Cartesian frame

## Slide 4: Local Conductor Frame Normal and Shear Stress
4
Local cable frame
x: tangent (along cable)
y: radial (along broad face)
z: bi-normal (along thin edge)
x
y
Broad Face (z-const)
Szx
Szy
Thin Face (y-const)
Syx
Syz

## Slide 5: Normal: tangent stress (along cable)
Local cable frame
x
y
At pole there is a gradient from positive to negative across the cable (+/- 30 MPa due to bending)
Scale capped at +/-30 MPa

## Slide 6: Normal: radial stress
Local cable frame
x
y
Scale capped at +30 MPa

## Slide 7: Normal stress towards the wall (bi-normal)
Local cable frame
x
y
ZZ represents pulling or pushing in the direction of the channel wall (first several turns want to separate)
In reality, the turns will likely separate long before 80 MPa

## Slide 8: Layer 2 is similar, but higher
Local cable frame
x
y
In reality, the turns will likely separate long before 100 MPa
But, most training quenches in CCT5 were in the inner layer

## Slide 9: Shear Stress in Local Frame (16 kA)
9
Broad Face (z-const)
Szx
Szy
distributed at +/- 45 deg and concentrated on inner edge
Thin Face (y-const)
Syx
Syz
“holds” back cable on the broad face from moving radially
“holds” back cable on the broad face from moving along channel (tangent)
“holds” back cable on the thin face from moving along bi-normal
“holds” back cable on the thin face from moving along channel (tangent)
peak is localized, 3D effect near pole

## Slide 10: First set of Subscale Magnets will Probe Different Stress States by Adjusting the Spar Thickness of Layer 1
Thick spars
High shear
Low normal
Thin spars
Low shear
High normal
8 mm spar
-35 MPa
35 MPa
2 mm spar
-35 MPa
35 MPa
1 mm spar
-35 MPa
35 MPa
Thin spar test
Thick spar test
Sxy (radial-azimuthal)

## Slide 11: Summary / Thoughts
CCT stress distribution is complicated and has several strong 3D effects
potential locations of trouble
  normal separation of turns from starting in the pole region
  shear at channel/conductor interface concentrated at +/- 45 deg
diagnostics which can resolve quench locations as a function of angle (azimuthal) can help correlate potential trouble spots with training quenches
thick/thin spar subscale tests will probe trade-off between shear/normal stress