## Slide 1
M. Marchevsky
Update on CCT4 acoustic data analysis
D. Arbelaez and S. Prestemon
LBNL

## Slide 2: Outline
Introduction on the canted-cosine-theta CCT4 dipole: test results, training plot and acoustic instrumentation
Acoustic signal analysis
  Event count
  Released energy and scaling
  Accumulated displacement
Wavelet frequency analysis for event type identification
Conclusions

## Slide 3: CCT4 Canted-Cosine-Theta Nb3Sn dipole: training summary
104 training quenches in total
11 quenches in the OL, the rest is IL
Highest quench current: 16731 A
Bore dipole field: 9.14 T
Field at the conductor: 10.32 T
“Short sample” limit: 19.3 kA (4.5 K)
Good quench memory after thermal cycle: reached 16590 A in 9 quenches
Training plot of the CCT4 magnet
B
I
Slope change
Tested in 2017

## Slide 4: Acoustic instrumentation
Cryogenic acoustic sensors
Broadband: ~350 kHz bandwidth
Epoxy cracking, de-lamination, or slip-stick motion of the conductor or a structural part are the common sources of Acoustic Emission
1200
Shell
IL
OL
Shell sensors
(8x)
1200 apart
1200 apart
Stop
Sbot
We collected acoustic signals in both triggered mode (for all 8 sensors, triggered by the magnet quench detection system) and in continuous streaming mode for 2 acoustic sensors, magnet current and voltage.
The continuous rate was either 1 MHz or 500 kHz; we then re-sampled all 1 MHz data to 500 kHz for a consistency of analysis.

## Slide 5: Quench locations
Quench locations we determined using AE triangulation, they appear to be distributed uniformly around the coil
What is the physics of energy releases responsible for premature quenching?
What defines the length of the training process
What defines the shape and slopes of the training plot?

## Slide 6: Visible coil defects after testing
49⁰
Transverse cracking
De-bonding/ separation

## Slide 7: Acoustic signal parameters
Acoustic voltage: U(t) ~ instant displacement
~ net displacement
# of zero crossings = how many times the oscillatory waveform crossed time axis within the event window
Event energy:
Frequency: (# of zero crossings) / Dt
Event window Dt : time interval between first and last threshold crossing
Padding: added interval before event start time
Gap: interval in which there are no threshold crossings (defining the end of the event window)
Acoustic event thresholding from a continuous stream
Bias:

## Slide 8: Acoustic event count
We sampled and thresholded continuous acoustic signal streams sequentially within 1s - long intervals. AE events were counted in each interval, and net count was plotted vs. magnet current.
AE events occur only when current is being ramped. For a fixed ramping rate the AE rate is non-linear with the current. When current ramping rate is changed, the acoustic event rate changes as well.
However, the AE net count plots for different quenches collapse towards a universal asymptotic power-law dependence at high current values.
Quench 1
Quench 2
Quench 3
Quench 90

## Slide 9: Power-law scaling of AE energy
AE energy per event exhibits no scaling with current up to ~ 9500 A and distinct power-law scaling above that current. Fit for Q59 yields E0 = 0.00066 [V2], I0= 9951 [A] and n = 3.12
As strain in the magnet is , we then get E() , where 1.56
The first quench was at 9677 A (~I0 ) !
Power–law scaling is a hallmark of critical dynamics seen in many physical systems including superconductors, magnetics, geoscience, etc.
This result suggests that the critical dynamics emerges in the magnet at I0, and is sustained throughout the current ramp until the quench. Also, a step divergence from the power-law develops a few seconds prior the quench for some ramps.
No scaling
Power law
Divergence

## Slide 10: Displacement (bias) accumulation
When plotting bias vs current squared, a proxy for the stress-strain dependence can be obtained that uniquely characterizes magnet interfaces affected by the training process.
The linear dependence is eventually recovered for high quench numbers suggesting “clearing up” of mechanical barriers and evolution towards more elastic behavior in the end of the training process

## Slide 11: Event energy statistics
Q39
Q59
Q76
Q103
Q6
Histograms of peak energy (V2) vs event counts adhere to a universal power law scaling with the exponent ~1 (similar to Gutenberg-Richter law observed for earthquakes and may other self-organized critical systems).
However, the low current ramps reveal an excess of high energy events while latest training ramps to high current exhibit an excess of mid-level events.

## Slide 12: Typical acoustic signatures of mechanical transients
Acoustic waves both in the in bulk (high frequency) and along separating surfaces (lower frequency)
v
Surface (S-) wave
Bulk (P-) wave
v
Bulk (P-) wave
Surface (S-) wave
Bulk resonances
Predominantly a high-frequency bulk wave
Low-frequency structural resonances

## Slide 13: Wavelet analysis
To analyze transient waveforms such as AEs, wavelet transforms are most convenient as they allow to accurately estimate frequency content of the signals.
We used the Morlet Wavelet
with the central frequency of ¾ Hz
For the scale the corresponding frequency value is then
As scale value is inversely proportional to frequency, we choose a set of values so that the center frequencies of the wavelets at the analyzed scales evenly sample the frequency range from 0 to /2 (where is signal sampling rate)
A1
A2
A3
A4
Example of AE transient signal and its scalogram (64 frequency scales)
For our analysis we sub-divide the scalogram over four equally-sized frequency bands and compare integrated relative amplitude in those bands.

## Slide 14: Beginning of training (Q6)
Few large high-frequency events
Voltage response in the coil

## Slide 15: Beginning of training (Q6)
Few large high-frequency events
Voltage response in the coil

## Slide 16: End of training (Q103)
Numerous multiplet events
Many large high-frequency events, followed by excitation of structural resonances (de-bonding?)
No voltage response in the coil

## Slide 17: Conclusions
We observed two distinct AE regimes during ramping to quench. In the beginning of training AE energy is independent on the magnet current. With continuing training, a universal power-law scaling of AE energy emerges which is a hallmark of critical dynamics. Also, a clear divergence from the power-law is seen in this second regime within seconds of the upcoming quench.
Accumulated displacement (AE waveform bias) plotted versus Lorentz force converges towards a linear dependence (= recovered elastic behavior) as training progresses.
We applied wavelet-based analysis to AE signals, and observed emergence of multiplet transients at high currents that can be attributed to a successive crack propagation. We also identified high-frequency (>200 kHz) bursts immediately followed by excitation of low-frequency structural resonances that may be indicative of interfacial debonding.
Analysis of CCT4 AE data will continue…

## Slide 18
Localization of hot spots in solids using acoustic waves
Technology Commercialization Fund project
Supported by the Office of Technology Transitions, US Department of Energy
In collaboration with
C. Sanabria, M. Segal
Commonwealth Fusion Systems
M. Marchevsky, R. Teyber
LBNL

## Slide 19: Scope of the project
Future generation and distribution markets based on the use of high-temperature superconductor (HTS) materials. Traditional quench detection methods for LTS relying on fast normal propagation zones (e.g. measuring a voltage increase of the system) do not work for HTS devices. The technology we are proposing was laboratory-tested on HTS tape conductors and small coils for detecting hot spot development down to liquid helium temperature.
Now we want to focus on the localization aspect of the technology it to be able not only detect hot spots but also provide their location information.
Demonstration of hot spot detection and localization in a commercial transformer device
Demonstration of hot spot detection in a conductor sample provided by CFS
Testing of HTS cable sample under operational conditions at BNL test facility in collaboration with CFS
Milestones
U*x(t)
delay
c
autocorrelation
cross-correlation
Dt
URef(t)

## Slide 20: Equivalence to voltage-based detection has been demonstrated
DT~1.6 K
Dtrel ~ 3.5 ns
DUmax ~ 7.6 mV (68 mV/cm)
Pulser
Receiver
Bi-2212 coil RC3
Coil design and test by T Shen / K. Zhang
Experiment at 4.2 K. Current ramp stopped at 6100 A (stable) and then increased by 30 A (quenching)
*STTR with ACT
M.M., E. Hershkovitz (LBNL)

## Slide 21: Coda wave “diffusion” provides means for localization of a weak change
Diffusion properties of the coda wave can be explored to evaluate distance to the point of weak change or heat source
Thomas Planès and Eric Larose, “LOCADIFF: Locating a weak change with diffuse ultrasound”, AIP Conference Proceedings, v. 1511, p.405 (2013)

## Slide 22: Simulations and tests on a mock-up fusion cable
Pulses of 2.3 ms duration were applied 5 Hz repetition rate. Pulse amplitude is ~40 V p-p.
Shear piezo-plate
Heater was placed at the middle of the cable (~25 cm from the ends; its power is 0.753 W. Heater was on for 100 s, 100 s and 50 s respectively
Tabletop test on a mock-up “cable”: a 50 cm-long copper rod:
ANSYS simulation of acoustic wave propagation and scattering in the fusion cable geometry
Shear piezo-plate
Copper rod with a central flow channel and flattened end
Well-formed shear wave propagates along the cable
In collaboration with

## Slide 23: Simulations to optimize transducer placement
In order to couple the acoustic transducer to the fusion cable in a best possible way, we investigated vibrational modes of a fusion cable geometry using ANSYS modal analysis. Several vibrational modes that are well coupled to the surface of the cable cooling channel (cable ID) and also close to the resonance frequency of the piezo-transducer were found, including a prominent one at 410 kHz (shown in the left image).
We have therefore decided to mount the acoustic transducers to the ID of the cable cooling channel for best efficiency and stronger mechanical coupling to the cable. The ID is also a “free surface” that would not be mechanically coupled to anything else when the cable is wound in a coil.

## Slide 24: Heater array design
2-layer Flex PCB
  Allows mounting to a cylindrical surface
  Minimizes change in vibrational modes due to mass, damping of heater assembly
Linear array of 11 small, surface mount resistors
  Any individual or pairs of resistors can be powered
  Can attach multiple linear heater arrays to samples of interest
To deliver localized heat to the cable sample for testing and calibration purposed, we have developed and built a flexible array of spot heaters capable of inducing small temperature variations with a good spatial accuracy and minimal intrusion
R. Teyber

## Slide 25: Heater installation on the “mock-up” sample

## Slide 26: Experimental setup
USB relay card
Function
generator
Acoustic sensor coupling box and Picoscope-based ADC
DC power supply
Heater array
Pulser piezo
Amplified acoustic sensor
Analysis and localization software

## Slide 27: Signal processing for hot spot localization
The original hot spot detection algorithm is based on measuring time shift variation for a small portion of coda waveform that is empirically selected to achieve maximal signal-to-noise ratio for the detection
Because coda is a result of multiple acoustic scattering inside the sample, it encodes different locations within the samples not uniformly, but in some “biased” way when different locations contribute differently to each particular segment of the coda. The exact relation between the location of the “disturbance” and its “encoding” in complex and not known. Still, such relation may be exploited for hot spot localization.
We do it by conducting a calibration procedure to create a “database” of coda variations specific to hot spots generated at different sample locations. Once created, such “database” can be then used to localize unknown disturbances by matching the measured variation to the database.
To realize this in practice, we programmed and tested a new algorithm that sub-divides the coda into 100 sequential intervals of equal duration and calculates time shift for each of those interval independently.

## Slide 28: New software was developed to monitor time shift simultaneously over multiple coda segments
We expanded our original quench detection software to include calculation of time shift along the pre-selected number of intervals along the coda, plot is as a waterfall plot as function of number of pulses (=time), and also calculate average variation of the time shift for those pre-defined segments as it accumulates over time.
Average time shift per segment
“Waterfall plot” of time shift vs time
Number of segments to calculate time shift
“Instant“ (per pulse) time shift measured along the coda
Coda

## Slide 29: Examples for different heaters producing time shift at different positions along the coda waveform
Segments of the coda along the time axis that are exhibiting largest time shift in response to a heater firing are marked with arrows. The “bar code” pattern in Time Shift vs Time waterfall plot are clearly different for different heaters, showing a potential for using this property for hot spot localization.
Heater 1 fired
Heater 11 fired
Coda
Instant time shift along the coda
Average time shift along the coda
Time

## Slide 30: Automated sampling and localization software
A program randomly fires the heaters using USB relay card, collects time shift variation data, update the database and localize the heater based on the data that is already in the database.
Time shift vs time monitored for an arbitrary chosen coda segment (shown on the left)
Spot heater voltage vs. time
Accumulated average time shift per coda segment (100 pts)
Kendall’s Tau coefficient for the current waveform comparing it to the waveforms in the database corresponding to different heaters
Localized vs actual heater location. Heaters are fired randomly

## Slide 31: Actual vs localized heater locations
Heaters were fired at random 120 times and localization was performed. The result is plotted above.
In 48% of cases heater firing location was determined exactly, in another 36% of cases heater firing location was determined with a +/- 1 accuracy, corresponding to an inter-heater distance of 26 mm. This clearly demonstrates feasibility of our localization approach. As number of event in the “database” increases with each consecutive heater firing, the accuracy of localization increases as well. Further improvement can be made using more advanced classifier methods based on machine learning algorithms, and we plan to adapt it for future (real cable sample) experiments.
Percentage of cases plotted vs absolute error

## Slide 32: Sketch of the cryogenic testing setup
~300 mm
G-10 spacers
~30 mm
Cernox thermometers
Flexible strip with spot heaters
Piezoelectric element
(ring)
To the acoustic DAQ
From the pulse generator
Cable sample
This sketch represents basics of the planned test setup and instrumentation, and preparations to the test are ongoing at BNL (funded by the INFUSE project that CFS and BNL are part of).
We are working on preparing for a cryogenic test at Brookhaven National Lab in Dec 2020.
The sample will be sealed inside a “cassette” that will be installed in the bore of BNL’s 10 T common coil magnet for testing at 4.2 K / 10 T background field.