## Slide 1: Update on Costheta cross section
V. Marinozzi
11/30/2020

## Slide 2: Assumptions
Goal: compare different cross sections
6 layers
50 mm aperture
HTS is Bi-2212 rutherford cable, with filamentery strands
LTS is Nb3Sn
Conductor parameters from existing cable
No harmonics optimization

## Slide 3: Critical current
Jc in SC obtained by scaling Jc engineering from Paolo slides
Still using linear approximation in the peak field zone
Jc for Nb3Sn: 1928 A/mm2 @16 T, 1.9 K
Jc for Bi2212: 2944 A/mm2 @20 T, 1.9 K

## Slide 4: Conductor for comparison with Paolo model
Quantity | Bi-2212 | Nb3Sn
Strand diameter | 0.8 mm | 0.8 mm
Number of strands | 30 | 30
Cu(stabilizer)/SC | 3 | 1
Bare width | 13.76 mm | 13.3 mm
Bare height (inner) | 1.44 mm (0.9 packing) | 1.44 mm (0.9 packing)
Bare height (outer) | 1.56 mm (0.5 keystone) | 1.55 mm (0.5 keystone)
Insulation thickness | 0.15 mm | 0.15 mm
From DCC017
From RC coil (17 strands)

## Slide 5: Iron yoke

## Slide 6: Baseline classic costheta (size optimized): v9b
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 40 – 35 – 30
Cable width: 18.35 – 16.06 – 13.3 mm
Stabilizer/Superconductor: 3 – 3 – 1.5
Coil width: 100 mm
Current: 10820
Peak field: 20.42 – 15.86 – 12.82 T
Margin: 81.9 – 82.3 – 83.3 %
Jcu on LTS: 1195 A/mm2

## Slide 7: Baseline classic costheta (HTS optimized): v11
2 layer HTS, 4 layer LTS
Strands: 0.8 – 1.1 – 0.8 mm, 40-35-30
Cable width: 18.35 – 21.3 – 13.3 mm
Stabilizer/Superconductor: 3 – 1 – 1
Coil width: 110 mm
Current: 11650
Peak field: 20.7 – 15.77 – 11.43 T
Margin: 86.2 – 83.3 – 73.6 %
Jcu on LTS: 700 – 1545 A/mm2

## Slide 8: SMCT-like with 3 mm rings (v9 evo): v9c
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 40 – 35 – 30
Cable width: 18.35 – 16.06 – 13.3 mm
Stabilizer/Superconductor: 3 – 3 – 1.5
Coil width: 112 mm
Current: 11500
Peak field: 20.51 – 15.52 – 12.34 T
Margin: 85.2 – 85.4 – 82.5 %
Jcu on LTS: 1271 A/mm2

## Slide 9: SMCT-like with 5 mm rings (v9 evo): v9d
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 40 – 35 – 30
Cable width: 18.35 – 16.06 – 13.3 mm
Stabilizer/Superconductor: 3 – 3 – 1.5
Coil width: 122 mm
Current: 13000
Peak field: 20.59 – 15.65 – 12.73 T
Margin: 92.4 – 93.7 – 87.5 %
Jcu on LTS: 1436 A/mm2

## Slide 10: SMCT-like with 5 mm rings: v12
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 46 – 40 – 30
Cable width: 21.1 – 18.35– 13.3 mm
Stabilizer/Superconductor: 3 – 3 – 1.5
Coil width: 132 mm
Current: 13790
Peak field: 20.54 – 15.39 – 12.78 T
Margin: 87.6 – 88.3 – 83.8 %
Jcu on LTS: 1828 A/mm2

## Slide 12: Cross sections

## Slide 13: v2

## Slide 14: v3

## Slide 15: V4

## Slide 16: v5

## Slide 17: v6

## Slide 18: v8

## Slide 19: v9

## Slide 20: v10

## Slide 21: v11