## Slide 1: Thermal modeling, interfaces, test results
LBNL Composites Workshop
February 29-March 3, 2016

## Slide 2: Thermal modeling of our typical detector structures, like ATLAS pixel local supports, is interesting
  thermal-mechanical deflection
  steady-state heat transfer
  non-trivial thermal interfaces
  thin-wall and thick-wall
  convection
  2 phase flow
  oh yes, and composite materials
    fiber-reinforced
    particle-reinforced
    foam/filler hybrid
0.6W/cm^2 @-7C
Thermal Grease 1.4W/mK
CC 40 X 200W/mK (0.5mm)
-20C
Flat tube —increase area
Sector ‘05
Carbon Foam (20-40W/mK)
0.6W/cm^2 @-15C
Thermal Grease 1.4W/mK
-30C
CFRP 1 X 200W/mK (0.075mm)
Buried tube (higher pressure)
Current Concept

## Slide 3: High in-plane thermal conductivity can be achieved for CFRP
  Typically use pitch-based fibers with high thermal conductivity (K)
  K1 of fiber itself can be extraordinary
    K13D2U fiber is 800 W/m*K, which is 2x copper
    this in the fiber direction (1-direction)
  K1 of a unidirectional ply is ~½ that
    rule of mixtures: K1,ply = Kf1 * Vf + Km * Vm
  K1 of a typical stackup is ~½ that again
    tensor rotation of each ply K1
    weighted average by ply thicknesses
  So for the high-performance pitch fibers, we end up with aluminum-like thermal conductivity in-plane, ~200 W/m*K

## Slide 4: Thru-thickness thermal conductivity is generally 2-3 orders of magnitude lower
  This is the out of plane direction (K3)
  K3 ~ 1 W/m*K
  K1 / K3 ~ 10² to 10³
  In special cases we can do a bit better than K11 = 200 W/m*K, but it often doesn’t matter:
    In many practical applications the limiting factor is getting the heat into or through the thickness of the laminate
  For a ply, K2 = K3 ~ (Vf / Kf2 + Vm / Km)-1
  Typical Kf2 ~ 2-10 W/m*K
  Typical Km ~ 0.2 W/m*K

## Slide 5: The interfaces are important resistors in our typical geometries
They certainly cannot be ignored.
Generally need to modeled as discrete solids, with finite thickness.
Silicon Module
CFRP Face Sheet
CVD Foam (30-40W/mK)
~0.5W/m2
1.25 W/mK (100m) SE4445
Thermal Interface Material
~1.0 W/mK (~200m)
1.1 W/mK (100m)
Interface Equivalent
Cooling Tube BC

## Slide 6: Our interfaces at foam-facesheet or foam-tube depend deeply on fabrication details
(A) 50um resin film, 25um peel
(B) No resin film, 25um peel
(C) No resin film, 75um peel
Epoxy + BN
Co-cured sample

## Slide 7: We need to use solids for thermal models in FEA
  For structural FEAs, we often use shell bodies (2D) to represent composite laminates
    This works because the thru-thickness loads (shear and out-of-plane modulus) are negligible
  For thermal FEAs, the thru-thickness conductivity is essential
    So we have to model 3D bodies of finite thickness
    This adds overhead to model setup
      more contact surfaces to define
      may need a discrete body for every ply
      and each ply body needs a discrete coord system to define its orientation
      some FE pre-processors (such as ACP) can make this work much faster (for complex geometries, read “possible”) to do

## Slide 8: We’ve more or less standardized on a typical method for assessing thermal performance of staves for detectors
  Stave has all fab processes and materials
  2+ Si/Pt dummy module heaters
  IR camera images heaters on and off
  ΔT = Ton – Toff , typical spec ΔT < 8-10°C
  This type of test includes the interfaces.

## Slide 9: Thermal-mechanical behavior is pretty straightforward to do in FEA
  Solve the thermal problem
  Pass temperature data as input to structural
  Solve the structural problem
It is not straightforward to test.

## Slide 10: We’ve used combined IR (thermal) + TVH (interferometry) to do this on I-beam
IR temp data
 B.C. for FEA
TV holography data
 Differential deflection between 2 setpoints (2 different power inputs to silicon)
Solve two thermal-stress analyses at the two setpoints and then compare to TVH data

## Slide 11: It is highly effective at validating FEA, but takes some work to do
FEA
TVH
meas.

## Slide 12: We typically fill our epoxies with particles to enhance Km
  Typical unfilled epoxy (Hysol 9396), K = 0.2 W/m*K
  Baseline filler for most of our applications is micron-sized BN, which gets you to K ~ 1.1 W/m*K at 20-30% mass fraction
    easy to use, safe, gives nice viscosity
  Another typical filled material is SE4445, with K = 1.25 W/m*K
    frequently used to mount Si modules
    proprietary filler, Dow material

## Slide 13: There’s been a lot of activity recently on finding new fillers for resins, to enhance K
We should be able to reliably get above ~1.5 W/m*K in practice with Hysol.
3 W/m*K is about the conceivable limit.
(and “nano” was not magical)

## Slide 14: Thermal conductivity is important, but filled adhesives still need to be used as adhesives
  Here is a nicely-spreadable typical BN-filled epoxy.

## Slide 15: Here is an example of an unusable mixture.

## Slide 16: A lower viscosity resin allows more filler, and perhaps better exfoliation / distribution
  This also highlights the importance of mixing quality.
  A mixing machine with 2 spin axes (centrifugal + local) is an essential piece of equipment.
Sample
‘too conductive’
To measure

## Slide 17: Thermal modeling is about intimate investigation of the materials and interfaces
  Interfaces must be modeled discretely
  K is often fabrication process-dependent
  Testing properties and validating FEAs is generally not-so-simple:
    accuracy and cross-calibration of temperature sensors
    thermal interfaces to temperature sensors
    thermal interfaces to heat sources
    natural convection or other losses
    cost of producing many samples
    variability of samples
    combining thermal and mechanical
    plumbing is required
  It takes a lot of iteration.
  A good IR camera is really helpful.