## Slide 1: Status of CCT at PSI
D. Arbelaez (LBNL), B. Auchmann (CERN/PSI), A. Brem (PSI), L. Brouwer (LBNL), S. Caspi (LBNL), M. Daly (PSI), M. Dhallé (UTwente), C. Hug (PSI), A. Kario (UTwente), G. Montenero (PSI), S. Otten (UTwente), S. Sidorov (PSI), H. ten Kate (UTwente), D. Tommasini (CERN)
1. March, 2021, US MDP Annual Meeting
Work supported by the Swiss State Secretariat for Education, Research and Innovation SERI.

## Slide 2: Overview
MagDev
CHART1 FCC Conceptual Design and CD1
CHART2 MagDev Goals
BOX Program
Summary

## Slide 3: Overview
MagDev
CHART1 FCC Conceptual Design and CD1
CHART2 MagDev Goals
BOX Program
Summary

## Slide 4: CHART1 Goals
CHART1 goals (mid-2016 to mid-2019) :
  the design of an optimised 16 T Canted Cosine Theta (CCT) dipole magnet, as an option for the FCC hadron collider main magnet;
  the development (design and prototype) of a high-field dipole magnet with CCT technology; and
[B. Auchmann et al., Electromechanical Design of a 16-T CCT Twin-Aperture Dipole for FCC, IEEE Trans. on Appl. SC 28 (April, 2018) no. 3.]
[M. Benedikt et al., FCC Conceptual Design Report, Vol. 3 – The Hadron Collider (FCC-hh), pp. 50-52, submitted to Eur. Phys. J. ST, (December 2018).]

## Slide 5: CHART1 Goals
CHART1 goals (mid-2016 to mid-2019):
  the design of an optimised 16 T Canted Cosine Theta (CCT) dipole magnet, as an option for the FCC hadron collider main magnet;
  the development (design and prototype) of a high-field dipole magnet with CCT technology; and
[G. Montenero et al., Coil Manufacturing Process of the First 1-m-Long Canted-Cosine-Theta (CCT) Model Magnet at PSI, IEEE Trans. on App. SC., Vol 29(5), 2019.] [G. Montenero et al., Mechanical Structure for the PSI Canted-Cosine-Theta (CCT) Magnet Program, IEEE Trans. on Appl. SC., Vol 28(3), 2018.]

## Slide 6: CHART1 MagDev Lab
90 m2 laboratory refurbished, equipped, commissioned for construction of CD1.
Production-readiness review (http://indico.psi.ch/event/cd1prr).
Vacuum Impregnation
Coil reaction
Portal crane
4-m winding/instrum/assembly bench
Winding table
Storage

## Slide 7: CD1 Construction

## Slide 8: Shipping Odyssey
CD1 construction was finished in Oct. 2019.
The magnet arrived (after problems in transit) in Feb. 2020.

## Slide 9: CD1 in Berkeley
The test preparation was interrupted by COVID 19 and resumed in Aug. 2020.
Magnet test started in Sept. 2020 but interrupted by cryo problem.
Max. current after 2 quenches: 11.1 kA or 62.5% of short sample, 6 T in the bore.
PSI has built a magnet (no more and no less can be said at this stage).
LBNL has provided technology transfer, and support, as well as test and -preparation. We cannot thank the LBNL team enough for their generous support and collaboration.
Courtesy D. Arbelaez, LBNL.
CD1

## Slide 10: Challenges Identified on CD1
CCT-inherent technological challenges:
  bonding of cable in winding channels.
  reliable insulation.
FCC-parameter specific challenges:
  winding and annealing on small diameter.
  plastic deformation of thin mandrel at 665ºC.
[Cable-channel delamination in CCT5 after testing. Photo courtesy of LBNL]
 | CD1 | CCT5
ID | 63.6 mm | 90 mm
Spar | 3/2 mm | 7.4/3 mm
Layer interface | Sliding plane | Bend & Shim
Mechanical structure | Bladder & Key | Al shell
Resin | FSU Mix 61 | FSU Mix 61

## Slide 11: CCT4FCC Pros and Cons
Design:
  Mechanical support of each turn  reduced coil stress and avoidance of stress-induced degradation.
  Easy field quality (on paper).
  Ideally suited for LTS/HTS hybrid magnets due to easy stacking of heterogeneous layers.
  Simpler external mechanical structure  more iron between the apertures and better magnetic separation  less cross-talk.
  Hope to fix training: getting one turn “right”, the entire magnet would work; no discontinuities towards the end regions
Fabrication:
  Simple and safe coil-manufacturing process; little tooling needed; coil always protected by former.
Instrumentation and protection:
  Efficient CLIQ protection as every turn is a high-field turn.
  Co-winding of instrumentation (fibers, wires, etc.) is supposedly easy.
Design:
  Every turn must be glued to metal surfaces; delamination would preclude good performance.
  Reduced efficiency by winding angle, rib thickness, and spar thickness.
  Check FQ variation along z-axis due to lack of control on turn position.
  Some axial strain on cable in every turn.
  No radial pre-compression possible.
Fabrication:
  Tricky winding on small ID with wide cable.
  Difficult to obtain reliable insulation.
  Difficult to keep cable in groove on small IDs.
  Interplay between former and cable during reaction.
Instrumentation and protection
  No heater protection possible.
Scaleup:
  Involved former manufacturing; cost and time consuming; difficult to scale to 15 m.
  Difficult assembly for long magnets – assembly gaps reduce performance.

## Slide 12: Overview
MagDev
CHART1 FCC Conceptual Design and CD1
CHART2 MagDev Goals
BOX Program
Summary

## Slide 13: CHART MagDev Embedded Timeline
2020
2021
2022
2023
2024
2025
2026
2027
CHART3
CHART2
CHART1
Enabling Technologies
Infrastructure
LTS Magnt R&D
HTS Magnt R&D
Welding Press
MagDev Lab, CF Test Station Upgrade
Furnace, VI
Improved Testing
Resins and constitutive modeling
Sizing, Curing, Coil composite analysis
Interfaces Bonding, Sliding
Processes
CD1
BOX Program
SM Collaboration US-MDP
HFM Concept Study
Tech. Coil
Tech. Coil
Tech. Coil
SuperBend Technology Demo
HFM CableTech
HTS Feasibility Study
16 T Technology Program
20 T Technology Program
Subscale sample manufacturing
ESPP Update
ESPP Update

## Slide 14: MagDev Laboratory and Team
Christoph Hug Technician
Michael Daly LTS, BOX
André Brem
Materials
Jaap Kosse
REBCO
Dariusz Pullikowksi
LTS, starting June
HTS Winding
LTS Winding
Assembly, Loading, Metrology
Heat Treatment
Impregnation

## Slide 15: Overview
MagDev
CHART1 FCC Conceptual Design and CD1
CHART2 MagDev Goals
BOX Program
Summary

## Slide 16: BOX Concept
MagDev1 conceived the below BOnding eXperiment (BOX) to test technological solutions to the bonding problem.
University of Twente tests the BOX samples with a SC transformer in up to 11 T background field.
For the CCT cable, the maximum pull-out force is reached with 7.5 T background field.
Courtesy M. Daly et al.

## Slide 17: BOX1 & 2
BOX1 and BOX2 were produced at PSI and tested U-Twente as a proof of concept and baseline for future improvements.
Acoustic sensors with cryogenic pre-amplifiers have been built and successfully deployed at PSI following LBNL design with support from Maxim – many thanks!
The BOX is a true fast-turnaround R&D platform:
  Material cost per BOX is < 1 kCHF, and test cost is ~ 5 kCHF.
  Manufacturing of a standard BOX takes ~ 2 weeks.
    More innovative BOXes require process R&D.
BOX1
BOX2
Accoustic sensors with (left) and without (right) cryoamplyfier.
BOX1 mounted on SC transformer
Courtesy M. Daly, C. Hug, A Kario, S. Otten, et al.

## Slide 18: BOX Powering
Powering and accoustic signals during a typical test.
Current ramp-up
(200 A/s)
Quench !
Current discharge
Primary ramp-down + cool down +
]preparation for next ramp-up (10mins)
Current ramp
Acoustics
Vtaps
Courtesy M. Daly, C. Hug, A Kario, S. Otten, et al.

## Slide 19: BOX1 & 2 Results
Consistent training in BOXes 1 and 2.
All sample segments see quenches. No quenches in leads.
Current direction
8
7
6
5
4
3
2
1
Vtap flags
AE Sensor
Magnetic Field
BOX 1
BOX 2
Courtesy M. Daly, C. Hug, A Kario, S. Otten, et al.

## Slide 20: BOX1 Post Mortem
Courtesy M. Daly, C. Hug, et al.
[Cable-channel delamination in CCT5 after testing. Photo courtesy of D. Arbelaez]
Initial microscopy and dye penetrant test appears to confirm debonding and cracking as main causes for quenches.
Additional analyses are under way.

## Slide 21: BOX3 and Outlook
BOX3 is a ”cleaner” version of BOX2
  sandblasted channel walls, ultrasound cleaned cable (following FSU advice), and air+heat cleaned glass insulation layer.
Performance to 90% of loadline was much improved.
BOX 3 recorded V-I transitions at background fields of 7.5 T and 10 T.
BOXes at uTwente, ready for testing:
  anodized-Al, CTD101K Nb-Ti (MQM cable)
  Shlomo BOX (non-impregnated NB3Sn)
  Paraphine wax impregnated NB3Sn.
Next BOXes in the pipline:
  anodized-Al, MY750 Nb-Ti (MQM cable).
  anodized-Al, Stycast Nb-Ti (filling tests under way).
  Alumina-coated bear-cable NB3Sn with Stycast or MY750 (filling and coating tests under way).
  Ultimate cleaning version of BOX1-3. (studies for O2 + heat cleaning, acid or base cleaning under way).
  Mullite+TiO slurry + Mix61 for a pre-filled system (thanks for Tengming for providing material).
BOXes 3-6 arrive arrive at uTwente. Courtesy of S. Otten and A. Kario

## Slide 22: Overview
MagDev
CHART1 FCC Conceptual Design and CD1
CHART2 MagDev Goals
BOX Program
Summary

## Slide 23: Summary
Besides the MagDev LTS program, there are other CHART ASC activities:
  MagDev has an HTS REBCO tape program, initially focused on demonstrating NI technology for an SLS2.0 superbend magnet, in collaboration with Tokamak Energy Ltd.
  Nb3Sn conductor characterization and development is carried out at UniGE,
  MagRes at ETHZ studies resin systems ,
  MagAM at ETHZ studies additive manufacturing of interpenetrating phase layers for reliable bonding to 3D printed parts,
  MagDev at PSI studies reaction residues, heat-resistant coatings, 10-stack properties, manufacturing processes, etc.
  MagNum at ETHZ, pending approval, shall produce a framework for sustainable multiphysical model development and design.
In parallel to the BOX program, and awaiting futher results from CD1, we are working (with G. Vallone) on an alternative proposal for a CHART MagDev 16-T Nb3Sn roadmap. A decision point is expected by the end of this year. We foresee to consult US-MDP for feedback in the process.
Independent of the next Nb3Sn coil type that will be built at PSI, the BOX program will continue and shall produce relevant technology R&D for, among others, the stress-management R&D roadmap in US-MDP at LBNL and FNAL.