## Slide 1: Modeling the stability of high-Cp Nb3Sn in context of other magnet conductors
Daniel S. Davis, Ulf P. Trociewitz, David C. Larbalestier
Applied Superconductivity Center - National High Magnetic Field Laboratory, Tallahassee, FL, USA
Thanks to DOE-OHEP support, the MagLab Core Grant support from NSF, the State of Florida
and the US Magnet Development Program Collaboration.
MDP Collaboration Meeting
March 2021

## Slide 2: Margin, Stability, and Current Sharing…
Margin: volumetric enthalpy [mJ/cm3] and local temperature change [K] at which deposited energy in the conductor causes some or all the transport current to generate Ohmic heating
Stability: How hard it is for small heat disturbances to generate propagating normal zones. Requires locally overcoming the margin and cooling vs Ohmic heating balance. Stability also refers to how much high conductivity normal metal is available for the current density shifting out of the superconductor.
Current Sharing: When the operating current exceeds IC(B,T) some, but not all of the current is carried in the normal metal stabilizer. The current balance is inherently dynamic, with IC(B,T), ρsc(I, T) and ρmetal(T) varying as Ohmic heating changes the temperature, but the relative impact of this behavior depends upon the critical temperature and margin (TC-TCS), stabilizer current density (1-fsc), and stabilizer resistivity (RRR).
Specific Heat Capacity, → Integrated to get enthalpy e(T)[J/m3]
Enthalpy margin is e(TC or TCS) – e(Top)
Temperature margin is (TC or TCS) - Top

## Slide 3: Nb3Sn margin is limited by field and Cu fraction, current sharing is limited by TC
A deposited heat of eCS will generate dissipation and current sharing until fully normal for eq deposited
  Current sharing region ~5x larger for HTS (970 mJ) than LTS (180 mJ) at 10 T
Bi-2212 eCS at 30 T (or eq at 40 T) same as Nb3Sn at 20 T
An order of magnitude drop in margin from 5 T to 30 T for Bi2212 for quench margin
10,000
0
0.25
0.5
0.75
0
0.25
0.5
0.75
Increasing Current
Specific Heat Capacity → Integrated to get enthalpy
{common form of data fit}
Enthalpy to Quench {TC}
Enthalpy to Current Sharing {TCS}
Current Sharing Temperature
{linear dependence is common}
Nb3Sn
Bi-2212
Cu
Nb-Ti
Nb3Sn
Bi-2212

## Slide 4: Bi-2212 is Like a Higher Field Nb3Sn with More Current Sharing
10,000
0
0.25
0.5
0.75
0
0.25
0.5
0.75
Increasing Current
Nb3Sn
Bi-2212
L. Bottura, “Margin, Stability and Quench Models and Simulation,” presented at the 1st International School on Numerical Modeling for Applied Superconductivity, Lausanne, Switzerland, 23-Jun-2016.
A deposited heat of eCS will generate dissipation and current sharing until fully normal for eq deposited
  Current sharing region ~5x larger for HTS (970 mJ) than LTS (180 mJ) at 10 T
Bi-2212 eCS at 30 T (or eq at 40 T) same as Nb3Sn at 20 T
An order of magnitude drop in margin from 5 T to 30 T for Bi2212 for quench margin
Nb-Ti
Nb3Sn
Bi-2212
Specific Heat Capacity → Integrated to get enthalpy
{common form of data fit}
Enthalpy to Quench {TC}
Enthalpy to Current Sharing {TCS}
Current Sharing Temperature
{linear dependence is common}

## Slide 5: Bi-2212 is Like a Higher Field Nb3Sn with More Current Sharing
10,000
0
0.25
0.5
0.75
0
0.25
0.5
0.75
Increasing Current
Nb3Sn
Bi-2212
L. Bottura, “Margin, Stability and Quench Models and Simulation,” presented at the 1st International School on Numerical Modeling for Applied Superconductivity, Lausanne, Switzerland, 23-Jun-2016.
Below Bi-2212 Margin
A deposited heat of eCS will generate dissipation and current sharing until fully normal for eq deposited
  Current sharing region ~5x larger for HTS (970 mJ) than LTS (180 mJ) at 10 T
Bi-2212 eCS at 30 T (or eq at 40 T) same as Nb3Sn at 20 T
An order of magnitude drop in margin from 5 T to 30 T for Bi2212 for quench margin
Always ramp LTS first to lower margin on HTS
Specific Heat Capacity → Integrated to get enthalpy
{common form of data fit}
Enthalpy to Quench {TC}
Enthalpy to Current Sharing {TCS}
Current Sharing Temperature
{linear dependence is common}

## Slide 6: Nb3Sn and high Cp Nb3Sn modelled IC(B,T,ε) Fit
ESE Spreadsheet - Ian Pong and Jack Ekin v2.1
  Replicated model and fit parameters into margin calculation
As a comparable modern wire, I chose a Larp QXF conductor,
  0.85 mm, 108/127
  IC(12 T) =674 A
J. W. Ekin, N. Cheggour, L. Goodrich, J. Splett, B. Bordini, D. Richter, and L. Bottura, "Extrapolative Scaling Expression: A fitting equation for extrapolating full IC(B,T,ε) data matrixes from limited data", Applied Superconductivity Conference 2016, IEEE Trans. Appl. Supercond., vol. 27, no. 4, Art. no. 8400607, June 2017.

## Slide 7: Calculation Inputs
Rule of mixtures for specific heat capacity
Figure 5. Measured specific heat of Gd2O3 [18].
X. Xu, A. V. Zlobin, E. Barzi – Fermilab; C. Buehler, M. Field, B. Sailer, M. Wanior, H. Miao – Bruker EST; C. Tarantini – Florida State University. “Enhancing specific heat of Nb3Sn conductors to improve stability and reduce training”. Presented at CEC-ICMC 2019
 | Density [g/cm^3]
Nb3Sn | 8.95
Bi-2212 | 6.6
Ag | 10.49
Cu | 8.94
  ~4.12% Area fraction Gd2O3 elements
  1% and 10% also run for comparison

## Slide 8: 4 % High Cp Nb3Sn additions provide a moderate boost to the margin
High Cp in Nb3Sn magnets development
Helps utilization of JC
Does not decrease stabilizer current density at the same current
Addresses disturbance spectrum
Does not increase current sharing region to as much as Bi-2212 (higher TC)
Strongest impact at high current fraction i=Iop/IC
Nb3Sn
Bi2212
Nb-Ti
Points for 4% Gd2O3
X. Xu, A. V. Zlobin, E. Barzi – Fermilab; C. Buehler, M. Field, B. Sailer, M. Wanior, H. Miao – Bruker EST; C. Tarantini – Florida State University.
“Enhancing specific heat of Nb3Sn conductors to improve stability and reduce training.“ Presented at CEC-ICMC 2019
High field extrapolated from 16T high Cp data
i=
0
0.25
0.5
0.75
0
0.25
0.5
0.75
Increasing Current

## Slide 9: 10 % High Cp Nb3Sn additions would help close the gap between Nb3Sn and Bi-2212
High Cp in Nb3Sn magnets development
Nb3Sn
Bi2212
Nb-Ti
Points for 10% Gd2O3
X. Xu, A. V. Zlobin, E. Barzi – Fermilab; C. Buehler, M. Field, B. Sailer, M. Wanior, H. Miao – Bruker EST; C. Tarantini – Florida State University.
“Enhancing specific heat of Nb3Sn conductors to improve stability and reduce training.“ Presented at CEC-ICMC 2019
High field extrapolated from 16T high Cp data
i=
0
0.25
0.5
0.75
0
0.25
0.5
0.75
Increasing Current
Helps utilization of JC
Does not decrease stabilizer current density at the same current
Addresses disturbance spectrum
Does not increase current sharing region to as much as Bi-2212 (higher TC)

## Slide 10: Comparison with MQE data
L. Bottura, “Margin, Stability and Quench Models and Simulation,” presented at the 1st International School on Numerical Modeling for Applied Superconductivity, Lausanne, Switzerland, 23-Jun-2016.
4% Gd2O3
10% Gd2O3
[1]E. Barzi, F. Berritta, D. Turrioni, and A. V. Zlobin, “Heat Diffusion in High-Cp Nb3Sn Composite Superconducting Wires,” Instruments, vol. 4, no. 4, p. 28, Sep. 2020, doi: 10.3390/instruments4040028.

## Slide 11: Stability is a mix of margin and stabilizer area fraction
  (compare to low-stability but huge margin of single-strand YBCO)
  Bi-2212 (PMM170123), 0.8 mm IC(4.2K,5T) = 600 A (1193 A/mm2); superconducting fraction fsc=0.25
    Ag fraction 75% (newest Engimat wires closer to 80% Ag)
  Nb3Sn –LARP QXF conductor, 0.85 mm, 108/127, IC(4.2K,12T)= 674 A. RRR>150
    Cu fraction >52.4%,
    High Cp, assume reduction in Cu fraction by 4% to 48.4%
  Example Cases:
  Same Margin, Practical Fields: The enthalpy margin of both conductors is 15.8 mJ/cm3 for Nb3Sn at 10 T, Bi2212 at 15.53 T, and high Cp Nb3Sn at 17.16 T
    Bi-2212 at 0.75*IC (4.2 K, 15.53 T)(319 A) the Ag stabilizer current density is 847 A/mm2
    Nb3Sn at 0.75*IC (4.2 K, 10 T)(750 A) the Cu stabilizer current density is 2521 A/mm2
    High Cp at 0.75*IC (4.2 K, 17.16 T)(143 A) the Cu stabilizer current density is 520 A/mm2
  Same field as previous Nb3Sn (10 T), same current as that for Bi-2212 at 10 T
    High Cp at 0.75*IC (4.2 K, 10 T)(750 A) the Cu stabilizer current density is 2730 A/mm2
    Bi-2212 at 0.75*IC (4.2 K, 10 T)(370 A) the Ag stabilizer current density is 981 A/mm2
    Nb3Sn at 0.75*IC (4.2 K, 13.5 T)(368 A) the Cu stabilizer current density is 1239 A/mm2
    High Cp at 0.75*IC (4.2 K, 13.5 T)(368 A) the Cu stabilizer current density is 1341 A/mm2
  Higher Fields: The enthalpy margin of both conductors is 5.1 mJ/cm3 for Nb3Sn at 20 T, Bi-2212 at 34.35 T, and high Cp Nb3Sn at 22.16 T
    Nb3Sn at 0.75*IC (4.2 K, 20 T)(48 A) the Cu stabilizer current density is 162 A/mm2
    Bi-2212 at 0.75*IC (4.2 K, 34.35 T)(228 A) the Ag stabilizer current density is 605.1 A/mm2
    High Cp at 0.75*IC (4.2 K, 22.16 T)(11.5 A) the Cu stabilizer current density is 41 A/mm2
  Bi-2212 has a higher stabilizer fraction of Ag rather than Cu, has a flat JE(B), combined with the higher enthalpy margin and slow normal zone propagation makes it more stable than Nb3Sn over a large field range up to 40 T or more low-stability but huge margin of single-strand YBCO)
Closer to Nb3Sn Bc2

## Slide 12: Extra time to protect for the same margin, from Tcs to Tc
In addition to larger margin from TCS to TC for HTS:
Slower heating through that transition
  Resistance rises progressively from TCS to TC :
    (lower index n-value of I-V transition)
      Property distribution, flux creep, multifilament & multistrand & high RRR Ag matrix current sharing
  Less ohmic heat will be generated near TCS than near TC
  This allows more stable operation near TCS
Higher MQE, slower normal zone propagation
Ohmic Heating
T
Tc
LTS
HTS
Tcs
Imatrix
Imagnet/IC
1
LTS
HTS
Notes: Another layer of complexity in HTS is the broad V-I transition with a low power-law index or n-value, which results in superconductor/stabilizer current sharing well beyond the critical current.
The delayed stabilizer current rise reduces the integrated Ohmic heating, increasing the minimum quench energy and slowing the normal zone propagation.
This results in more stable operation near the current sharing temperature even for minimal cooling

## Slide 13: Can we find a stable balance between LTS and HTS?

## Slide 14
Extra Slides

## Slide 15: 1% High Cp Nb3Sn additions provide a moderate boost to the margin
High Cp in Nb3Sn magnets development
Helps utilization of JC
Does not decrease stabilizer current density
Addresses disturbance spectrum
Does not increase current sharing region to as much as Bi-2212 (higher TC)
Nb3Sn
Bi2212
Nb-Ti
High field extrapolated from 16T high Cp data
Points for 1% Gd2O3
X. Xu, A. V. Zlobin, E. Barzi – Fermilab; C. Buehler, M. Field, B. Sailer, M. Wanior, H. Miao – Bruker EST; C. Tarantini – Florida State University.
“Enhancing specific heat of Nb3Sn conductors to improve stability and reduce training.“ Presented at CEC-ICMC 2019
i=
0
0.25
0.5
0.75
0
0.25
0.5
0.75
Increasing Current

## Slide 16: We have only observed two types of quench limitations in Bi-2212 Coils. Can high Cp Nb3Sn behave similarly?
Broad V-I Transitions
Power-Law V-I voltages clear at 80% or less of quench current
Quench currents can be slightly increased with faster ramp rates
  Low AC losses & NZPV so outrun thermal run-away
Quench currents follow S.S. IC(B) trend
  Only small, saturating (<5%), drops in IQ
Quench detection and protection less challenging
Local degradation/low-IC
Characterized by rapid high n-value transition.
  Short length normal zone
Quench currents following are the same or lower
  Combination of Lorentz force induced mechanical or fabrication/processing degradation (mitigation: OPHT witness samples, Fabrication R&D of RC-program)
Field dependence is more rapid than S.S. IC(B)
Protection challenging, but degradation precedes quench.
Only need to focus on LTS initiated quenches
If below operation current: new coil. Else, focus on LTS initiated quenches
Neither case requires training