## Slide 1: MDP Collaboration Meeting 20 T hybrid magnet and comparative analysis
P. Ferracin
US Magnet Development Program

## Slide 2: Outline
General organization of working group
Goals of working group
Design criteria for a 20 T hybrid magnets
Analytical estimates of general dimensions and stresses
  Thick shell with cos-theta current distribution
Preliminary magnetic analysis
  CT, SMCT, CCT
  Block, Common-coil
Next plans and conclusions

## Slide 3: General organization of working group
Members
  LBNL: P. Ferracin
  FNAL: G. Ambrosio, E. Barzi, V. Kashikhin, V. Marinozzi, I. Novitski, A. Zlobin
  NHMFL: L. Cooley
  BNL: R. Gupta, B. Yahia
Contributions from
  Diego Arbelaez and Lucas Brower (LBNL)
  Etienne Rochepault (CEA)
  Jillien Stern (TUFTS University, Prof. Luisa Chiesa)

## Slide 4: General organization of working group

## Slide 5: Outline
Goals of the working group
Model and assumptions
Estimates of radiuses, dimensions, and stresses
  Bi2212 and REBCO cases
Preliminary cos-theta and common coil cross-sections
Appendix
  Design criteria for a 20 T hybrid magnet
  Details of REBCO case

## Slide 6: Goals of the working group
Conceptual design of a 20 T hybrid HTS-LTS magnet
  Comparative analysis of different design options for a 20 T hybrid
    Cos design and its stress-management options
      “Traditional” Cos
      Canted Cos (CCT)
      Stress management Cos (SMCT)
    Block-type coil design (block with flared ends)
    Common-coil design (block with racetrack coil)
  Definition of general design criteria: aperture, field, margin…..
  Analysis of challenges specifically of hybrid magnets
    Integration of LTS/HTS, mechanics, protection, powering, diagnostics, test facility…..
Review and follow-up of current work on hybrid magnets
  Collect and organize information from these programs (responsibility of area I and area II) to provide inputs for 20 T hybrid design

## Slide 7: Goals of the working group (from the updated roadmap)

## Slide 8: Snowmass LOI

## Slide 9: Design criteria for a 20 T hybrid magnet
Previous work within MDP on a 16 T dipole magnet
  GianLuca Sabbi, Alexander Zlobin, MDP General meeting – May 17, 2017
https://conferences.lbl.gov/event/82/

## Slide 10: Design criteria for a 20 T hybrid magnet
Geometrical
  Number of apertures 1
  Free coil aperture 50 mm
Comments
  The common coils will naturally provide 2 apertures
    This will be taken into account on the comparison
  No “strong” constraints on
    Magnet total length (<2 m)
    Magnet straight section (>200 mm)
    Maximum magnet OD
      Reference numbers: 620 mm (FNAL/1.9K), 660 mm (BNL/1.9K), 914 mm (LBNL/4.5K)

## Slide 11: Design criteria for a 20 T hybrid magnet
Operational
  Reference temperature 1.9 K
    4.5 K option can be considered: it would impact the ratio of HTS vs LTS
  Operational bore field 20 T
  Margin on the load-line @ 1.9K >= 15 %
    With respect to round strand Ic including self field and 5% cabling degradation
  Short sample bore field 23.5 T
  Geometrical harmonics at Rref=17 mm and 20 T: bn<5 for n<10
    Magnet straight section
  Target design field 20 T

## Slide 12: Design criteria for a 20 T hybrid magnet
Operational
  Maximum Nb3Sn coil stress >180 (<150) MPa at 1.9 (293) K
  Conditions of coil-pole or rib interfaces at 20 T
    If bonded 20 MPa max. tension
      ‘Corner spikes’ (~1 contact element, 1 mm) neglected
    If separation allowed: Half cable width in contact or < 50 µm max gap
      Conditions may be different depending on the design

## Slide 13: Design criteria for a 20 T hybrid magnet
Bonded vs separation-allowed
  Test Facility Dipole (by G. Vallone)

## Slide 14: Design criteria for a 20 T hybrid magnet
Bonded vs separation-allowed
  MQXF (by G. Vallone)

## Slide 15: Material limits (by Giorgio Vallone)

## Slide 16: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  Strand diameter 0.7-1.2 mm
  Cu:non-Cu ratio 0.8-2.0
  Non-Cu Jc round strand with self-field
    12 T, 4.2 K 2980 A/mm2
    15 T, 4.2 K 1640 A/mm2
    16 T, 4.2 K 1250 A/mm2
      See next slide for reference fit
  RRR (after cabling) >50
  Ic degradation due to cabling 5%
  Maximum number of strands in cable 60
  Cable Insulation thickness 0.150 mm

## Slide 17: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  Reference Jc(B,T) fit:
  , ,
    where 𝑡=𝑇/𝑇c0; 𝑏=𝐵p/𝐵c2 (𝑡), Bp is the conductor peak field, Tc0 = 16 K, Bc20 =29.77 T, C0 = 223900 T.A/mm2.
  Fit of data from recent (03/2020) RRP 108/127, 1.1 mm diameter, 1.1 Cu/non-Cu

## Slide 18: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  “3000” A/mm2 kind of conductor, round, with self field
Jc round
Jc , 5% deg.
Je , 5% deg.

## Slide 19: Design criteria for a 20 T hybrid magnet
Nb3Sn Conductor and cable
  In general, it would be better to stay within already tested parameters (min, max)
Dimension before reaction; In MQXF, assumed expansion during reaction is 4.5 % (th), 1.2 % (w)

## Slide 20: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable (input from T. Shen and L. Garcia Fajardo)
  The wire diameter:
    from 0.6 mm to 1.5 mm
  Cable width: basically same possibilities as with Nb3Sn cables

## Slide 21: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable (input from T. Shen and L. Garcia Fajardo)
  Record performance strand RC5/6 about 20% higher than what is currently “comfortably” produced.

## Slide 22: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable (input from T. Shen and L. Garcia Fajardo)

## Slide 23: Design criteria for a 20 T hybrid magnet
Bi2212 Conductor and cable
  Maximum Nb3Sn coil stress: <120 MPa (293) K

## Slide 24: Design criteria for a 20 T hybrid magnet
REBCO Conductor
  CORC cable
    3.42mm diameter including 30 micron thick insulation.
  STAR cable
    1.3 mm diameter without insulation (#3)
    2.04 mm diameter without insulation (#4)

## Slide 25: Design criteria for a 20 T hybrid magnet
REBCO Conductor
  We use the following parameterization
    Ic(B, 4.2 K) = 10^(*log(B)+c)
  Where

## Slide 26: Design criteria for a 20 T hybrid magnet
REBCO Conductor
  Stress degradation

## Slide 27: Design criteria for a 20 T hybrid magnet
With properties describe above
  Nb3Sn and Bi2212 cross at
    14.5 T at 4.2 K
    16.5 T at 1.9 K
  Nb3Sn and REBCO cross at
    15.0 T at 4.2 K
    17.5 T at 1.9 K

## Slide 28: Design criteria for a 20 T hybrid magnet
Quench protection
  Nb3Sn
    Maximum hot spot temperature 350 K
    Total time delay 40 ms
    Maximum J in the Cu 1350 A/mm2
    Maximum voltage to ground @ quench 1.0 kV
    Ground insulation design voltage >5 kV
  Bi2212 and REBCO
    See next slides
  Powering in series

## Slide 29: Design criteria for a 20 T hybrid magnet
Quench protection
  Bi2212: Tmax= 400-450 K

## Slide 30: Design criteria for a 20 T hybrid magnet
Quench protection
  REBCO

## Slide 31: Design criteria for a 20 T hybrid magnet
Summary on Hot spot temperature
  For all 3 materials, 350 K maximum hot spot temperature appears to be a reasonable value

## Slide 32: Outline
Goals of the working group
Model and assumptions
Estimates of radiuses, dimensions, and stresses
  Bi2212 and REBCO cases
Preliminary cos-theta and common coil cross-sections
Appendix
  Design criteria for a 20 T hybrid magnet
  Details of REBCO case

## Slide 33: Field in at 20 T hybrid dipole magnet
Bbore_op = 20 T with load-line margin of 15%  85% of Iss
  Same load-line margin for HTS and LTS
Bpeak_op = 20.8 T
  Assumption: 4% increase Bbore to Bpeak
Bbore_ss = 23.5 T
Bpeak_ss = 24.4 T
  Assumption: 4% increase Bbore to Bpeak

## Slide 34: “Sector coil” analytical model
Sector coil (60) with J = J0 distribution
  No iron
  Constant Jo
Definitions
  Jc = J in superconductor area
  Je = J in strand area
  Jo = J in coil area
MQXF/11T cable parameters
  Je = Jc * 0.48
  Jo = Je * 0.67
  Jo = Jc * 0.32
No grading
  Same current, same J everywhere
    As if HTS and LTS use the same cable, and are powered in series

## Slide 35: Outline
Goals of the working group
Model and assumptions
Estimates of radiuses, dimensions, and stresses
  Bi2212 and REBCO cases
Preliminary cos-theta and common coil cross-sections
Appendix
  Design criteria for a 20 T hybrid magnet
  Details of REBCO case

## Slide 36: Nb3Sn vs Bi2212
With properties describe in appendix, Nb3Sn and Bi2212 cross at 14.5 T at 4.2 K and 16.5 T at 1.9 K

## Slide 37: 20 T Bi2212-Nb3Sn hybrid
Bi2212
  At short sample
    Bp_ss = 24.4 T
    Je_ss = 670 A/mm2
    Jo_ss = 450 A/mm2
  So, at 85% of short sample
    Bp_op = 20.8 T
    Je_op = 570 A/mm2
    Jo_op = 382 A/mm2

## Slide 38: 20 T Bi2212-Nb3Sn hybrid
Nb3Sn
  At short sample
    Bp_ss = 17.3 T
    Je_ss = 670 A/mm2
    Jo_ss = 450 A/mm2
  So, at 85% of short sample
    Bp_op = 14.7 T
    Je_op = 570 A/mm2
    Jo_op = 382 A/mm2

## Slide 39: 20 T Bi2212-Nb3Sn hybrid
50 mm aperture
Under the previous assumption (sector coil, constant Jo everywhere, no stress management, no iron)
  ID Nb3Sn = 146 mm
  OD Nb3Sn = 200 mm
  76 m total coil thickness
    49 mm thick Bi2212 coil
    27 mm thick Nb3Sn coil
  Area Bi2212: 2540 mm2 (1 quadrant)
  Area Nb3Sn: 2470 mm2 (1 quadrant)
  Stored energy: 2.86 MJ/m (4 quadrants)
20 T = 13 T + 7 T
Bi2212
Nb3Sn

## Slide 40: 20 T Bi2212-Nb3Sn hybrid Stress at B-bore = 20 T
Azimuthal stress on the mid-plane  Max: 188 MPa
Radial stress  Max: 206 MPa
  No shear, no bending….
Azimuthal
Radial

## Slide 41: 20 T Bi2212-Nb3Sn hybrid Test separately the Nb3Sn and the Bi2212 coils
Bi2212
Nb3Sn
Bi2212
Bi2212
Nb3Sn
Nb3Sn
ID: 50 mm
OD: 146 mm
W: 49 mm
ID: 146 mm
OD: 200 mm
W: 27 mm
ID: 50 mm
OD: 200 mm
W: 76 mm

## Slide 42: 20 T Bi2212-Nb3Sn hybrid Bi2212 “only”
Bi2212
  At short sample
    Bp_ss = 18.4 T
    Bbore_ss = 17.4 T
    Je_ss = 769 A/mm2
    Jo_ss = 515 A/mm2
  So, at 85% of short sample
    Bp_op = 15.6 T
    Bbore_op = 14.7 T
    Je_op = 653 A/mm2
    Jo_op = 438 A/mm2

## Slide 43: 20 T Bi2212-Nb3Sn hybrid Bi2212 “only”, Stress at B-bore = 14.7 T
Azimuthal stress on the mid-plane  Max: 128 MPa
Radial stress  Max: 122 MPa
  No shear, no bending….
Azimuthal
Radial

## Slide 44: 20 T Bi2212-Nb3Sn hybrid Nb3Sn “only”
Nb3Sn
  At short sample
    Bp_ss = 15.3 T
    Bbore_ss = 12.1 T
    Je_ss = 985 A/mm2
    Jo_ss = 660 A/mm2
  So, at 85% of short sample
    Bp_op = 13.0 T
    Bbore_op = 10.3 T
    Je_op = 837 A/mm2
    Jo_op = 561 A/mm2

## Slide 45: 20 T Bi2212-Nb3Sn hybrid Nb3Sn “only”, Stress at B-bore = 10.3 T
Azimuthal stress on the mid-plane  Max: 232 MPa
Radial stress  Max: 77 MPa
  No shear, no bending….
Azimuthal
Radial

## Slide 46: Outline
Goals of the working group
Model and assumptions
Estimates of radiuses, dimensions, and stresses
  Bi2212 and REBCO cases
Preliminary cos-theta and common coil cross-sections
Appendix
  Design criteria for a 20 T hybrid magnet
  Details of REBCO case

## Slide 47: 20 T REBCO-Nb3Sn hybrid (work in progress…)
With properties describe in appendix
  Nb3Sn and Bi2212 cross at
    14.5 T at 4.2 K
    16.5 T at 1.9 K
  Nb3Sn and REBCO cross at
    15.0 T at 4.2 K
    17.5 T at 1.9 K

## Slide 48: 20 T REBCO-Nb3Sn hybrid
REBCO
  At short sample
    Bp_ss = 24.4 T
    Je_ss = 504 A/mm2
    Jo_ss = 338 A/mm2
  So, at 85% of short sample
    Bp_op = 20.8 T
    Je_op = 429 A/mm2
    Jo_op = 287 A/mm2

## Slide 49: 20 T REBCO-Nb3Sn hybrid
Nb3Sn
  At short sample
    Bp_ss = 18.7 T
    Je_ss = 504 A/mm2
    Jo_ss = 338 A/mm2
  So, at 85% of short sample
    Bp_op = 15.9 T
    Je_op = 429 A/mm2
    Jo_op = 287 A/mm2

## Slide 50: 20 T REBCO-Nb3Sn hybrid
50 mm aperture
Under the previous assumption (sector coil, constant Jo everywhere, no stress management, no iron)
And also, from CORC/STAR Je to Jo like in MQXF  “Rutherford cable with CORC/START wires” (see later)
  ID Nb3Sn = 144 mm
  OD Nb3Sn = 252 mm
  101 m total coil thickness
    47 mm thick REBCO coil
    54 mm thick Nb3Sn coil
  Area Bi2212: 2387 mm2 (1 quadrant)
  Area Nb3Sn: 5532 mm2 (1 quadrant)
  Stored energy: 3.92 MJ/m (4 quadrants)
20 T = 9 T + 11 T
REBCO
Nb3Sn

## Slide 51: 20 T REBCO-Nb3Sn hybrid Test separately the Nb3Sn and the Bi2212 coils
REBCO
Nb3Sn
REBCO
Nb3Sn
ID: 50 mm
OD: 144 mm
W: 47 mm
ID: 144 mm
OD: 252 mm
W: 54 mm
ID: 50 mm
OD: 252 mm
W: 101 mm

## Slide 52: Summary
ID: 50 mm
OD: 146 mm
W: 49 mm
B_bore_op = 14.7 T
/ r =128/122
ID: 146 mm
OD: 200 mm
W: 27 mm
B_bore_op = 10.3 T
/ r =232/77
ID: 50 mm
OD: 200 mm
W: 76 mm
B_bore_op = 20 T
/ r =188/206
ID: 50 mm
OD: 144 mm
W: 47 mm
B_bore_op = 12.8 T
/ r =99/93
ID: 144 mm
OD: 252 mm
W: 54 mm
B_bore_op = 13.1 T
/ r =201/114
ID: 50 mm
OD: 252 mm
W: 101 mm
B_bore_op B = 20 T
/ r =165/194
Bi2212
REBCO

## Slide 53: Summary
REBCO hybrid still larger than Bi2212
  Because of a lower Je
    And also with “unrealistic” assumption on Jo
We need to build a
  13-14 T HTS magnet (50 mm)
  10-13 T LTS magnet (large bore)
    120 mm seems a good start, but we may need more for an hybrid magnet
In hybrid 20 T, radial stress seems higher than azimuthal
  When tested separately, very high azimuthal stress in LTS

## Slide 54: Very…very…preliminary magnet size
20 mm collar
250 mm thick yoke
  However, for a single short model, higher stray field could be accepted
50 mm thick shell
  Fx/t = 200 MPa
OD: 850 mm

## Slide 55: Size comparison
LHC MQXF FRESCA2 ????

## Slide 56: Action items
Update thick shell analysis with iron (by J. Stern)

## Slide 57: CT- SMCT options
Summary

## Slide 58: CT option 4 HTS 2 LTS
v9b : 4 HTS 2 LTS
  increase cable LTS to 16 to reduce stress (right now 170 MPa)

## Slide 59: V9e: wider LTS conductor
v9e : 4 HTS 2 LTS
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 40 – 35 – 36
Cable width: 18.35 – 16.06 – 15.96 mm
Stabilizer/Superconductor: 3 – 3 – 1
Coil width: 105 mm
Current: 10920
Peak field: 20.48 – 15.88 – 12.53 T
Margin: 82.5 – 82.8 – 74.5 %
Jcu on LTS: 1206 A/mm2
Peak azimuthal Lorentz force: 151/142 MPa (LTS/HTS) (151/170 MPa in v9b)

## Slide 60: CT option 2 HTS 4 LTS
- v11: CT option with 2 HTS 4 LTS
  - Try with a larger HTS cable to increase margin
  - Optimize layer 3-4: try removing top blocks and larger cable

## Slide 61: V11b: larger HTS conductor
2 layer HTS, 4 layer LTS
Strands: 1.1/1.1/0.8 mm, 40 – 35 – 30
Cable width: 25.23 –21.3 – 13.3 mm
Stabilizer/Superconductor: 3 – 3 – 1
Coil width: 123 mm
Current: 14200
Peak field: 20.26 – 15.96 – 13.72 T
Margin: 66 – 86 – 89 %
Jcu on LTS: 1883 A/mm2
Peak azimuthal Lorentz force: 92/233 MPa (LTS/HTS)
I want to reduce layer 1 and 2 width, slightly increase layer 3-4, increase layer 5-6

## Slide 62: SMCT option 4 HTS 2 LTS
- v12: SMCT option with 4 HTS 2 LTS
  - Increase margin
  - Smaller ribs
  - Increase top angle
V12b: same but with mid-planes ribs
  - to be done with 2mm per side

## Slide 63: v12b
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 46 – 40 – 30
Cable width: 21.1 – 18.35– 13.3 mm
Stabilizer/Superconductor: 3 – 3 – 1.5
Coil width: 132 mm
Current: 11820 A
Peak field: 20.5 – 16.18 – 13.95 T
Margin: 79.5 – 80.2 – 85.8 %
Jcu on LTS: 1567 A/mm2
Increase layer 5-6 width?

## Slide 64: v12c: 2 mm rib on midplane
Bore field: 19.94 T

## Slide 65: Additional cases
- v13: SMCT option with 2 HTS 4 LTS
  - to be done
- v9b with only top blocks of layer 3-4 with HTS, the rest LTS (4-5 with lower angle to allow splice)

## Slide 66: CT preliminary design (D. Arbelaez)
6 layers, same cable
MQXF cable
With Iron
5 mm thick spars

## Slide 67: CT preliminary design (D. Arbelaez)

## Slide 68: CT preliminary design (D. Arbelaez)
Coil OR: 165 mm

## Slide 69: Block option

## Slide 70: Common-coil option
Designs to be updated

## Slide 71: Next plans and conclusions
Next plans and conclusions
Continue the analysis of each option until a complete design study is carried out
  Then, start with the comparison
    Comparison criteria to be further defined
Resources……
  A student/Post-doc available to work for a significant fraction of his/her time is strongly needed.

## Slide 72: Appendix
Design criteria
Details of REBCO case

## Slide 73: 20 T REBCO-Nb3Sn hybrid Stress at B-bore = 20 T
Azimuthal stress on the mid-plane  Max: 165 MPa
Radial stress  Max: 194 MPa
  No shear, no bending….
Azimuthal
Radial

## Slide 74: 20 T REBCO-Nb3Sn hybrid REBCO “only”
REBCO
  At short sample
    Bp_ss = 16.0 T
    Bbore_ss = 15.1 T
    Je_ss = 697 A/mm2
    Jo_ss = 467 A/mm2
  So, at 85% of short sample
    Bp_op = 13.6 T
    Bbore_op = 12.8 T
    Je_op = 592 A/mm2
    Jo_op = 397 A/mm2

## Slide 75: 20 T REBCO-Nb3Sn hybrid REBCO “only”, Stress at B-bore = 12.8 T
Azimuthal stress on the mid-plane  Max: 99 MPa
Radial stress  Max: 93 MPa
  No shear, no bending….
Azimuthal
Radial

## Slide 76: 20 T REBCO-Nb3Sn hybrid Nb3Sn “only”
Nb3Sn
  At short sample
    Bp_ss = 17.7 T
    Bbore_ss = 15.4 T
    Je_ss = 622 A/mm2
    Jo_ss = 417 A/mm2
  So, at 85% of short sample
    Bp_op = 15.0 T
    Bbore_op = 13.1 T
    Je_op = 529 A/mm2
    Jo_op = 354 A/mm2

## Slide 77: 20 T REBCO-Nb3Sn hybrid Nb3Sn “only”, Stress at B-bore = 13.1 T
Azimuthal stress on the mid-plane  Max: 201 MPa
Radial stress  Max: 114 MPa
  No shear, no bending….
Azimuthal
Radial