## Slide 1: Update on Costheta cross section
V. Marinozzi
04/20/2021

## Slide 2: Critical current
Jc in SC obtained by scaling Jc engineering from Paolo slides
Still using linear approximation in the peak field zone
Jc for Nb3Sn: 1928 A/mm2 @16 T, 1.9 K
Jc for Bi2212: 2944 A/mm2 @20 T, 1.9 K

## Slide 3: Iron yoke

## Slide 4: Baseline classic costheta (size optimized): v9e
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 40 – 35 – 36
Cable width: 18.35 – 16.06 – 15.96 mm
Stabilizer/Superconductor: 3 – 3 – 1
Coil width: 105 mm
Current: 10920
Peak field: 20.48 – 15.88 – 12.53 T
Margin: 82.5 – 82.8 – 74.5 %
Jcu on LTS: 1206 A/mm2
Peak azimuthal Lorentz force: 151/142 MPa (LTS/HTS)

## Slide 5: Baseline classic costheta (size optimized): v9f
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 40 – 35 – 30
Cable width: 18.35 – 16.06 – 13.3 mm
Stabilizer/Superconductor: 3 – 3 – 1
Coil width: 100 mm
Current: 11120
Peak field: 20.51 – 16.02 – 12.69 T
Margin: 83.4 – 84.1 – 75.5 %
Jcu on LTS: 1229 A/mm2
Peak azimuthal Lorentz force: 156/145 MPa (LTS/HTS)

## Slide 6: Baseline classic costheta (HTS optimized): v11b
2 layer HTS, 4 layer LTS
Strands: 1.1/1.1/0.8 mm, 40 – 35 – 30
Cable width: 25.23 –21.3 – 13.3 mm
Stabilizer/Superconductor: 3 – 3 – 1
Coil width: 104 mm
Current: 14200
Peak field: 20.26 – 15.96 – 13.72 T
Margin: 66 – 86 – 89 %
Jcu on LTS: 1883 A/mm2
Peak azimuthal Lorentz force: 92/233 MPa (LTS/HTS)

## Slide 7: Baseline classic costheta (HTS optimized): v11c
2 layer HTS, 4 layer LTS
Strands: 0.9/1.1/0.8 mm, 40 – 40– 36
Cable width: 20.65 –24.38 – 15.96 mm
Stabilizer/Superconductor: 3 – 1 – 1
Coil width: 126 mm
Current: 13610
Peak field: 20.41 – 16.01 – 12.3 T
Margin: 81.6 – 84.6 – 77 %
Jcu on LTS: 1504 A/mm2
Peak azimuthal Lorentz force: 105/171 MPa (LTS/HTS)

## Slide 8: SMCT-like with 5 mm rings: v12c
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 46 – 40 – 30
Cable width: 21.1 – 18.35– 13.3 mm
Stabilizer/Superconductor: 3 – 3 – 1
Coil width: 132 mm
Current: 11820 A
Peak field: 20.5 – 16.18 – 13.95 T
Margin: 79.5 – 80.2 – 85.8 %
Jcu on LTS: 1567 A/mm2

## Slide 9: SMCT-like with 5 mm rings: v12d
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 46 – 40 – 35
Cable width: 21.1 – 18.35– 15.51 mm
Stabilizer/Superconductor: 3 – 3 – 1
Coil width: 136 mm
Current: 12000 A
Peak field: 20.74 – 16.33 – 13.77 T
Margin: 80.6 – 81.3 – 82.3 %
Jcu on LTS: 1364 A/mm2

## Slide 10: Next steps
2 HTS + 4 HTS SMCT
Field quality
Quench protection studies

## Slide 11: Cross sections

## Slide 12: v2

## Slide 13: v3

## Slide 14: V4

## Slide 15: v5

## Slide 16: v6

## Slide 17: v8

## Slide 18: v9

## Slide 19: v10

## Slide 20: v11